Copyright 2000, The American Institute of Architects (AIA)

# SECTION 07115 - BITUMINOUS DAMPPROOFING

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

# PART 1 - GENERAL

1.1	RELATED DOCUMENTS

A.	Site drawings produced by Pinkham and Greer Consulting Engineers, foundation/basement plan drawings produced by TFH Architects PA and Structural Design Consulting, building drawings produced by TFH Architects, mechanical drawings produced by TFH Architects, electrical and lighting drawings produced by TFH Architects.  Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division 1 Specification Sections apply to all sections.

1.2	SUMMARY

A.	This Section includes the following:

Adjust list below to suit Project.

- Cold-applied, cutback asphalt damp proofing.

  - SUBMITTALS

A.      General:  Submit each item in this Article according to the Conditions of the Contract and Division 1 Specification Sections.

B.	Product Data:  For each type of product indicated.  Include recommendations for method of application, primer, number of coats, coverage or thickness, and protection course.

B.	Material Certificates:  For each product, signed by manufacturers.

1.4	QUALITY ASSURANCE

A.	Source Limitations:  Obtain primary damp proofing materials and primers through one source from a single manufacturer.  Provide secondary materials recommended by manufacturer of primary materials.

1.5	PROJECT CONDITIONS

Delete paragraph below if all applications are interior.

A.	Weather Limitations:  Proceed with installation only when existing and forecasted weather conditions permit asphalt damp proofing to be performed according to manufacturers' written instructions.

Delete below if no enclosed or interior applications are included in Project.

B.	Ventilation:  Provide adequate ventilation during application of damp proofing in enclosed spaces.  Maintain ventilation until damp proofing has thoroughly cured.

# PART 2 - PRODUCTS

# 2.1	MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

# A.	Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain above for nonproprietary or below for semiproprietary specification.  Refer to Division 1 Section "Product Requirements."

# B.	Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

1.	Cold-Applied, Cut-Back (Solvent-Based) Asphalt Damp proofing:

Before retaining manufacturers listed below, verify that their products comply with local VOC regulations, if any.

a.	Gardner Asphalt Corporation.

b.	Henry Company.

c.	Karnak Corporation.

d.	Koppers Industries, Inc.

e.	Malarkey Roofing Company.

f.	Meadows, W. R., Inc.

g.	Sonneborn, Div. of ChemRex, Inc.

h.	Tamms Industries.

# 2.2	BITUMINOUS DAMPPROOFING

Delete first paragraph below if no interior uses.  Add other general limitations as required.

Product in paragraph below is solvent based.  Delete if solvent release is not allowed.

A.	Cold-Applied, Cut-Back Asphalt Damp proofing:

Select one or both subparagraphs below; coordinate with applications selected in Part 3.

1.	Trowel Coats:  ASTM D 4586, Type I.

2.	Brush and Spray Coats:  ASTM D 4479, Type I.

Product in paragraph below is water based and generally contains little or no VOCs but may re-emulsify if any significant ground water is present.

# 2.3	MISCELLANEOUS MATERIALS

Product in paragraph below is solvent based.  Delete if solvent release is not allowed.

A.	Cut-Back Asphalt Primer:  ASTM D 41 or

Product in paragraph below is water based and generally contains little or no VOCs.  Product can be used with either cut-back or emulsion topcoats and is generally more tolerant of damp substrates than product above.

Retain first paragraph below if required for flashings and corner protection stripping at internal and external corners, changes in plane, construction joints, etc.

# PART 3 - EXECUTION

# 3.1	EXAMINATION

A.	Examine substrates, with Applicator present, for compliance with requirements for surface smoothness and other conditions affecting performance of work.

1.	Begin damp proofing application only after substrate construction and penetrating work have been completed and unsatisfactory conditions have been corrected.

# 3.2	PREPARATION

A.	Protection of Other Work:  Mask or otherwise protect adjoining exposed surfaces from being stained, spotted, or coated with damp proofing.  Prevent damp proofing materials from entering and clogging weep holes and drains.

B.	Clean substrates of projections and substances detrimental to work; fill voids, seal joints, and apply bond breakers if any, as recommended by prime material manufacturer.

# 3.3	APPLICATION, GENERAL

A.	Comply with manufacturer's written recommendations unless more stringent requirements are indicated or required by Project conditions to ensure satisfactory performance of damp proofing.

1.	Apply additional coats if recommended by manufacturer or required to achieve coverages indicated.

2.	Allow each coat of damp proofing to cure 24 hours before applying subsequent coats.

B.	Apply damp proofing to footings and foundation walls where opposite side of wall faces building basement interior whether indicated or not.

1.	Apply from finished-grade line to top of footing, extend over top of footing, and down a minimum of 6 inches (150 mm) over outside face of footing.

2.	Extend 12 inches (300 mm) onto intersecting walls and footings, but do not extend onto surfaces exposed to view when Project is completed.

Normally retain subparagraph below.  Corners are generally the weakest link in dampproofing protection.

3.	Install flashings and corner protection stripping at internal and external corners, changes in plane, construction joints, cracks, and where shown as "reinforced," by embedding an 8-inch- (200-mm-) wide strip of asphalt-coated glass fabric in a heavy coat of damp proofing.  Damp proofing coat required for embedding fabric is in addition to other coats required.

# 3.4	INSTALLATION OF PROTECTION COURSE

A.	Install protection courses if required by dampproofing installation recommendations.  Install protection course over completed-and-cured damp proofing.  Comply with damp proofing material manufacturer's written recommendations for attaching protection course.  Support protection course with spot application of trowel-grade mastic where not otherwise indicated.

# 3.5	CLEANING

A.	Remove damp proofing materials from surfaces not intended to receive damp proofing.

# END OF SECTION 07115