SECTION 09650 - RESILIENT FLOORING (Resilient Linoleum Sheet Flooring)

PART 1 GENERAL

1.1 	SUMMARY

A.	Section Includes: Resilient linoleum sheet flooring.

- Homogeneous linoleum sheet flooring, adhesive and heat welded seams installation.

B.	 Related Sections: Section(s) related to this section include:

  - Concrete: Refer to Division 3 Concrete Sections for cast-in-place concrete, concrete toppings, and cementitious underlayments.

  - Wood Subflooring: Refer to Division 6 Carpentry Section for wood subflooring and wood underlayment.

  - Resilient Flooring Accessories: Refer to Division 9 Finishes Sections for resilient wall bases, reducer strips, metal edge strips and other resilient flooring accessories.

1.2	 REFERENCES

A. 	American Society for Testing and Materials (ASTM):

- ASTM E 648-88 Test Method for Critical Radiant Flux of Floor Covering Systems Using a Radiant Energy Source.

- ASTM E 662-83 Test Method for Specific Density of Smoke Generated by Solid Materials.

- ASTM F 710-86 Practice for Preparing Concrete Floors and Other Monolithic Floors to Receive Resilient Flooring.

- ASTM F 970-87 Test Method for Static Load Limit.

1.3	SYSTEM DESCRIPTION

A.	Performance Requirements: Provide flooring which has been manufactured, fabricated and installed to performance criteria certified by manufacturer without defects, damage, or failure.

1.4	 SUBMITTALS

A. 	General: Submit listed submittals in accordance with "Conditions of the Contract" and Division 1 Submittal Procedures Section.

B. 	Product Data: Submit product data, including manufacturer's SPEC-DATA product sheet, for specified products.

C. 	Samples: Submit selection and verification samples for finishes, colors, and textures.

D. 	Quality Assurance Submittals: Submit the following:

- Certificates: Product certificates signed by manufacturer certifying materials comply with specified performance characteristics and criteria, and physical requirements.

- Manufacturer's Instructions: Manufacturer's installation instructions.

E.	 Closeout Submittals: Submit the following:

1.       Operation and Maintenance Data: Operation and maintenance data for installed products in accordance with Division 1 Closeout Submittals (Maintenance Data and Operation Data) Section. Include methods for maintaining installed products, and precautions against cleaning materials and methods detrimental to finishes and performance.

2.       Warranty: Warranty documents specified herein.

1.5 	QUALITY ASSURANCE

A.	 Installer Qualifications: Installer experienced in performing work of this section who has specialized in installation of work similar to that required for this project and whose work has resulted in construction with a record of successful in-service performance.

B.	 Regulatory Requirements:

1. 	Fire Performance Characteristics: Provide resilient linoleum sheet flooring with the following fire performance characteristics as determined by testing products in accordance with ASTM method indicated below by a certified testing laboratory or another testing and inspecting agency acceptable to authorities having jurisdiction:

a.	 Critical Radiant Flux: Class 1 Rating per NFPA 253 (ASTM 648) (0.45 watts/cm² or greater).
b.        Smoke Density: Less than 450 per NFPA 258 (ASTM E 662).

1.6 	DELIVERY, STORAGE, AND HANDLING

A. 	General: Comply with Division 1 Product Requirements Sections.

B.	Ordering: Comply with manufacturer's ordering instructions and lead time requirements to avoid construction delays.

C.	Delivery: Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

D.	Storage and Protection: Store materials protected from exposure to harmful weather conditions and at temperature and humidity conditions recommended by manufacturer.

1. 	Material should be stored in areas that are fully enclosed, weathertight with the permanent HVAC system set at a uniform temperature of at least 68 degrees F (20 degrees C) for 72 hrs. prior to, during and after installation.

1.7 	PROJECT CONDITIONS

A.	 Environmental Requirements/Conditions: In accordance with manufacturer's recommendations, Areas to receive flooring shall be clean, fully enclosed, weathertight with the permanent HVAC set at a uniform temperature of at least 68 degrees F. The flooring material should be conditioned in the same manner. Maximum temperature should not exceed 100 degrees F after installation.

B. 	Temperature Requirements: Maintain air temperature in spaces where products will be installed for time period before, during, and after installation as recommended by manufacturer.

1. 	Temperature Conditions: 68 degrees F (20 degrees C) for 72 hours prior to, during and after installation.

C. 	Field Measurements: Verify actual measurements/openings by field measurements before fabrication; show recorded measurements on shop drawings. Coordinate field measurements and fabrication schedule with construction progress to avoid construction delays.

1.8 	SEQUENCING AND SCHEDULING

A.	 Finishing Operations: Install tile flooring after finishing operations, including painting and ceiling operations, have been completed.

B.	 Concrete Curing: Do not install tile flooring over concrete substrates until substrates have cured and are dry to bond with adhesive as determined by resilient flooring manufacturer's recommended bond, moisture test, and pH test.

1.9	 WARRANTY

A.	 Project Warranty: Refer to "Conditions of the Contract" for project warranty provisions.

B.	 Manufacturer's Warranty: Submit, for Owner's acceptance, manufacturer's standard warranty document executed by authorized company official. Manufacturer's warranty is in addition to, and not a limitation of, other rights Owner may have under Contract Documents.

 1. 	Warranty Period: Five (5) year limited warranty commencing on Date of Substantial   Completion.

1.10 	MAINTENANCE

A.	Extra Materials: Deliver to Owner extra materials from same production run as products installed. Package products with protective covering and identify with descriptive labels. Comply with Division 1 Closeout Submittals (Maintenance Materials) Section.

1.	 Quantity: Furnish quantity of flooring units equal to 5% of amount installed.
2.	 Delivery, Storage and Protection: Comply with Owner's requirements for delivery, storage and protection of extra materials.

PART 2 - PRODUCTS

2.1	 RESILIENT LINOLEUM SHEET FLOORING

A.	 Manufacturer: Forbo Industries, Inc. or approved equal.

 1. 	Contact: Humboldt Industrial Park, P.O. Box 667, Hazleton, PA 18201; Telephone: 800 842 7839, 717 459 0771; Fax: 717 450 0258.

B. 	Proprietary Product(s):  Marmoleum Real/Marmoleum Fresco Linoleum Sheet and Linoleum Adhesive.

1. 	Description: Homogenous sheet linoleum of primarily natural materials consisting of linseed oil, wood flour and rosin binders, mixed and calendered onto natural jute backing.  Pattern and color shall extend throughout total thickness of material.

2.	 Width: 79" (2 Meters).
3. 	Length: 105 Linear Feet (32 Meters).
4. 	Gauge:  1/10" (2.5 MM).
5. 	Backing: Jute.
6. 	Pattern and Color: As selected by Architect from manufacturer's standard patterns and colors.
7. 	Adhesive: Forbo Industries, Inc., L910 Adhesive.
8. 	Heat Welding Rod: Artoweld color-matched welding rod.

C.	Product criteria forms:  Refer to product criteria forms as an attachment to this section.

1.	Product Forms:  Subject to compliance with specified requirements, provide products specified in each product data sheet at end of this section.

2.2 	PRODUCT SUBSTITUTIONS

A. 	Substitutions: Submit substitution product data and equivalency specifications with initial selection.

2.3 	RELATED MATERIALS

A. 	Related Materials: Refer to other sections for related materials as follows:

1. 	Underlayment and Patching Compound: Refer to Division 3 Concrete Sections for portland cement-based underlayments and patching compounds.
2. 	Resilient Flooring Accessories: Refer to Division 9 Finishes Sections for resilient flooring accessories.

2.4 	SOURCE QUALITY

A.	Source Quality: Obtain flooring product materials from a single manufacturer.

PART 3 -  EXECUTION

3.1 	MANUFACTURER'S INSTRUCTIONS

A. 	Compliance: Comply with manufacturer's product data, including product technical bulletins, product catalog installation instructions, and product carton instructions for installation.

3.2 	EXAMINATION

A.	Site Verification of Conditions: Verify substrate conditions (which have been previously installed under other sections) are acceptable for product installation in accordance with manufacturer's instructions.

B.	Material Inspection: In accordance with manufacturer's installation requirements, visually inspect materials prior to installation. Material with visual defects shall not be installed and shall not be considered as a legitimate claim.

3.3	PREPARATION

A.	Adjacent Surfaces Protection: Protect adjacent work areas and finish surfaces from damage during product installation.

B.	Surface Preparation:

1. 	General: Prepare floor substrate in accordance with manufacturer's instructions. 
2.	 Floor Substrate: Prepare floor substrate to be smooth, rigid, flat, level, permanently dry, clean and free of foreign materials such as dust, paint, grease, oils, solvent, curing and hardening compounds, sealers, asphalt and old adhesive residue.
3. 	Concrete Floor Substrate: Concrete floor substrate shall have a minimum compressive strength of 3500 psi. Refer to Division 3 Concrete sections for patching and repairing crack materials, and leveling compounds with portland cement-based compounds. Do not use or install flooring over gypsum-based leveling or patching materials.

a. Reference Standard: Comply with ASTM F 710 Practice for Preparing Concrete Floors and Other Monolithic Floors to Receive Resilient Flooring.

C. 	Concrete Moisture Test: Perform moisture tests on concrete floors regardless of the age or grade level with a minimum of three tests for the first 1000 square feet. The test shall be a calcium chloride test. One test shall be conducted for every 1000 sq. ft. of flooring. The test shall be conducted around the perimeter of the room, at columns and where moisture may be evident. The moisture emission from the concrete shall not exceed 5.0 lbs. per 1000 sq. ft. in 24 hrs. For the most accurate results, the weight of the calcium chloride dish shall be made on the job site at the start and end of each test. A diagram of the area showing the location and results of each test shall be submitted to the architect, general contractor or end user. If the test results exceed the limitations, the installation shall not proceed until the problem has been corrected.

D.	Concrete pH Test: Perform pH tests on concrete floors regardless of the age or grade level. If the pH is greater than 10, it must be neutralized prior to beginning the installation.

E.	 Wood Subfloor Substrate: Prepare wood subfloor substrate to be rigid, double construction with a one inch minimum thickness, free from harmful movement and have at least 18 inches of well ventilated air space below. Do not install flooring over wooden subfloors built on sleepers over, on or below grade concrete floors.

1. 	Refer to Division 6 Carpentry sections for wood subfloor construction.

3.4 	INSTALLATION

A.	Adhesive Flooring Installation: Cut required length of linoleum flooring from roll, allowing enough material to extend up the wall 4 to 6 inches at either end. Layout and position sheet flooring so that any seams will fall at least 6 inches from underlayment joints or saw cuts in concrete substrate. Scribe and cut flooring material to shape of vertical surfaces, including walls and partitions. Apply adhesive and lay sheet flooring into wet adhesive and roll with a 100 pound roller. Install sheet flooring square with room axis.

1.	 Adhesive, Seamless Flooring Installation: Rout out seams and heat weld together with complementary colored heat welding rod of complimentary composition in accordance with resilient flooring manufacturer's recommendations.
2.	Adhesive Material Installation: Use trowel as recommended by flooring manufacturer for specific adhesive. Spread at a rate of approximately 150 sq. ft./gal. as recommended by flooring manufacturer.

B. 	Installation Techniques:

1. 	Where demountable partitions and other items are indicated for installation on top of finished flooring, install flooring before these items are installed.
2. 	Scribe, cut, fit flooring to butt tightly to vertical surfaces, permanent fixtures and built-in furniture, including pipes, outlets, edgings, thresholds, nosings, and cabinets.
3. 	Extend flooring into toe spaces, door reveals, closets, and similar openings.
4. 	Install flooring on covers for telephone and electrical ducts, and similar items occurring within finish floor areas. Maintain overall continuity of color and pattern with pieces of flooring installed on these covers.
5. 	Do not install resilient flooring over expansion joints. Use expansion joint covers manufactured for use with resilient flooring. Refer to other specification sections for expansion joint covers.
6. 	Adhere resilient flooring to substrate without producing open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, or other surface imperfections in completed installation.

a.	 Use adhesive applied to substrate in compliance with flooring manufacturer’s recommendations, including those for trowel notching, adhesive mixing, and adhesive open and working times.
7. 	Roll resilient flooring as required by resilient flooring manufacturer.

3.5 	CLEANING

A. 	Cleaning: Remove temporary coverings and protection of adjacent work areas. Repair or replace damaged installed products. Clean installed products in accordance with manufacturer's instructions prior to owner's acceptance. Remove construction debris from project site and legally dispose of debris.

1. 	Remove visible adhesive and other surface blemishes using cleaning methods recommended by tile floor manufacturer.
2. 	Sweep and vacuum floor after installation.
3. 	Do not wash floor until after time period recommended by tile flooring manufacturer.
4. 	Damp-mop tile flooring to remove black marks and soil.

3.6 	PROTECTION

A.	Protection: Protect installed product and finish surfaces from damage during construction. Remove and legally dispose of protective covering at time of Substantial Completion.

3.8	 SCHEDULE

A.	Schedules:  See finish schedule.

END OF SECTION