Copyright 2003 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 061600 - SHEATHING

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

Adjust list below to suit Project.

          - Wall sheathing.

          - Roof sheathing.

          - Subflooring.

          - Underlayment.

        - Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

          - Division 06 Section "Rough Carpentry" for plywood backing panels.

      - SUBMITTALS

        - Product Data:  For each type of process and factory-fabricated product.  Indicate component materials and dimensions and include construction and application details.

          - Include data for wood-preservative treatment from chemical treatment manufacturer and certification by treating plant that treated plywood complies with requirements.  Indicate type of preservative used and net amount of preservative retained.

Delete subparagraph below if fire-retardant-treated plywood is not required.

          - For products receiving a waterborne treatment, include statement that moisture content of treated materials was reduced to levels specified before shipment to Project site.

          - Include copies of warranties from chemical treatment manufacturers for each type of treatment.

Retain subparagraph below if applicable.

          - For building wrap, include data on air-/moisture-infiltration protection based on testing according to referenced standards.

        - LEED Submittals: Follow submittal requirements of Division 01 Section “Submittal Requirements” and provide product data on the LEED Materials Documentation Cover Sheet attached as an Appendix to Division 01 Section “Sustainable Design and LEED Requirements.”

Retain subparagraph and associated subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if wood products are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

Insert specific model code organization in paragraph below or revise if report must be from another source.

      - QUALITY ASSURANCE

Retain paragraph and subparagraph below for fire-rated assemblies.

        - Fire-Test-Response Characteristics:  For assemblies with fire-resistance ratings, provide materials and construction identical to those of assemblies tested for fire resistance per ASTM E 119 by a testing and inspecting agency acceptable to authorities having jurisdiction.

Indicate design designations of specific assemblies on Drawings.

          - Fire-Resistance Ratings:  Indicated by design designations from UL's "Fire Resistance Directory."

        - Provide required materials for Integrated Exterior Mockup.

Paragraph and subparagraphs below may be retained to specify wood products made from certified wood for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  An alternative method of complying with Credit MR 7 requirement is to retain requirement in Division 01 Section "Sustainable Design Requirements" that gives Contractor the option and responsibility for determining how Credit MR 7 requirement will be met.

      - DELIVERY, STORAGE, AND HANDLING

        - Stack plywood and other panels flat with spacers between each bundle to provide air circulation.  Provide for air circulation around stacks and under coverings.

- PRODUCTS

      - WOOD PANEL PRODUCTS, GENERAL

        - Meet requirements of LEED for Homes Mid-Rise 2010 Credit MR 2.2 as defined in Division 01 Section “Sustainable Design and LEED Requirements” for this type of material.

Select one of two options in paragraph below; usually the second.  DOC PS 2 is a performance-based standard that does not include requirements for grades of veneers.  Second option includes phrase ", unless otherwise indicated" to allow for underlayment that is specified to comply with DOC PS 1 because a minimum face veneer grade is required; delete if phrase is not needed.

        - Plywood:  DOC PS 1.

Delete paragraph below if oriented strand board is not used.

        - Oriented Strand Board:  DOC PS 2.

Retain first paragraph below if a minimum thickness is shown on Drawings.

        - Thickness:  As needed to comply with requirements specified, but not less than thickness indicated.

        - Factory mark panels to indicate compliance with applicable standard.

      - PRESERVATIVE-TREATED PLYWOOD

Delete this Article if not applicable.  See Evaluations for discussion of formulations.

        - Preservative Treatment by Pressure Process:  AWPA C9.

See Evaluations for information about treatment chemicals.

          - Preservative Chemicals:  Acceptable to authorities having jurisdiction and containing no arsenic or chromium.

        - Mark plywood with appropriate classification marking of an inspection agency acceptable to authorities having jurisdiction.

Select first option in paragraph below and delete others if total treatment is required; otherwise, select second option with or without third option.

        - Application:  Treat items indicated on Drawings.

Edit list below to suit local code and Project.

      - WALL SHEATHING

If retaining paragraph below, select one of four options.  Structural I provides increased racking resistance.  See Evaluations for information about durability classifications of plywood.

        - Plywood Wall Sheathing:  Exposure 1, Structural I (CDX) sheathing.

Select one of four options in subparagraph below.

          - Span Rating:  Not less than 24/0 or 32/16.

If retaining subparagraph below, usually select first option for studs 16 inches (406 mm) o.c., second option for studs 24 inches (610 mm) o.c.  Select third option for more stringent requirement.

          - Nominal Thickness:  As indicated on the drawings.

        - Gypsum Wall Sheathing: Contractor has the option of using any of the following products:

          - Glass-Mat Gypsum Wall Sheathing:  ASTM C 1177/1177M.

            - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

              - GlasRoc Sheathing; CertainTeed (BPB America, Inc.)

              - Dens-Glass Gold; Georgia-Pacific Corporation.

              - E2XP Extended Exposure Sheathing; Gold Bond.

              - Securock Sheathing; United States Gypsum Co.

            - Type and Thickness:  Type X, 5/8 inch thick.

            - Size:  48 by 96 inches minimum.

          - Cellulose Fiber-Reinforced Gypsum Wall Sheathing:  ASTM C 1278/C 1278M, gypsum sheathing.

            - Product:  Subject to compliance with requirements, provide "Fiberock Sheathing with Aqua-Tough" by United States Gypsum Co.

            - Type and Thickness:  Type X, 5/8 inch thick.

            - Size:  48 by 96 inches minimum.

If retaining paragraph below, select one of two options.  Structural I provides increased racking resistance.  See Evaluations for information about durability classifications of oriented strand board.

      - ROOF SHEATHING

If retaining paragraph below, select one of four options.  Structural I provides increased racking resistance.  See Evaluations for information about durability classifications of plywood.

If retaining paragraph below, select one of two options.  Structural I provides increased racking resistance.  See Evaluations for information about durability classifications of oriented strand board.

        - Oriented-Strand-Board Roof Sheathing:  Exposure 1, Structural I sheathing.

          - Span Rating:  Not less than 24/0 or 32/16.

If retaining subparagraph below, usually select first option for spans of 16 inches (406 mm), second option for spans of 24 inches (610 mm).  Select third option for more stringent requirement.

          - Nominal Thickness:  As indicated on the drawings.

          - Product: AdvanTech by Huber Engineered Woods.

      - SUBFLOORING AND UNDERLAYMENT

For resilient flooring, APA recommends separate subflooring and underlayment rather than single-layer floor.  See Evaluations for information about durability classifications of plywood.

For resilient flooring, APA recommends separate subflooring and underlayment rather than single-layer floor.  See Evaluations for information about durability classifications of oriented strand board.

If retaining paragraph below, select one of four options.  Structural I provides increased racking resistance.  For resilient flooring, APA recommends separate subflooring and underlayment rather than single-layer floor.  See Evaluations for information about durability classifications of plywood.

        - Plywood Subflooring:  Exposure 1, Structural I (CDX) single-floor panels or sheathing.

Select one of first five options and possibly one of last three options in subparagraph below.

          - Span Rating:  Not less than 24 o.c. or 32/16.

          - Edge Detail:  Tongue and groove.

If retaining subparagraph below, usually select first option for spans of 16 inches (406 mm); second option for spans of 24 inches (610 mm).  For more stringent requirement, select second option for spans of 16 inches (406 mm) or third option for spans of 24 inches (610 mm).

          - Nominal Thickness:  As indicated on the drawings.

If retaining paragraph below, select one of two options.  Structural I provides increased racking resistance.  For resilient flooring, APA recommends separate subflooring and underlayment rather than single-layer floor.  See Evaluations for information about durability classifications of oriented strand board.

        - Underlayment, General:  Provide underlayment in nominal thicknesses indicated or, if not indicated, not less than 1/4 inch over smooth subfloors and not less than 3/8 inch over board or uneven subfloors.

See Evaluations for information about durability classifications of plywood.

If retaining paragraph below, select one of four grades.  Verify availability of grade selected.

        - Plywood Underlayment for Resilient Flooring:  DOC PS 1, 3-ply Canadian poplar plywood with fully sanded face.

          - Nominal Thickness:  1/4 inch.

          - Product: Multiply Underlayment by Multiply Plywood.

Paragraph below is based on TCA Methods F 142 and F 143 for installation over plywood subflooring of not less than 5/8-inch (15.9-mm) nominal thickness.  Cementitious backer units specified in Division 09 Section "Tiling" can also be used as underlayment for ceramic tile.

        - Plywood Underlayment for Carpet:  DOC PS 1, Exterior, C-C Plugged, not less than 1/4-inch nominal thickness.

If retaining paragraph below, select one of three grades.  Verify availability of grade selected.

If retaining paragraph below, verify acceptability with floor covering manufacturers.

      - FASTENERS

        - General:  Provide fasteners of size and type indicated that comply with requirements specified in this Article for material and manufacture.

          - For roof and wall sheathing, provide fasteners with hot-dip zinc coating complying with ASTM A 153/A 153M.

        - Nails, Brads, and Staples:  ASTM F 1667.

Standard in first paragraph below covers power-driven staples, nails, P-nails, and allied fasteners.

        - Power-Driven Fasteners:  NES NER-272.

        - Wood Screws:  ASME B18.6.1.

        - Screws for Fastening Wood Structural Panels to Wood Framing:  ASTM C 954, except with wafer heads and reamer wings, length as recommended by screw manufacturer for material being fastened.

          - For wall and roof sheathing panels, provide screws with organic-polymer or other corrosion-protective coating having a salt-spray resistance of more than 800 hours according to ASTM B 117.

        - Screws for Fastening Gypsum Sheathing to Wood Framing:  Steel drill screws, in length recommended by sheathing manufacturer for thickness of sheathing board to be attached, with organic-polymer or other corrosion-protective coating having a salt-spray resistance of more than 800 hours according to ASTM B 117.

      - SHEATHING JOINT-AND-PENETRATION TREATMENT MATERIALS

        - General: If required by the selected Air Barrier manufacturer, provide the following joint sealant:

If desired and a separate weather-resistant barrier over sheathing is not required by authorities having jurisdiction, retain this Article.  See "Weather-Resistive Barriers" Article in the Evaluations.

        - Sealant for Glass-Mat Gypsum Sheathing Board:  Elastomeric, medium-modulus, neutral-curing silicone joint sealant compatible with joint substrates formed by gypsum sheathing and other materials, recommended by sheathing manufacturer for application indicated, and complying with requirements for elastomeric sealants specified in Division 07 Section "Joint Sealants."

          - Available Product:  895 Silicone building Sealant by Pecora Corporation.

Retain paragraph above or first two paragraphs below.  If retaining above, verify compatibility with sheathing selected.

Product in first paragraph below is an open mesh tape for use with sealant in paragraph above.

        - Sheathing Tape for Glass-Mat Gypsum Sheathing Board:  Self-adhering glass-fiber tape, minimum 2 inches wide, 10 by 10 or 10 by 20 threads/inch, of type recommended by sheathing and tape manufacturers for use with silicone emulsion sealant in sealing joints in glass-mat gypsum sheathing board and with a history of successful in-service use.

Revise first paragraph below if stainless-steel drill screws are required.

      - MISCELLANEOUS MATERIALS

According to APA, only certain solvent-based glues are suitable for nonveneer panels with sealed surfaces and ends.

        - Adhesives for Field Gluing Panels to Framing:  Formulation that is approved for use with type of construction panel indicated by manufacturers of both adhesives and panels.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  VOC limits are those for subfloor adhesives and multipurpose construction adhesives, respectively.

          - Use adhesives that have a VOC content of 50 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

- EXECUTION

      - INSTALLATION, GENERAL

        - Do not use materials with defects that impair quality of sheathing or pieces that are too small to use with minimum number of joints or optimum joint arrangement.

        - Cut panels at penetrations, edges, and other obstructions of work; fit tightly against abutting construction, unless otherwise indicated.

        - Securely attach to substrate by fastening as indicated, complying with the following:

          - NES NER-272 for power-driven fasteners.

Retain one of two subparagraphs below, with or without subparagraph above, to comply with requirements of Project and local codes.

          - Table 2304.9.1, "Fastening Schedule," in ICC's "International Building Code."

Retain first paragraph below if wood framing is used.  Revise to indicate other kinds of nails if required.

        - Use common wire nails, unless otherwise indicated.  Select fasteners of size that will not fully penetrate members where opposite side will be exposed to view or will receive finish materials.  Make tight connections.  Install fasteners without splitting wood.

        - Coordinate wall and roof sheathing installation with flashing and joint-sealant installation so these materials are installed in sequence and manner that prevent exterior moisture from passing through completed assembly.

        - Do not bridge building expansion joints; cut and space edges of panels to match spacing of structural support elements.

        - Coordinate sheathing installation with installation of materials installed over sheathing so sheathing is not exposed to precipitation or left exposed at end of the workday when rain is forecast.

      - WOOD STRUCTURAL PANEL INSTALLATION

        - General:  Comply with applicable recommendations in APA Form No. E30S, "Engineered Wood Construction Guide," for types of structural-use panels and applications indicated.

        - Fastening Methods:  Fasten panels as indicated below:

Delete fastening methods not required.  Coordinate with building code requirements.

          - Subflooring:

            - Glue and nail to wood framing.

            - Space panels 1/8 inch apart at edges and ends.

          - Wall Sheathing:

A continuous bead of glue applied to framing at edges of wall sheathing panels will help seal panel joints so sheathing will function as an air barrier.

            - Nail to wood framing.

            - Space panels 1/8 inch apart at edges and ends.

          - Roof Sheathing:

A continuous bead of glue applied to framing at edges of wall sheathing panels will help seal panel joints so sheathing will function as an air barrier.

            - Glue and nail to wood framing.

            - Space panels 1/8 inch apart at edges and ends.

          - Underlayment: Install in accordance with manufacturer’s recommendations.

            - Nail to subflooring, 2 inches on center along edges and 4 inches on center in the field.

            - Butt panels together at edges and ends.

            - Leave 1/4 to 1/2inch gap at walls.

Delete subparagraph below if wood structural panels are not used as underlayment for resilient flooring.

            - Fill and sand edge joints of underlayment receiving resilient flooring right before installing flooring.

      - GYPSUM SHEATHING INSTALLATION

        - Comply with GA-253 and with manufacturer's written instructions.

Retain applicable subparagraph(s) below or insert requirements to suit Project.

          - Fasten gypsum sheathing to wood framing with screws.

          - Install boards with a 3/8-inch gap where non-load-bearing construction abuts structural elements.

          - Install boards with a 1/4-inch gap where they abut masonry or similar materials that might retain moisture, to prevent wicking.

        - Apply fasteners so heads bear tightly against face of sheathing boards but do not cut into facing.

Revise first paragraph below if horizontally installed boards do not have tongue-and-groove edges.

        - Horizontal Installation:  Install sheathing with V-grooved edge down and tongue edge up.  Interlock tongue with groove to bring long edges in contact with edges of adjacent boards without forcing.  Abut ends of boards over centers of studs, and stagger end joints of adjacent boards not less than one stud spacing.  Attach boards at perimeter and within field of board to each steel stud.

          - Space fasteners approximately 8 inches o.c. and set back a minimum of 3/8 inch from edges and ends of boards.

Retain subparagraph above or below.  Delete below if not applicable or not permitted.

          - For sheathing under stucco cladding, boards may be initially tacked in place with screws if overlying self-furring metal lath is screw-attached through sheathing to studs immediately after sheathing is installed.

        - Seal sheathing joints according to sheathing manufacturer's written instructions.

Retain subparagraph below for taping joints in foam-plastic sheathing.

Insert requirements for removing protection if it does not become part of final assembly.  Paragraph above assumes that weather-resistant sheathing paper will be installed to comply with requirements for incorporating it into final assembly.

END OF SECTION 061600