SECTION 06100

ROUGH CARPENTRY

1.	GENERAL

1.1	GENERAL PROVISIONS

A.	SCOPE:  Drawings and general provisions of Contract, including General Conditions and Division 1 specifications, apply to work in this section.  Performance shall meet the 	requirements of these Specifications.

1.2	DESCRIPTION OF WORK

A.	The work covered by this section of Specifications consists of the following:

- All rough carpentry work as required by Drawings and as specified under this section to include: blocking, roof sheathing, vestibule siding and exterior trim and other misc. items specified elsewhere and shown on Drawings.

2.	PRODUCTS:

  - LUMBER

- Lumber shall conform to Product Standard 20-70 (American Softwood Lumber Standard).  Lumber shall bear the grade and trademark of the Association under whose rules it is produced and a mark of mill identification.

- Protect all lumber and keep dry, both in transit and at the job site.

- All lumber shall be well seasoned and contain not more than 19% moisture content

- All two inch nominal framing lumber unless otherwise noted, shall be #2 Eastern Spruce or better grade and shall have the following minimum allowable stresses:

  - Extreme fiber in blending, Fb = 950 psi.

  - Tension parallel to grain, Ft = 425 psi.

  - Compression parallel to grain, Fc = 700 psi.

  - Modulus of elasticity, E = 1,400,000 psi.

- Engineered Wood Products: Provide Engineered Wood Products manufactured by TrusJoint/MacMillian or Approved alternate.

2.2  	PLYWOOD

- Each panel shall be identified with appropriate American Plywood Association grade-trademark, showing  panel type, span rating, thickness, veneer grade, species group member, edge detail (where applicable), and exposure grade.

- Each panel shall meet requirements of U.S. Product Standard PS 1/ANSI A199.1 for Construction and Industrial Plywood, or APA Performance standards where noted below for flooring panels.

- Plywood noted “exterior” on drawings, or which is used in exterior locations such as walls or roofs, shall be APA Exterior or Exposure 1 Grade.  Plywood used in interior locations subject to high humidity or water leakage shall be APA Exterior, Exposure 1, or Exposure 2 Grade.  Other plywood may be interior grade.

- Plywood with one face exposed-to-view shall be APA A-D Veneer Grade or better.  Plywood which is not exposed to view shall be APA-C-D Plugged Grade or better.

- Plywood used in sub flooring under separate underlayment panels or structural finish floor, and plywood used  as wall, soffit, and roof sheathing, shall be APA Rated Sheathing type construction panel.

- Plywood used as flooring underlayment over separate plywood sub flooring shall be APA Underlayment Grade, sanded face, Exterior, Exposure 1, or Exposure 2 Grade.

- Provide plywood as shown on drawings.

3. 	EXECUTION:

3.1 	GENERAL:  The Contractor shall carefully lay out and erect all structural members of rough carpentry, framing, sheathing, blocking, bridging and other items of work as necessary to install the finished work as shown on Drawings and as noted in Specifications.  All members shall be properly braced, plumbed and leveled.

3.2	BLOCKING:

A.	(2x6, 2x8 or wider) shall be provided as necessary for the application of plumbing and fixtures as defined in Section 15400, toilet accessories, grab bars and kitchen cabinets located on Drawings, drapery track and other wall mounted accessories, electrical and communications equipment.  Provide either blocking for or center stud in closet backwalls for closet rod/shelf bracket.

END OF SECTION