SECTION 07530

FLEXIBLE SHEET ROOFING SYSTEM

PART 1  GENERAL

1.01  DESCRIPTION OF WORK

A.	Fully adhered EPDM sheet roofing, tapered and flat roof insulation, elastomeric flashing,  wood nailers, lead coated copper edge strips and attic vents.

1.02  CODES, REGULATIONS AND STANDARDS

A.	Contractor Responsibility: The Contractor shall assume full responsibility and liability for compliance with all applicable Federal, State and local codes, regulations and standards pertaining to work practices, hauling, disposal, protection of workers and visitors to the site, and persons occupying areas adjacent to the site.  This includes modification of procedures to comply with changes to codes, regulations and standards which occur during the work of this contract.  The Contractor is responsible for providing medical examinations and maintaining medical records of personnel as required by the applicable Federal, State and local regulations.  The Contractor shall hold the Owner and Owner's Representatives harmless for failure to comply with any applicable work, hauling, disposal, safety, health or other regulations on the part of himself, his employees or his subcontractors.

1.03  QUALITY ASSURANCE

A.	Roofing contractor to be approved in writing by the membrane manufacturer.  Contractor shall be able to substantiate that he has been trained by the membrane manufacturer.

1.04  SUBMITTALS

A.	Sample ten (10) year watertight warranty for the EPDM membrane

B.	Sample twenty (20) year material warranty for the EPDM membrane.

C.	Current EPDM membrane manufacturer's application specifications.

1.05  PRODUCT DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in their original, unopened containers, clearly labeled with manufacturer's name.  All material to be stored in waterproof trailers or sheds, up on raised platforms and under lock and key until use.  Do not use materials damaged in handling or storage.  Replace damaged material with new material.  Store adhesives between 60 and 80 degrees F.  Should they be exposed to lower temperatures,  restore to room temperature for three to five days prior to use.

1.06  WARRANTY

A.	A ten (10) year watertight warranty and twenty (20) year material warranty shall be issued by the EPDM membrane manufacturer.

B.	The roofing contractor shall furnish the Owner with his personal two (2) year watertight warranty.

PART 2  PRODUCTS

2.01  ROOF INSULATION

A.	Tapered and flat roof insulation to be polyisocyanurate closed-cell foam core and manufacturer's standard facing laminated to both sides, complying with FS HH-I-1972/2, Class 1.

B.	Over the metal deck where thermal insulation is not required the roof insulation to be one inch (1") thick high density fiberboard such as Structodek by AC-1 Masonite Class “C”.

C.	Over all foam insulation, install one layer of 1/2" high density fiberboard roof insulation.  The high density fiberboard roof insulation to be Structodek by AC-1 Masonite Class “C”.

2.02  MEMBRANE ROOF SYSTEM

A.	Membrane roofing to be fully adhered .060" EPDM sheet roofing furnished in twenty five foot (25') wide (or wider) rolls by Firestone, Carlisle or Versico.  Roof membrane to be fully adhered to the high density fiberboard roof insulation.

B.	Use the roof membrane for flashing of curbs and walls per the manufacturer's standard details.  Use reinforced EPDM anchor strips to avoid splice joints at walls and edges.

C.	Adhesives, sealants, thinner, cleaner and accessories to be furnished by the membrane manufacturer.

D.	Seven inch (7”) wide seam tape will be required for all field seams.

2.03  METAL FLASHING

A.	Edge strip to be formed using 16 ounce lead coated copper.  Concealed clips to be formed using 20 ounce plain copper.

2.04  WOOD NAILERS AND BLOCKING

A.	All wood nailers and blocking shall be #2 or better pressure treated with non-leachable waterborne salt such as Osmose K-33.  Plywood to be exterior type and pressure treated.

2.05  FASTENERS

A.	Use fasteners recommended by the membrane manufacturer to secure anchor bars and termination bars.

B.	Wood nailers to be secured using annular-ring hot dipped galvanized nails, galvanized dry-wall screws, #14-10 Heavy Duty Roofing Fasteners, carriage bolts or expansion anchors.

C.	Fasteners used to secure roof insulation to the deck to be #14-10 Heavy Duty Roofing Fasteners with CR-10 coating, a minimum shank diameter of 0.170" and a thread diameter of 0.125".  Pressure plates to be 3" diameter Galvalume plates.  Screws and plates to be manufactured by Olympic Fasteners or approved equal.  Length, size and accessories to be as required by the EPDM membrane manufacturer selected.

D.	Copper flashing to be secured with annular-ring copper nails as shown on attached drawings.

PART 3  EXECUTION

3.01  PREPARATION OF SURFACES

A.	Prior to cutting the old built-up roofing, sweep all loose gravel from the roof.  Completely remove existing built-up roofing, roof insulation, base felt, vapor retarder,  sheathing paper, base flashing, edge strips and vent flashing.  Promptly remove from site and dispose of properly.

B.	Surfaces on which the roofing system is to be applied shall be clean, smooth, dry, free of fins, rot, sharp edges, loose and foreign materials, oil and grease.

3.02  ROOF INSULATION

A.	Insulation shall be tightly butted with joints not more than  1/8" in width.  Stagger joints with those in layer below.  Fiberboard to be installed with a 1/16"-1/8" gap at all joints when board size is greater than 2' x 4'.

B.	Fasten insulation to the roof deck with the appropriate screws and plates.  Fastener quantity and layout must meet all requirements that may be imposed by the EPDM manufacturer.

C.	Stagger joints in one direction for each course.  For multiple layers, stagger joints in both directions between courses leaving no gaps, allowing a complete thermal envelope to be formed.

D.	Provide tapered units to suit drainage pattern indicated.

E.	Do not install more insulation in a day than can be covered with membrane before end of day or before start of inclement weather.

3.03  ROOF MEMBRANE

A.	Adhere the .060" EPDM membrane to the high density fiberboard in strict accordance with the manufacturer's specifications.

B.	Seven inch (7”) wide seam tape will be required for all field seams.

3.04  FLASHING - - WALLS, PARAPETS, CURBS AND VENTS

A.	Remove all existing flashing.

B.	Use the longest pieces of material which are practical.  All flashing and terminations shall be done in accordance with the applicable manufacturer's details.

C.	Care must be taken to set the elastomeric flashing so it does not bridge where there is a change of direction (i.e. where a parapet meets the roof deck).  This can be accomplished by creasing the membrane into the angle change prior to adhering up the wall.  Excess bridging will be cause for rejection and will be re-done at the contractor's expense.

D.	Install termination bars at the top of all base flashing, fastening a minimum of 6" on center.

E.	Raise existing curb height as necessary to obtain a minimum of 8" high flashing.

3.05  EDGE STRIPS

A.	Bottom edge of lead coated copper edge strips to be secured with continuous cleats.  Nail top flange with annular-ring nails, three inches (3") on center.  Strip top flange with 6" pressure sensitive  flashing.

3.06  WOOD NAILERS AND BLOCKING

A.	Securely fasten new pressure treated wood nailers to structural members so as to resist a force of 200 pounds per lineal foot in any direction.

3.07 TEMPORARY WATER CUT-OFF

A.	Temporary water cut-offs are to be constructed at the end of each working day to protect the insulation, roofing, building and building interior from damage due to wind, snow and rain.

B.	Temporary water cut-offs are to be detailed by the contractor and approved by the manufacturer and Owner.

3.08  CLEAN UP

A.	Site clean-up shall be complete and to the satisfaction of the Owner.

B.	All roofs, building, landscape and parking areas shall be cleaned of all trash, debris and dirt caused by or associated with this work.

C.	Any areas stained, dirtied, discolored or otherwise damaged due to this work shall be cleaned, restored and replaced as required.

D.	All debris shall be removed from the premises promptly and the construction area left clean daily.

3.9  INSPECTION AND TESTING

THE OWNER RESERVES THE RIGHT TO INSPECT AND TEST ALL CONSTRUCTION OPERATIONS AND MATERIALS.

A.	Any defect or noncompliance discovered by inspection shall be reported to the contractor who shall promptly remove any defective material from the site.

B.	The Owner reserves the right to inspect the work or parts of it as he chooses.  His failure to inspect the work in progress shall not relieve the contractor of the responsibility for properly executing the contracted work, nor shall it impair the Owner's right to reject deficiencies he may subsequently discover.

PART 4  JOB CONDITIONS

A.	Roofing to be applied in dry weather.

B.	Completed roof areas shall not be trafficked.  The work shall be coordinated to prevent this situation by working toward the roof edges.

C.	This project is subject to compliance with all requirements of the Occupational Safety and Health Administration (OSHA).  All work on this project must meet the requirements of all applicable state and local codes, laws and ordinances.

END OF SECTION