SECTION 09510

ACOUSTICAL CEILINGS

1.   	GENERAL

1.1  	REFERENCES

A.  	Drawings and general provisions of Contract, including General Conditions and Division 1 				Specifications, apply to work in this section.

B.  	Gypsum Drywall:  Section 09250

C.  	Mechanical and Electrical:  Division 15 and 16

D.  	Underwriters Laboratories  (UL)

E.  	American Society for Testing and Materials (ASTM)

1.2  	DESCRIPTION OF WORK

A.  	Extent of Acoustical Ceilings is shown on the drawings.

1.3  	SUBMITTALS

A.  	Submittals under this Section shall include:

1.  	Manufacturers' data and installation instructions on all specified products;

2.  	Color range;

3.  	Samples of acoustical units;

4.  	Shop drawings indicating materials, pattern number, tile number, and manufacturer.

B.  	Provide, as maintenance material, 1 percent of each acoustical unit used on job, in clean, marked 			cartons.

2.   	PRODUCTS

2.1  	SUSPENSION SYSTEMS

A. 	Suspension System, unless noted otherwise, shall be "Suprafine" - White series, Low Gloss Baked Enamel Finish as manufactured by Armstrong, or approved equal.

B.  	Suspension system shall comply with ASTM C 635.  Detailed design of system is manufacturer's 			responsibility, including materials, metal thickness, dimensions of necessary component section 			configurations, hanger and assembly devices, and provision of necessary accessory items.

C.  	System shall support design load with a maximum deflection of 1/360 between supports.  				Component materials that oxidize or corrode in normal environments shall have protective 				treatment or coatings, such as hot dipped galvanizing or anodizing.

D.  	Structural classification (per Table 1, ASTM C 635): intermediate-duty.

E.  	Minimum runner support:  12 gauge wire at 4'-0" intervals, staggered.

F.  	For circular penetrations at ceiling, provide edge moldings fabricated to fit penetration exactly.  			Fry Column Collar edge molding or approved equal.

2.2  	MINERAL-FIBER ACOUSTICAL UNITS

A.  	Tile shall be manufactured by Armstrong as follows:

1.  	#1:  Armstrong # 535 24” x 24” x ¾ - White

2.  	#2:  Hardware friendly option - Cirrus

3.   	EXECUTION

3.1  	INSTALLATION

A.  	Before beginning installation, examine areas to receive ceiling system for dampness, structural 			weakness, and other conditions which would affect quality of finished work.  Coordinate layout 			with work in Divisions 15 and 16, for alignment of equipment with ceiling suspension system.

B.  	Installation of suspension system shall comply with ASTM C 636.  Finished installation shall be 			level to within 1/4 in. in 10 ft.

1.  	Space hangers not over 48 in. o.c. in direction of main runner channels, and within 6 in. of 				ends of main runner runs and of boundary walls, structural steel, partitions, and similar 					interruptions of ceiling continuity.  Install additional hangers at ends of each suspension 					member and at ceiling equipment not separately suspended, 6 in. from vertical surfaces.  Do 				not splay wires more than 5 in. in a 4 ft. vertical drop.  Wrap wire a minimum of three times 				horizontally, turning ends upward.

2.  	Attach hangers directly to ceiling structure, or to supplementary framing members supplied 				and installed under this Section.  Hangers may not be suspended from mechanical or 					electrical equipment such as ductwork, conduit or piping.

3.  	Install main and cross runners level and perpendicular to walls, at right angles to one another.

4.  	Install wall molding at intersection of suspended ceiling and vertical surfaces.  Miter corners 				where wall moldings intersect or install corner caps.  Attach to vertical surfaces with 					mechanical fasteners.

C.  	Install lay-in panels to bear fully on suspension system.  Neatly cut acoustical units as required for 			sprinkler heads and HVAC equipment.

D.  	At completion of job, clean soiled or discolored unit surfaces after installation.  Touch up 				scratches, abrasions, voids, and other defects in painted surfaces.  Remove and replace damaged or 		improperly installed units.

END OF SECTION