# SECTION 09511

# ACOUSTICAL PANEL CEILINGS

PART 1 - GENERAL

1.01	RELATED DOCUMENTS

- Drawings and general provisions of Contract, including General and Supplementary 	Conditions and Division 1 Specifications Sections, apply to this Section.

1.02	SUMMARY

- This Section includes the following:

1.	Acoustical panel

2.	Exposed suspension system

- Related Sections include the following:

1.	Division 9 Section “Gypsum Board Assemblies” for suspension systems provided 				for gypsum board ceilings.

1.		Division 15 and 16 Section for coordination of air handling devices, fire 					protection devices and electrical devices installed in ceiling systems.

1.03	DEFINITIONS

- CAC: Ceiling Attenuation Class

- NRC: Noise Reduction Coefficient.

1.04	SUBMITTALS

- General:  Submit in accordance with Section 01330.

- Product data for each type of product specified.

- Samples: For each component indicated and for each exposed finish required, prepared on samples 	of size indicated below:

1.	Acoustical Panel: Set of 6 inch square samples of each type, color, pattern and texture.

2.	Exposed Suspension System Members, Moldings and Trim: Set of 12 inch long samples 			of each type, finish and color.

- Product Testing Reports: Based on evaluation of comprehensive tests performed by a qualified testing 	agency, for each acoustical panel ceiling.

1.05	QUALITY ASSURANCE

- Source Limitations:

1.	Acoustical Ceiling Panel: Obtain each type through one source from a single manufacturer.

2.	Suspension System: Obtain each type through one source from a single manufacturer.

- Fire-Performance Characteristics:  Provide acoustical panel ceilings that comply with the 	following requirements:

  - Fire-Resistance Characteristics:  Where indicated, provide acoustical panel ceilings 	identical to those of assemblies tested per ASTM E 119 by UL or another testing and 	inspecting agency acceptable to authorities having jurisdiction.

  - Surface Burning Characteristics:  Provide acoustical panels with the following surface-	burning characteristics complying with ASTME 1264 for Class A materials as 	determined by testing identical products per ASTM E 84.

a.	Smoke Developed:  450 or less.

1.06	DELIVERY, STORAGE, AND HANDLING

- Deliver acoustical panels, suspension system components and accessories to project site in 	original, unopened packages and store them in a fully enclosed, conditioned space where they will 	be protected against damage from moisture, direct sunlight, surface contamination, and other 	causes. Store materials flat.

- Before installing acoustical ceiling units, permit them to reach room temperature and a stabilized 	moisture content.

- Handle acoustical ceiling units carefully to avoid chipped edges or damaging units in any 	way.

1.07	PROJECT CONDITIONS

- Environmental Limitations: Do not install acoustical panel ceilings until spaces are enclosed and 	weatherproof, wet work in spaces is complete and dry, work above ceilings is complete and 	ambient temperature and humidity conditions are maintained at the levels 	indicated for project 	when occupied for its intended use.

- Mechanical, electrical, and other utility service installations above the ceiling plane shall have 	been completed prior to the installation of the ceilings.

1.08	COORDINATION

- Coordinate layout and installation of acoustical panels and suspension system with other 	construction that penetrates ceilings or is supported by them, including light fixtures, HVAC 	equipment, fire-suppression system, and partition assemblies.

PART 2 - PRODUCTS

2.01	MANUFACTURERS

- In other Part 2 articles where titles below introduce lists, the following requirements apply for 	product selection:

1.	Products: Subject to compliance with requirements, provide one of the products 				specified.

  - ACOUSTICAL PANELS, GENERAL

- Acoustical Panel Standard: Provide manufacturer’s standard panels of configuration indicated that 	comply with ASTM E 1264 classifications as designated by types, patterns, acoustical ratings, and 	light reflectance, unless otherwise indicated.

1.	Mounting Method for Measuring NRC: Type E-400; plenum mounting in which face of 			test specimen is 15 3/4 inches away from test surface per ASTM E 795.

2.	Test Method for Ceiling Attenuation Class (CAC): Where acoustical panel ceilings are 			specified to have a CAC, provide units identical to those tested per ASTM E 1414 by a 			qualified testing agency.

  - Acoustical Panel Colors and Patterns: Match appearance characteristics indicated for each 	product 	type.

2.03	ACOUSTICAL PANELS: TWO PORTLAND SQUARE

- Acoustic Panels: Complying with ASTM E 1264, matching existing panels, and having the 	following characteristics:

1.	ACT 1: Armstrong, Dune Angled Teqular; Product #1774.

2.	Color: White

3.	NRC: Not less than 0.50

4.	CAC: Not less than 35

5.	Size: 24x24x5/8”

6.	Fire Hazard Classification: Class A.

- ACT 2: Product: Match existing 2 x 2 ActClq. tile and grid system

2.05	METAL SUSPENSION SYSTEMS, GENERAL

- Metal Suspension Systems Standard:  Provide manufacturer's standard direct-hung metal 	suspension systems of types, structural classifications, and finishes indicated that comply with 	applicable requirements in ASTM C 635.

- Finishes and Colors, General:  Comply with NAAMM’s “Metal Finishes Manual for Architectural and 	Metal Products” for recommendations for applying and designating finishes. Provide manufacturer's 	standard factory-applied finish for type of system indicated.

- High-Humidity Finish: Comply with ASTM C 635 requirements for “Coating 	Classification for Severe Environmental Performance” where high-humidity finishes 	are indicated.

- Attachment Devices:  Size for 5 times design load indicated in ASTM C 635, Table 1, “Direct 	Hung” unless otherwise indicated.

- Power-Actuated Fasteners in Concrete: Fastener system of type suitable for application 	indicated, fabricated from corrosion-resistant materials, with clips or other accessory 	devices for attaching hangers of type indicated, and with capability to sustain, without 	failure, a load equal to 10 times that imposed by ceiling construction as determined by 	testing per ASTM E 1190, conducted by a qualified testing and inspecting agency.

- Wire Hangers, Braces and Ties:  Provide wires complying with the following requirements:

- Zinc-coated carbon-steel wire: ASTM A 641/A 641 M, Class 1 zinc coating, soft 	temper.

- Size: Select wire diameter so its stress at 3 times hanger design load (ASTM C 635, Table 	1, Direct-Hung), will be less than yield stress of wire, but provide not less than 0.106-inch 	diameter wire.

2.06	METAL SUSPENSION SYSTEMS FOR ACOUSTICAL PANEL CEILINGS

- Wide-Face, Capped, Double-Web, Steel Suspension System: Main and cross runners roll formed 	from cold-rolled steel sheet, prepainted, electrolytically zinc coated, or hot-dip galvanized 	according to ASTM A 653/A 653M, not less than G30 coating designation, with prefinished 15/16 	inch wide metal caps on flanges.

- Structural Classification: Intermediate-duty system

- End Conditions of Cross Runners: Override (stepped) or butt-edge type, as 	standard with manufacturer.

- Face Design: Flat, flush

- Cap Material: Steel or aluminum cold-rolled sheet, as standard with manufacturer.

- Cap Finish: Painted white

- Locations: For all suspended acoustical ceilings, except as otherwise noted.

- Products:

  - Armstrong World Industries, Inc.; Prelude Exposed Tee System, 7300 Series

  - Chicago Metallic Corporation; 1200 System

  - USG Interiors, Inc; DX System

PART 3 - EXECUTION

3.01	EXAMINATION

- Examine substrates, areas, and conditions, including structural framing to which ceiling system 	attaches or abuts, with Installer present, for compliance with requirements specified in this and 	other sections that affect installation and anchorage and with requirements for installation 	tolerances and other conditions affecting performance of acoustical panel ceilings.

- Do not proceed with installation until unsatisfactory conditions have been corrected.

3.02	PREPARATION

- Measure each ceiling area and establish layout of acoustical units to balance border widths at 	opposite edges of each ceiling.  Avoid use of less-than-half-width units at borders, and comply 	with reflected ceiling plans.

3.03	INSTALLATION, GENERAL

- General:  Install acoustical ceiling systems to comply with ASTM C 636 and seismic requirements 	indicated, per manufacturer's written instructions and CISCA "Ceiling Systems Handbook."

- Suspend ceiling hangers from building structural members and as follows:

- Install hangers plumb and free from contact with insulation or other objects within 	ceiling plenum that are not part of supporting structural or ceiling suspension system.

- Splay hangers only where required to miss obstructions and offset resulting 	horizontal forces by bracing, counter-splaying, or other equally effective means.

- Where width of ducts and other construction within ceiling plenum produces hanger 	spacings that interfere with the location of hangers at spacings required to support 	standard suspension system members, install supplemental suspension members and 	hangers in form of trapezes or equivalent devices.  Size supplemental suspension 	members and hangers to support ceiling loads within performance limits established 	by referenced standards and publications.

- Secure wire hangers to ceiling suspension members to supports above with a minimum of 	three tight turns. Connect hangers directly either to structures or to inserts, eye screws, or 	other devices that are secure and appropriate for substrate and that will not deteriorate or 	otherwise fail due to age, corrosion, or elevated temperatures.

- Space hangers not more than 48 inches o.c. along each member supported directly 	from hangers, unless otherwise indicated; provide hangers not more than 8 inches 	from 	ends of each member.

- Exposed pop rivets for grid alignment purposes shall not be permitted.

- Suspension system shall be reinforced to support diffusers, light fixtures and any additional 	members. Install hanger wires to grid at each corner of light fixtures. Coordinate location with 	electrical and other trades.

  - Each individual fixture and attachment with combined weight of 56 pounds or less shall 	have two 12 gage wire hangers attached at diagonal corners of the fixture. These wires 	shall be slack. Fixtures and attachments with a combined 	weight of greater than 56 pounds 	shall be independently supported from the structure at all four corners.

- Install edge moldings and trim of type indicated at perimeter of acoustical ceiling area and where 	necessary to conceal edges of acoustical units.

- Apply acoustical sealant in a continuous ribbon concealed on back of vertical's of 	moldings before they are installed.

  - Provide at all locations where gypsum wallboard does not go full height of studs.

- Screw attach moldings to substrate at intervals not more than 16 inches o.c. and not 	more than 3 inches from ends, leveling with ceiling suspension system to a tolerance of 	1/8 inch in 12 feet. Miter corners accurately and connect securely.

- Do not use exposed fasteners, including pop rivets, on moldings and trim.

- Install suspension system runners so they are square and securely interlocked with one another. 	Remove and replace dented, bent or kinked members.

- Install acoustical panels with undamaged edges and fit accurately into suspension system runners 	and edge moldings.  Scribe and cut panels at borders and at penetrations to provide a neat, precise 	fit.

3.04	CLEANING

- Clean exposed surfaces of acoustical ceilings, including trim, edge moldings, and 	suspension 	members.  Comply with manufacturer's instructions for cleaning and touch up of minor finish 	damage.  Remove and replace work that cannot be successfully cleaned and repaired to 	permanently eliminate evidence of damage.

END OF SECTION 09511