SECTION 09680

CARPET

PART 1 – GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of Contract, including General and Supplementary 				Conditions and Division 1 Specifications Sections, apply to this Section.

B.	Related Sections include the following:

1.	Division 2 Section "Selective Demolition and Alterations" for removing existing 					floor coverings.

2.	Division 9 Section "Resilient Flooring" for resilient wall base and accessories 					installed with carpet.

1.02	SUMMARY

A.	This Section includes tufted carpets and double stick carpet pad.

B.	Related Sections include the following:

1.	Division 2 Section "Selective Demolition and Alternations" for removing 						existing floor coverings.

2.	Division 9 Section "Resilient Flooring" for resilient wall base and accessories 					installed with carpet.

1.03	SUBMITTALS

A.	General:  Submit in accordance with Section 01330.

B.	Product Data:  For each type of product indicated. Include manufacturer's written data on 				physical characteristics, durability, and fade resistance. Include installation 					recommendations for each type of substrate required.

- Shop Drawings – Show the following:

1.	Columns, doorways, enclosing walls or partitions, built-in cabinets, and locations 				where cutouts are required in carpet.

2.	Carpet type, color and dye lot.

3.	Seam locations, types and methods.

4.	Type of installation for each type of substrate.

5.	Pattern type, repeat size, location, direction, and starting point.

6.	Type, color, and location of edge, transition and other accessory strips.

7.	Transition details to other flooring materials.

8.	Carpet pad type and installation.

D.	Samples:  For each of the following products and for each color and texture required. Label 	each sample with manufacturer's name, material description, color, pattern, and designation 	indicated on drawings and in schedules.

1.	Carpet:  12-inch square sample.

2.	Exposed Edge Stripping and Accessory:  12-inch long samples.

E.	Test Results:  Provide results of specified moisture tests and manufacturer's written 	moisture requirements for each type of carpet specified.

F.	Maintenance Data:  For carpet to include in maintenance manuals specified in Division 1.	Include 	the following:

1.	Methods for maintaining carpet, including cleaning and stain removal products and 			procedures and manufacturer's recommended maintenance schedule.

2.	Precautions for cleaning materials and methods that could be determined to carpet.

1.04	QUALITY ASSURANCE

A.	Fire-Test-Response Characteristics:  Provide products with the critical radiant flux 				classification indicated in Part 2, as determined by testing identical products per ASTM E 			648 by an independent testing and inspecting agency acceptable to authorities having 				jurisdiction.

B.	Source Limitations:  Obtain each type of carpet through a single source from a single 				manufacturer.

C.	Preinstallation Conference:  Conduct conference at project site. Review specified 				moisture test results, installation process, adhesive application, seam sealing procedures 				and seam layouts.

1.05	DELIVERY, STORAGE, AND HANDLING

A.	General:  Comply with CRI 104, Section 5, "Storage and Handling".

B.	Deliver materials to project site in original factory wrappings and containers, labeled with 			identification of manufacturer, brand name, and lot number.

C.	Store materials on-site in original undamaged packages, inside well ventilated area 				protected from weather, moisture, soilage, extreme temperatures, and humidity. Lay flat 				with continuous blocking off floor.

1.06	PROJECT CONDITIONS

A.	General:  Comply with CRI 104, Section 7.2, "Site Conditions: Temperature and 					Humidity" and Section 7.12, "Ventilation".

B.	Environmental Limitations:  Do not install carpet until wet work in spaces is complete 				and dry, and ambient temperature and humidity conditions are maintained and will 				continuously be maintained at the levels indicated for project when occupied for its 				intended use.

D.	Do not install carpet over concrete slabs until slabs have cured and are sufficiently dry to 				bond with adhesive and concrete slabs have pH range recommended by carpet 					manufacturer.

1.07	WARRANTY

A.	General Warranty:  Special warranty specified in this article shall not deprive owner of 				other rights owner may have under other provisions of the contract documents and shall 				be in addition to, and run concurrent with, other warranties made by contractor under 				requirements of the contract documents.

B.	Special Carpet Warranty:  Written warranty, signed by carpet manufacturer agreeing to 				replace carpet that does not comply with requirements or that fails within specified 				warranty period. Warranty does not include deterioration or failure of carpet due to 				failure of substrate, vandalism, or abuse. Warranty shall not require the use of chair pads. 				Failures include, but are not limited to, more than 10 percent loss of face fiber, edge 				raveling, snags, zippering, backing resiliency loss, and delamination.

PART 2 – PRODUCTS

2.01	CARPET

A.	C-1:  Shall be J&J Commercial Flooring.  Collection: The Art & Soul Collection, style 				Cubism 4830 in color indicated on Interior Finish Legend; no substitutions. No seconds 				or imperfections shall be acceptable. Carpet shall meet the following minimum 					construction:

1.  Style No. 	7483M

2.  Yarn  	100% Nylon: 100% Solutia 6.6 Ultron®			Prismatic Bulked Continuous Filament

3.  Dye Method  	Beck Dyed

4.  Surface Texture	Dense Patterned Loop

5.  Patterning Technique	None

6.  Pattern Repeat  	12" W x 24" L approx. (60.96 x 60.96 cm)

7.  Gauge  	1/12 (4.72 tows/cm)

8.  Tufted Stitches per Inch	10

9.  Yarn Weight	30 oz/sy (1017 grams/m2)

10. Finished Pile Thickness	.179 inch (4.55 cm) (ASTM D-418)

11. Density  	6,353

12. Weight Density  	190,590

13. Secondary Backing  	Nexus® Modular

14. Special Treatments	ProTex® - Fluorochemical (Standard)

Colorloc® Plus

(optional with a 100 sq. yd. minimum)

15. Tile Size	24 in x 24 in

16. Flammability		Class 1

17. Smoke			Less than 450 blaming

18. Static Generation	Less than 3.0 kv (AATCC-134)

19. ADA Compliance	Compliant for Accessible Routes

20. Warranties		Lifetime Wear

Lifetime Static

Lifetime Against Delamination

Lifetime Against Tuft Bind Failure (edge ravel, yarn 					pulls, zippering)

Lifetime Dimensional Stability

21. Recommended Installation	Monolithic, quarter-turn, ashlar.

B. 	C-2:  Shall be J&J Commercial Style:  Textures 36 in color indicated on Interior Finish 				Legend; no substitutions. No seconds or imperfections shall be acceptable. Carpet 				shall meet the following minimum construction:

1.  Manufacturer Style No. 	4655

2.  Product Type 	Broadloom

3.  Yarn	100% Solutia 6.6 BCF nylon

4.  Dye Method  		Beck

5.  Surface Texture			Textured cut and loop

6.  Patterning Technique	Technoweave 1

7.  Gauge	1/8

8.  Yarn Weight		36 oz/sq. yd.

9.  Finished Pile Thickness	.22 inch

10. Density		5,891

11. Secondary Backing	Actionbac®

12. Special Treatment 	ProTex® Fluorochemical

13. Width				12 feet (3.658 m)

14. Warranties	 		15 Year Limited Wear

Lifetime Static

3 Year Warranty Against Delamination, and tuft 									bind failure) edge ravel, yarn pulls, zippering)

C.	C-3:  Invision® Style Name: Tussah in color indicated on Interior Finish Legend; no 				substitutions. No seconds or imperfections shall be acceptable. Carpet shall meet the 				following minimum requirements:

1.  Manufacturer Style No. 	Tussah 9144

2.  Patterning Technique	Inter-Lok Tufting System

3.  Gauge	10 rows/inch (3.94 rows/cm)

4.  Finished Pile Thickness	0.210 inch (5.33 mm)

5. Yarn Weight		37 oz/y2 (1,255 g/m2)

6. Pattern Repeat	24 in. x 28 in. (approximate)

60.96 cm x 71.12 cm (approximate)

7. Face Yarn	 	Solutia Ultron®Color Nylon 6, BCF w/Permanent 								Static Protection

9.  Dye Method		Piece Dyed

10. Secondary Backing	ActionBac®

11. Special Treatment	Solutia Approved Carpet Protector

12. Standard Width		12 feet (3.658 m)

13. Physical Testing		Flooring Radiant Panel - (Class 1), Pill Test - (Passes),

Smoke Density - Less than 450 flaming,

ADA compliance (compliant for accessible routes),

CRI indoor air quality testing program #39158636

14. Warranties	 		Lifetime Wear Warranty

Lifetime Static Protection Warranty

3 Year Limited Warranty Against Manufacturing 									Defects

D.	C-4:  Shall be J&J Commercial Flooring.  Collection: The Art & Soul Collection, style 		Surrealism 482Din color indicated on Interior Finish Legend; no substitutions. No seconds 	or imperfections shall be acceptable. Carpet shall meet the following minimum construction:

1.  Style No. 	482D

2.  Yarn  	100% Nylon: 100% Solutia 6.6 Ultron®			Prismatic Bulked Continuous Filament

3.  Dye Method  	Beck Dyed

4.  Surface Texture	Dense Patterned Loop

5.  Patterning Technique	None

6.  Pattern Repeat  	.625" W x .000" L

7.  Gauge  	1/10 (3.94 rows/cm)

8.  Yarn Weight	28 oz./sq. yd. (949 grams/m2)

9. Finished Pile Thickness	.15 inch (3.81 cm)

10. Density  	6,720

11. Secondary Backing  	Action Bac

12. Special Treatments	ProTex® - Fluorochemical (Standard)

Colorloc® Plus

(optional with a 100 sq. yd. minimum)

13. Width:	12 feet (3.66 m)

14. Flammability		Class 1

15. Smoke			Less than 450 blaming

16. Static Generation	Less than 3.0 kv (AATCC-134)

17. ADA Compliance	Compliant for Accessible Routes

2.02	INSTALLATION ACCESSORIES

A.	Concrete Slab Primer:  Nonstaining type provided or recommended by the carpet 					manufacturer.

B.	Trowelable Leveling and Patching Compounds:  Portland-cement-based formulation 				provided by or recommended by carpet manufacturer.

C.	Adhesives:  Premium grade, water-resistant, mildew-resistant, nonstaining type to suit 				products subfloor conditions indicated, that complies with flammability requirements for 				installed carpet and that is recommended by the carpet manufacturer, permitting a 				moisture emission rate up to 5 lb/1000 sq.ft./24 hours.

D.	Seaming Cement:  Adhesive product recommended by carpet manufacturer for sealing 				seams and butting cut edges at backing to form secure seams.

PART 3 – EXECUTION

3.01	EXAMINATION

A.	Examine substrates, areas, and conditions, with Installer present, for compliance with 				requirements for maximum moisture content, alkalinity range, installation tolerances, and 			other conditions affecting carpet performance. Verify that substrates and conditions are 				satisfactory for carpet installation and comply with requirements specified.

B.	Concrete Subfloors:  Verify that concrete slabs comply with ASTM F-710 and the 				following:

1.	Slab substrates are dry and free of curing compounds, sealers, hardeners, and other 					materials that may interfere with adhesive bond. Determine adhesion and dryness 					characteristics by performing bond and moisture tests recommended by carpet 					manufacturer, carpet cushion manufacturer, and with the following specified 					requirements:

a.	An independent testing agency shall perform calcium chloride moisture tests 						on concrete slabs-on-grad and elevated slabs to receive carpeting at the rate of 						1 test per 1000 sq. ft. of floor area at locations receiving glue down installation.

b.	Maintain a minimum temperature of 70 degrees Fahrenheit in spaces to be 						tested for at least 72 hours prior to and during the tests.

c.	Tests shall be conducted in accordance with ASTM F-1869-02, except that the 						area of the CaC12 dish shall not be deducted.

2.	Concrete pH Test:  Perform pH tests on concrete floors regardless of age or grade 					level.

3.	Subfloor finishes comply with requirements specified in Division 3 Section "Cast-					in-Place Concrete" for slabs receiving carpet.

4.	Subfloors are free of cracks, ridges, depressions, scale and foreign deposits of any 					kind.

C.	If conditions detrimental to work are encountered, prepare written report, signed by the 				Installer, documenting unsatisfactory conditions and send to the Architect.

D.	Proceed with installation only after unsatisfactory conditions have been corrected.

3.02	PREPARATION

A.	General:  Comply with CRI 104, Section 6.2, "Site Conditions: Floor Preparation", and 				carpet manufacturer's written installation instructions for preparing substrates indicated to 			receive carpet installation.

B.	Use towelable leveling and patching compounds, according to manufacturer's written 				instructions, to fill cracks, holes, and depressions in substrates using product 					recommended by manufacturer.

C.	Level subfloor with ¼-inch in 10 feet, noncumulative in all directions using product 				recommended by manufacturer. Sand or grind protrusions, bumps, and ridges.

1.	Use leveling and patching compounds to fill cracks, holes, and depressions in 					subfloor as recommended by carpet manufacturer.

D.	Remove coatings, including curing compounds, and other substances that are 					incompatible with adhesives and that contact soap, wax, oil, or silicone, without using 				solvents. Use mechanical methods recommended in writing by the carpet manufacturer.

E.	Existing Floor Slabs:  Scrape and remove adhesive from floor where existing floor 				coverings are removed. Trowel-apply underlayment, compound over entire floor to 				smooth substrate surface and prevent telegraphing of surface irregularities.

F.	Broom and vacuum clean substrates to be covered immediately before installing carpet. 				After cleaning, examine substrates for moisture, alkaline salts, carbonation, or dust. 				Proceed with installation only after unsatisfactory conditions have been corrected.

G.	Concrete Subfloor Preparation: Apply concrete slab primer, according to manufacturer's 				directions, where recommended by the carpet manufacturer.

3.03	INSTALLATION

A.	Direct-Glue-Down Installation:  Comply with RI 104, Section 9, "Direct-Glue-Down 				Installation", and manufacturer's requirements.

B.	Stair Installation:  Comply with CRI 104, Section 13, "Carpets on Stairs" and 					manufacturer's requirements.

C.	Comply with manufacturer's recommendations for seam locations and directions of 				carpet; maintain uniformity of carpet direction and lay of pile. At doorways, center seams 			under door in closed position.

D.	Where demountable partitions or other items are indicated for installation on top of 				finished carpet, install carpet before installation of these items.

E.	Cut and fit carpet to butt tightly to vertical surfaces, permanent fixtures, and built-in 				furniture including cabinets, pipes, outlets, edgings, thresholds, and nosings. Bind or seal 				cut edges as recommended by carpet manufacturer.

F.	Extend carpet under removable flanges and furnishings and into alcoves and closets of 				each space.

G.	Maintain references markers, holes and openings that are in place or marked for future 				cutting by repeating on finish flooring as marked on subfloor. Use nonpermanent, 				nonstaining marking device.

H.	Install pattern parallel to walls and borders.

3.04	CLEANING AND PROTECTION

A.	Perform the following operations immediately after installing carpet:

1.	Remove excess adhesive, seam sealer, and other surface blemishes using cleaner 					recommended by carpet manufacturer.

2.	Remove yarns that protrude from carpet surface.

3.	Vacuum carpet using commercial machine with face-beater element.

B.	Protect installed carpet to comply with CRI 104, Section 16, "Protection of Indoor 				Installations".

C.	Protect carpet against damage from construction operations and placement of equipment 				and fixtures during the remainder of construction period. Use protection methods 					indicated or recommended in writing by carpet manufacturer to ensure carpet is without 				damage or deterioration at the time of Substantial Completion.

END OF SECTION 09680