SECTION 12356

RESIDENTIAL CASEWORK

PART I – GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract, including General and 						Supplementary Conditions and Division 1 Specifications Sections, apply to this 					Section.

1.02	SUMMARY

A.	This Section includes the following:

1.	Wood-faced kitchen cabinets.

B.	Related Sections include the following:

1.	Division 6, Section "Architectural Woodwork" for custom fabricated cabinets 				and countertops.

2.	Division 11, Section "Residential Appliances" for appliances.

3.	Division 15 Sections for sinks and for plumbing fittings.

4.	Division 16 Sections for conduit and connections installed in casework for 					residential appliances.

1.03	DEFINITIONS

A.	Exposed Surface of Cabinets:  Surfaces visible when doors and drawers are closed, 			including visible surfaces in open cabinets or behind glass doors.

B.	Semi-exposed Surfaces of Cabinets:  Surfaces behind opaque doors or drawer fronts, 			including interior faces of doors and interiors and sides of drawers. Bottoms of wall 			cabinets are defined as "semi-exposed".

C.	Concealed Surfaces of Cabinets:  Surfaces not usually visible after installation, including 			sleepers, web frames, dust panels, bottoms of drawers, and ends of cabinets installed 			directly against and completed concealed by walls or other cabinets. Tops of wall cabinet 			and utility cabinets are defined as "concealed".

1.04	SUBMITTALS

A.	General:  Submit in accordance with Section 01330.

B.	Product Data for the following:

1.	Cabinets

2.	Cabinet hardware.

C.	Shop Drawings:  Include plans, elevations, details, and attachments to other work.

D.	Samples for Verification:  For the following materials; in sets showing the full range of 			color, texture, and pattern variations expected:

1.	Wood-veneered panels with transparent finish, 8-inches by 10-inches, for each 				species.

2.	Solid wood with transparent finish, 50-sq. inches for each species.

3.	Solid wood trim with transparent finish, 8-inches long, for each species.

4.	Thermoset decorative panels for cabinet interior finish, 8-inches by 10-inches.

5.	One unit of each type of exposed hardware.

1.05	QUALITY ASSURANCE

A.	Source Limitations for Cabinets:  Obtain cabinets type through one source from a 		single	manufacturer.

B.	Quality Standards:  Unless otherwise indicated, comply with the following 				standards:

1.	Cabinets: KCMA A161.1.

a.	KCMA Certification:  Provide cabinets with KCMA's "Certified 						Cabinet" seal affixed in a semi-exposed location of each unit and 						showing compliance with the above standard.

1.06	PROJECT CONDITIONS

A.	Environmental Limitations:  Do not deliver or install casework until building is 				enclosed, wet-work is complete, and HVAC system is operating and maintaining 				temperature and relative humidity at occupancy levels during the remainder of the 			construction period.

B.	Established Dimensions:  Where casework is indicated to fit to other construction, 			establish dimensions for areas where casework is to fit. Coordinate construction to 			ensure that actual dimensions correspond to established dimensions. Provide 				fillers and scribes to allow for trimming and fitting.

C.	Field Measurements for Countertops:  Verify dimensions of countertops by field 				measurements after base cabinets are installed but before countertop fabrication is 			complete. Coordinate fabrication schedule with construction progress to avoid 				delaying the Work.

1.07	COORDINATION

A.	Coordinate layout and installation of blocking and reinforcement in partitions for 	support 	of casework.

PART 2 – PRODUCTS

WOOD CABINETS

A.	Products:  Premier Series Casework:  Armstrong World Industries, Inc.

1.	Style:  Berkshire Maple Cabinetry with Vanilla Cream finish at the following 				locations:

a.	Lunchroom 334.

b.	Supply/Storage 336

2.	Upgrade:  Provide dovetail drawers with full extension drawer glides and wood 				panels for all exposed locations.

3.	Door and Drawer Pulls:  KraftMaid #205, Brushed Chrome Finish.

B.	Face Style:  Reveal overlay; door and drawer faces partially cover cabinet fronts.

C.	Cabinet Style:  Face Frame.

D.	Door and Drawer Fronts:  Solid wood.

E.	Face Frames:  3/4-inch by 1 5/8-inch solid wood to match exposed species.

F.	Exposed Cabinet End Finish:  Wood veneer, exterior veneer to match cabinet species, 			interior veneer to be manufacturer's standard.

1.	Exposed cabinet ends shall include ends of cabinets exposed at knee spaces, open 				sink bases, and similar conditions.

G.	Cabinet End Construction:  ½-inch thick plywood.

H.	Cabinet Tops and Bottoms:  ½-inch thick particleboard, fully supported by and secured in 		rabbets in end panels, front frame, and back rail.

I.	Back, Top, and Bottom Rails:  Solid wood, interlocking with end panels and rabbeted to 			receive top and bottom panels. Back rails secured under pressure with glue and with 			mechanical fasteners.

J	Wall-Hung-Unit Back Panels:  1/8-inch thick hardboard fastened to rear edge of end 			panels and to top and bottom rails.

K.	Base-Unit Back Panels:  1/8-inch thick hardboard fastened to rear edge of end panels and 			to top and bottom rails.

L.	Drawers:  Fabricate with exposed fronts fastened to subfront with mounting screws from 			interior of body.

M.	Shelves:  5/8-inch thick particleboard.

N.	Joinery:  Rabbet backs flush into end panels and secure with concealed mechanical 			fasteners. Connect tops and bottoms of wall cabinet and bottoms and stretchers of base 			cabinets to ends and dividers with mechanical fasteners. Rabbet tops, bottoms, and backs 			into end panels.

O.	Factory Finishing:  Finish cabinets at factory. Defer only final touch up until after 			installation.

2.02	CABINET HARDWARE

A.	Pulls:  Back-mounted decorative pulls.

B.	Hinges:  Concealed European style self-closing hinges.

C.	Drawer Guides:  Epoxy coated metal, self-closing, full extension drawer guides; 				designed to prevent rebound when drawers are closed; with nylon-tied, ball-				bearing rollers; 100 pound capacity.

D.	Drawer and Door Locks:  Cylindrical type, 5-pin tumbler and cam, satin nickel 				finish, complying with BHMA A156.11, Grade 1.

1.	Provide minimum of 2 keys per lock and 2 master keys.

2.	Location:  All doors and drawers in all Med Rooms; key according to Owner's 				instructions.

PART 3 – EXECUTION

3.01	INSTALLATION

A.	Install cabinets with no variations in flushness of adjoining surfaces; use concealed 			shims. Where cabinets abut other finished work, scribe, and cut for accurate fit. Provide 			filler strips, scribe strips, and moldings in finish to match cabinet face.

B.	Install cabinets without distortion so doors and drawers fit openings and are aligned. 			Complete installation of hardware and accessories as indicated.

C.	Install cabinets and countertop level and plumb to a tolerance of 1/8-inch in 8-feet.

D.	Fasten cabinets to adjacent units and to backing.

1.	Fasten wall cabinets through back, near top and bottom, at ends and not less than 				24-inches o.c. with No. 10 wafer-head screws sized for 1¼-inch penetration into 				concealed wood blocking, or hanging strips.

3.02	ADJUSTING AND CLEANING

A.	Adjust cabinets and hardware so doors and drawers are centered in openings and operate 			smoothly without warp or bind. Lubricate operating hardware as recommended by 			manufacturer.

B.	Clean casework on exposed and semi-exposed surfaces. Touch up factory applied 			finishes restoring damaged or soiled areas.

END OF SECTION 12356