###### Section 09220

Direct Applied Base Coat

# PART I:  GENERAL

1.01	DESCRIPTION

Provide labor, materials, equipment and supervision necessary to complete the application of product to the substrate.

1.02	QUALITY ASSURANCE

Products shall be installed by a trained applicator with a minimum of five years experience and meet the requirements of the specifier.

1.03	SUBMITTALS

- Manufacturer’s current product data bulletin.

- The trained applicator shall prepare a test panel of the repair installed on the actual building as a submittal for approval of proper application and adhesion.

- The trained applicator shall submit to the specifier a list of five projects that he has completed within the last five years, exhibiting the applicator’s skills. The list shall include project name, location, and description of work and completion date.

1.04	PRODUCT DELIVERY, STORAGE & HANDLING

- Deliver all products and all accessories in original labeled, sealed, and undamaged containers or bundles.

- Store all products in accordance with manufacturer’s printed instructions.

- Handle products in accordance with manufacturer’s printed instructions.

1.05	JOB CONDITIONS

All products shall be applied at substrate and ambient temperatures of 40°F or above. A minimum temperature of 40°F shall be maintained 24 hours after completion of work. Protect products from weather and other damage for a period of 24 hours after installation. Do not apply products to frozen surfaces.

  - COORDINATION & SCHEDULING

The work requires close coordination with related sections and trades.

PART II:  PRODUCTS

2.01	MANUFACTURERS

The following manufacturers are approved for the project.

Conproco Corporation

2.02	MATERIALS

- Conpro Start: A water-based consolidant, used to stabilize and strengthen concrete, masonry and stone.

- Structural Skin: Fiber-reinforced cement coating for vertical interior and exterior surfaces.

- K-88 Admix: An acrylic admix designed to enhance the performance of cement-based products.

2.03	PERFORMANCE CHARACTERISTICS

General Physical Properties:  The products shall meet or exceed the following performance standards:

Conpro Start:

| Physical state and appearance |  | Slightly clouded liquid |
| --- | --- | --- |
| Base |  | Aqueous |
| Odor |  | Slight alcohol |
| pH |  | >12 |
| Actives type |  | Inorganic mineral silicate |
| Solvent system |  | Water |
| Percent solids by weight |  | 8.35% |
| Flash point | ASTM D56 | >200°F Seta cc |
| Density of liquid coatings | ASTM D1475 | 8.4 lbs./gal. |
| Gain on mortar: |  | psi | % gain |
| Compressive strength | ASTM C109 |  |  |
| Prior to treatment |  | 990 |  |
| After treatment |  | 1700 | 71 |
| Gain on old concrete: |  | psi | % gain |
| Compressive strength | ASTM C109 |  |  |
| Prior to treatment |  | 3700 |  |
| After treatment |  | 3900 | 8 |

Structural Skin:

| Physical state and appearance |  | Gray or white powder |
| --- | --- | --- |
| Base |  | Portland cement |
| pH |  | >12 |
| Water/cement ratio |  | 0.6 – 0.49 with 2 quarts K-88 Admix |
| Setting time by vicat needle | ASTM C191 | Initial 60 minutes – Final 270 minutes |
| Durometer hardness | ASTM D2240 | 60-70 |
| Water penetration and leakage | ASTM E514 | 100% reduction in leakage |
| Carbon-arc weathering | ASTM G152 | 2000 hours - no effect |
| Length change | ASTM C157 | 300 µstrains @ 28 days |
|  |  | 7 Days | 14 Days | 28 Days |
| Compressive strength – psi With 2 quarts of K-88 Admix | ASTM C109 | 4150 5000 | 4400 5290 | 5100 6300 |
| Flexural strength – 3 point loading - psi | ASTM C78 |  |  | 1100 |
| Tensile strength – psi With 2 quarts of K-88 Admix | ASTM C307 | 400 600 | 430 600 | 430 635 |
| Allowable design stress based on gross area of the CMU (IBC) for mortar-less wall construction |
| Compressive stress – psi Standard block Ground block Shear stress |  | 45 85 10 |
| Tensile stress in flexure, vertical span - psi |  | 18 |

K-88 Admix:

| Physical state and appearance |  | Milky liquid |
| --- | --- | --- |
| Base |  | Aqueous |
| Polymer |  | 100 acrylic |
| Odor |  | Ammoniacal |
| pH |  | >8 |
| Percent solids by weight |  | 27% |
| Density of liquid coatings | ASTM D1475 | 8.4 lbs./gal. |
| Results typical for 3/4 – 3 inch mix |  | 7 Days | 14 Days | 28 Days |
| Compressive strength Design mix without K-88 Admix – psi Design mix with K-88 – psi Percent increase - % | ASTM C109 | 2725 3400 25 | 3375 4150 23 | 3725 4700 26 |
| Tensile strength Design mix without K-88 – psi Design mix with K-88 Admix – psi Percent increase - % | ASTM C307 | 95 385 30 | 360 390 8 | 360 400 11 |

PART III:  EXECUTION

3.01	GENERAL

- Installation shall be performed strictly in accordance with manufacturer’s current product data bulletin.

- Examine substrates and conditions under which materials will be installed.  Do not proceed with installation until unsatisfactory conditions are corrected.

- Coordinate installation with adjacent work to ensure proper sequence of construction.  Protect adjacent areas and landscaping from contact due to mixing, handling and application of materials.

3.02	SURFACE PREPARATION

- Remove loose and deteriorated material, laitance, dirt, dust, oil and any surface contaminants that will inhibit proper bond

- The substrate shall be flat, having no plane irregularities greater than 1/4".

  - MIXING

  - Conpro Start:  Mix until homogenous.

  - Structural Skin:

    - Place one 2 quarts of K-88 Admix and 2 to 3 quarts of water in a clean mortar mixer.

    - Add one 50 lb. bag of Structural Skin and mix for one to two minutes.  Avoid over mixing.

    - Add up to 1-pint water as need to obtain desired consistency.

    - Allow to breath for 1 minute and remix for 1 minute.

    - Apply immediately after mixing.  DO NOT retemper material once mixed.

  - APPLICATION

- Conpro Start:

  - All surfaces to be repaired shall be consolidated with Conpro Start by applying with brush, roller, or sprayer.

  - Surface should be saturated, but not flooded.

  - Allow approximately 12 hours for Conpro Start to cure.  Refer to data sheet for detailed instructions.

- Structural Skin (with 2 quarts of K-88 Admix)

  - Dampen substrate and keep moist prior to application.

  - Trowel Structural Skin to a minimum of 1/8”.  Apply with sufficient pressure to form a good key with the substrate.

  - Whenever possible, the entire wall panel shall be covered without stopping.  Interruptions of work will only be made at control joints, corners, and wall stops.

  - Trowel smooth to provide a surface receptive to the finish coat.

  - Allow Structural Skin approximately 24 hours to cure before subsequent finishes.

  - Curing

  - Keep Structural Skin damp with a fine mist of water for 24 hours when temperatures exceed 750 F.

  - Protect from direct sunlight, wind, rain, and frost during the curing period.

  - JOB SITE CLEANUP

A.	Material left over at the job site by the approved applicator shall be removed.

B.	All adjacent surfaces and materials shall be cleaned.

C.	Any foreign material resulting from the work of the approved applicator shall be removed.

*****END OF SECTION*****

17 PRODUCTION DRIVE, DOVER, NEW HAMPSHIRE 03820

TELEPHONE 800.258.3500   FAX 603.743.5744  WEB ADDRESS www.conproco.com