SECTION 02320

SLOPE PROTECTION AND EROSION CONTROL

PART 1  GENERAL

1.01	SECTION INCLUDES

A.	Temporary silt fence.

B.	Erosion control mesh.

C.	Hay bales, temporary erosion checks.

D.	Stone check dams.

E.	Plain riprap - machine placed stones on filter fabric.

1.02	RELATED SECTIONS

A.	Section 02230- Site Clearing and Grubbing.

B.	Section 02315 - Common Excavation, Embankment and Compaction.

1.03	ENVIRONMENTAL REQUIREMENTS

A.	Conform to Maine Department of Environmental Protection publication "Maine Erosion and Sediment Control Handbook for Construction:  Best Management Practices".

B.	Maintain erosion control installations in a functional condition at all times.  Inspect after each rainfall and at least daily during prolonged rainfall.  Immediately correct deficiencies

PART 2  PRODUCTS

2.01	MATERIALS

A.	Silt Fence:  MDOT Section 656.03.

B.	Erosion Control Mesh:  MDOT Section 717.061.

C.	Hay Bales:  Baled hay approximately 14" by 18" by 30" securely tied to form a firm bale.

D.	Plain Riprap:  MDOT Section 703.26.

E.	Stone check dams:  Crushed stone.

F.	Filter Fabric:  Mirafi 600x or Approved Equal.

PART 3  EXECUTION

3.01	EXAMINATION

A.	Verify that surfaces are ready to receive work.

B.	Beginning of installation means installer accepts existing surface conditions.

3.02	INSTALLATION

A.	Install silt fences before beginning excavation.

B.	Install silt fences in accordance with MDOT 656.08.

C.	Install erosion control mesh in accordance with MDOT 613.

D.	Install hay bales in accordance with MDOT Section 656.

E.	Install plain riprap in accordance with MDOT 610 with the exception that plain riprap shall be installed on filter fabric installed per manufacturer's recommendations.

3.03	FIELD QUALITY CONTROL

A.	Inspect and repair temporary erosion control measures at least weekly and after any significant storm.  A significant storm shall be defined as over 1 inch of precipitation in any consecutive 24 hour period.

3.04	MAINTENANCE

A.	Maintain erosion control installations in a functional condition at all times.  Inspect after each rainfall and at least daily during prolonged rainfall.  Immediately correct deficiencies

B.	Make a daily review of the location of erosion control measures in areas where construction activity causes drainage runoff to ensure that erosion control measures are properly located for effectiveness.

C.	Where deficiencies exist, install additional erosion control measures as approved or directed by the Owner.  No additional payment shall be made for additional erosion control measures which may be required.

3.05	TEMPORARY EROSION CONTROL REMOVAL

A.	Remove temporary silt fence and hay bales when no longer needed and dispose of in a proper manner.

B.	Remove stone check dams when no longer needed and dispose of in a proper manner.  Stone shall be raked out to a maximum depth of one layer to allow future vegetation to grow through the stone.

END OF SECTION