SECTION 09300

TILE

1. 	GENERAL

1.1	REFERENCES

A.  	Drawings and general provisions of Contract, including General Conditions and Division 1 			specifications, apply to work in this section.

B.  	Cast-in-Place Concrete:  Section 03300

C.  	Joint Sealants:  Section 07900

- Gypsum Drywall:  Section 09250

E.  	American National Standards Institute (ANSI)

1.2  	DESCRIPTION OF WORK:  Extent of Tile Work is shown on the drawings.

1.3  	QUALITY ASSURANCE

A.  	Tile materials and installation shall comply with recommendations of Tile Council of America 		Handbook for Tile Installation, and ANSI Standard Specification Series A108, A118, A136, 			and A137, as applicable.

B.  	The use of asbestos shall not be permitted in any product specified in this Section.

1.4  	SUBMITTALS

A.  	Submittals under this Section shall include manufacturers' data and installation instructions on 		all specified products; manufacturer's standard color range; and full size tile of each type and 			color of tile specified.

C.  	At job completion, supply two copies of manufacturers' maintenance instructions; and 1 				percent minimum of all types and colors of material provided under this Section as replacement 		stock, neatly packaged and clearly labeled.

2.   	PRODUCTS

2.1  	TILE

A.  	“Dal Terra Antica” Porcelain tile, color Celeste/Grigio TA04

B.  	Provide all matching trim necessary for finished installation, including stretcher pieces, cove 			bases, square inside corners, bullnose trim at outer corners and where tilework projects from 			jambs.

C.  	Where floor tile terminates against dissimilar flooring  material, provide aluminum threshold 			beveled as required for field conditions, centered under door or within frame, unless noted 			otherwise.

D.  	Colors to be chosen by Architect from manufacturer's full range of colors.

2.2  	SETTING AND GROUTING MATERIALS

A.  	Factory-mixed materials shall be by Boiardi Elastiment, C-Cure, H. B. Fuller, Laticrete, L&M 		Surco, Upco, or other manufacturer approved by tile manufacturer.  Setting bed, grout, and 			additive materials shall be by same manufacturer.

B.  	Tile shall be thin-set, using one of following:

1.  	Dry-set mortar: factory mixture of portland cement, sand, and water-retentive additives, 				mixed with water in field, complying with ANSI A118.1, as recommended by 						manufacturer for particular type of tile used.

2.  	Latex-portland cement mortar: factory mixture of portland cement and sand, with 					powdered PVA polymer or liquid PVA, styrene butadiene, or acrylic latex admixture 				added in field, complying with ANSI A118.4.

C.  	Grout tile with factory-formulated portland cement, dry-set, or latex portland cement grout 			(either acrylic or styrene butadiene powder or liquid additive), complying with ANSI 118.6.  			On-job sand-portland cement mixture may also be used, complying with ANSI A108.1.  Color 		to be selected from manufacturer's standard range.

2.3  	Concrete Sealer:  Provide manufacturer's recommended sealer compatible with concrete floor.

3.   	EXECUTION

3.1  	INSTALLATION

A.  	Provide floor protection to existing buildings when renovating or adding on.

B.  	Before beginning installation inspect surfaces to receive tile for excessive dampness, 				irregularity, loose material, oily or waxy areas impeding adhesion, or other conditions which 			would prevent proper installation.  Verify that surfaces are flat to within 1/4 in. in 10 ft., with 			no vertical irregularities exceeding 1/16 in. high.  Seal concrete floors if recommended or 			approved by the manufacturer.  Broom clean substrate before beginning installation.  				Commencement of work constitutes acceptance of floor condition.

C.  	Expansion joint location and construction shall conform to drawings and ANSI A108, 				Paragraph A-3.4, including requirement for joints over cold-pour, saw-cut, control, and 				structural joints.  Sealant materials and installation procedures are specified in Section 07900, 		Joint Sealants.

D.  	Mix dry-set and latex-portland cement mortars in accordance with manufacturer's instructions.

1.  	For dry-set mortars, add dry ingredients to water.  Mix thoroughly and allow mortar to 				stand 15 minutes, then re-mix.  Do not add water, additional mortar, or other ingredients 				after slaking period.

2.  	For latex-portland cement mortars, use brand of pre-packed dry mortar mix specified by 				latex manufacturer.  Add dry mortar to correct amount of latex, as specified by 					manufacturer, and mix thoroughly to obtain complete and visually uniform wetting of dry 			mortar mix.  When directions require dilution of latex with water, this shall be done with 				adequate mixing before dry mortar mix is added.  Slake for 15 minutes and re-mix before

using.

3.  	Spread mortar with notched trowel of type recommended by manufacturer.  Setting 					compound shall be of such consistency that ridges formed by trowel shall not flow or 				slump.  Cover surface uniformly without bare spots.  Apply setting compound only to as 				much area as can be covered with tile before mortar skins over.  Remove dried mortar, and 			apply new material.  Protect mortar from foot traffic and dirt.

E.  	Press individual tiles or tile sheets into mortar, maintaining accurate joint alignment and 				spacing.  Beat in tile with rubber-faced block to obtain maximum contact between tile back and 		setting compound.  Remove paper and glue from paper-mounted ceramic mosaics before 				mortar is firmly set, and align individual tiles.  Immediately remove setting compound from 			faces or front edges of tiles.

F.  	Center and balance tile areas.  Smooth cut edges.  Jagged or flaked edges or split tiles are 			prohibited.  Cuts shall be no smaller than half size, located on outer edges of field.  Make 			corners of all tile flush and level with corners of adjacent tile, with due allowance to tolerances 		for tile as specified in ANSI A137.1.

G.  	Keep all joint lines straight and of even width, including miters.  Finish floor and wall areas 			shall be flat and plumb, with no variations exceeding 1/4 in. in 10 ft. from required plane.

H.  	Allow sufficient time for setting compound to cure before grouting, 48 hours minimum.  				Remove spacers or ropes from joints.  Using a grout of type and mix specified under 				PRODUCTS, force maximum amount of grout into joints.  Clean joints of cushion edge tile to 		depth of cushion.

I.  	Fill joints of square-edge tile flush with surface.  Fill all gaps and skips.  Do not permit mortar 		to show through grouted joints.  Finished grout shall be uniform in color, smooth and without 			voids, pinholes or low spots.

J.  	After mortar joints have cured, clean unglazed tile with proprietary acidic preparation such as 		Sure-Klean Grout and Tile Cleaner, in strict accordance with manufacturer's instructions.  			Apply solutions to test patches before cleaning.

END OF SECTION