## SPECIFICATIONS

SECTION 09419

POLOMYX( 
MULTICOLOR WALL FINISH

Multicolor Wall

PART 1    GENERAL

1.01 SECTION INCLUDES

	A.   Multicolor finishes.

1.02 RELATED SECTIONS

            A.    Concrete Masonry Unit, Section 04200

1.03 PERFORMANCE

A.   Fire Safety:   Class “A” Fire Rated.  				ASTM E 84 (81a)

Flame Spread 5     Smoke Density 0

B.   ContinuousColor(:  Complete integration of color

particles within and throughout the paint finish.

	C.   Scrubability:  2000 cycles slight wear. 				ASTM D 2486.

# D.   Washability:   No more than 5% change 			Fed Std 141

# in specular gloss 							Method 6142

E.   Coverage:   Up to 125-175 square feet per gallon

(up to 13-18 sq meters per gallons) pending pattern size,

surface porosity and method of application.

F.   Specular Gloss:   Maximum of 10 @ 60(.			ASTM D-523

G.  Mildew and Fungal Resistance:   No growth.			ASTM G21.

H.  Accelerated Weathering:  1000 hours. 				ASTM G23 and

ASTM D822.

I.    Stain Resistance:   Resistant to the following:			ASTM D 1308

- 50% ethyl alcohol,

- 3% acetic acid

- 5% ammonia

- heptane (lighter fluid)

- 1% triton x 100

- detergent

- ketchup, margarine, butter, orange juice, coffee

- water-based marker, red grease pencil, #2 lead pencil

- urine

- betadine

- blood

J.    Bacterial Resistance:  No growth.				ASTM G22.

	K.   Flashpoint:   D.O.T. - Not Regulated				ASTM 3278

OSHA - Not Applicable

L.   Color Fastness:   500 hours OK				Fed Std 141
									Method 4561

M.   Self Lifting:   No Lifting  (Excellent intercoat adhesion)		Fed Std 141

Method 6252

N.   Alkali Resistance:  Product withstands 10%			ASTM D 1308

sodium hydroxide for 3 hours.

O.   Strippability:  Polomyx can be recoated, painted

or covered with sheet goods without stripping.

P.   Freeze Thaw:  Integrity maintained with no 			ASTM D 2337-84

change in spray texture after 3 cycles.

Q.   Permeability:  3.49 perms (with SP202 pva basecoat) 		ASTM D 1653-93

1.04 SUBMITTALS

A    Color Samples:  Two samples of each color (5”x 8”).			
B.   Product Data:  Submit manufacturer's product data and installation instructions.
C.   Submit letter from manufacturer stating that applicator has completed manufacturer's

training program.
D.   Control Samples:  Submit a spray-out with each batch of finish coat to demonstrate that

batches match approved samples.

1.05 QUALITY ASSURANCE

A.   Job Mock-Ups:

1    Minimum 100 sq ft mock-up application of specified coating system on each

type of surface.  [Provide separate mock-up for each color blend.]
2.   Upon approval by specifier, mock-ups serve as standard for the work.

- Mockup shall remain as part of the completed project.

B.   Fire Ratings:

1.   Class A Fire Hazard Classification

2.   Test Procedure ASTM E-84

C.   Applicator Qualifications:

- Applicator shall certify in writing that technicians utilized for work in this section have been trained by the manufacturer or its representative.

- Applicator shall include in his certification that specialized equipment as required by the manufacturer will be used for work in this section.

D.   Manufacturer:

1.   Manufacturer to certify they make all materials in specification.

2.   All materials within special coatings section including finishes, primers and                  	                    basecoats will be supplied by one manufacturer.

1.06 DELIVERY, STORAGE, AND HANDLING

A.   Deliver materials in their original, unopened containers bearing manufacturer's

labels.
B.   Provide fire extinguisher in storage area.  Do not leave containers open.

Remove empty cans and rags with oil or solvent from building every day.

C.   Store between 50 and 85 degrees F.

1.07 PROJECT CONDITIONS					

	A.   Apply coating under following conditions:
		1.   Temperature of air and substrate is between 50 and 85 degrees F.

2.   Temperature of substrate is above dew point.
		3.   Substrate is dry to touch.

- Protect surfaces not to be coated.

- Provide adequate illumination.

- Provide adequate fresh air and ventilation during application.

1.08 MAINTENANCE MATERIALS

A.  Provide two [2] sheets of finished FastFix( by Zolatone samples for [each]                         color blend used.
B.   Submit fully equipped Zolatone Interior Finishes Maintenance Manual for end-user records.  Mamual can be obtained Righter Group, Inc.

- Extra Stock:  Provide one  [1] gallons of [each] color blend used.  Provide in sealed, labeled containers.

- Equipment:  Provide Zolatone Interior Finishes approved cup gun with internal mix cap.

PART 2    PRODUCTS

2.01 MANUFACTURERS

A.   Polomyx is manufactured by Surface Protection Industries, Inc.; 400 Charter Way, N. Billerica, Ma; phone (888) 765-6699, fax (978) 663-2885 or 3440 E. 14th St., Los Angeles, Ca. 90023 (323-265-9999), fax (323-980-1149).  Distributed by Righter Group, Inc.; phone (800) 848-4841. Polomyx is a registered trademark of Surface Protection Industries, Inc.  Polomyx is listed as a standard for quality and generic type. Equal products will not be considered unless approved prior to bidding

  - MATERIALS

A.  Primers, Sealers and Fillers:   Provide basecoats recommended by manufacturer for substrates.  Do not tint basecoats.

- SP92 High Performance Drywall Sealer

- SP203 Acrylic Drywall Basecoat

- SP206 High Solids Block Filler

B   Intermediate and Finish Coats:
1.   Polomyx traditional formula multicolor interior wall finish. Finish shall be ready-mixed, no tinting required.

2.03	EQUIPMENT

A.  	Apply with equipment recommended by coating manufacturer.   Use conventional air-spraying

equipment with internal mix spray gun air cap; dual-regulated, ASME Code Certified, 110-PSI pressure tank, and compressor sized to provide necessary volume of air to spray gun on a continuous basis.

2.04	COLORS

A.	Polomyx Waterbase Multicolor – PWQ ZD55

3.01 PRE-WORK INSPECTION

	A.   Verify that substrates are ready to receive work of this Section and are in accordance

with coating manufacturer's requirements.  Report any conditions that would adversely affect

the appearance or performance of the coating systems.

- Do not proceed with surface preparation and application until the surface is acceptable or

authorization is given by the specifier.  Beginning of application means acceptance of

substrates

3.02 SURFACE PREPARATION					

            A.  General

1   Protection:   Prior to all surface preparation and application operations, completely mask, remove or otherwise protect all hardware, accessories, plates, lighting fixtures, floors and similar items in contact with or in the vicinity of coating surfaces, but not scheduled to receive special coating.  Protect and store removed items.  Reinstall items after completion of coating application.

- Cleaning:  Before applying special coating, thoroughly clean all surfaces

involved.  All surfaces shall be clean, dry, and adequately protected from dampness.  Surfaces shall be smooth, even and true to place, and free of any foreign material which will adversely affect adhesion or appearance of applied coating.

- Moisture Levels:  Drywall, Plaster, Concrete, and Masonry surfaces shall be

tested with moisture-testing device before coating is applied.  No coating shall be applied when moisture content exceeds 12 %, except as may be required by the manufacturer of the coating materials used.

- Mildew shall be removed and neutralized.

- pH of surface to be coated shall be under 10.

- Provide recommended Zolatone Interior Finishes basecoats for all surfaces to receive special coating.

- Contractor shall sand and reprime all abrasions and damage spots in the

surface of the basecoat before proceeding with subsequent finish coat.

B.   Masonry:   Tool joints and clean surfaces as specified in Section 04200.

Rinse off cleaning solutions and allow surface to dry.  Cure mortar 28 days minimum before application of coating.

C.   Gypsum  Board:  Apply joint tape and compound to joints, fastener heads, dents, and surface

flaws as specified in Section 09250.  Prepare surface to a minimum Level 3                   drywall finish.  Sand smooth and flush with adjacent surfaces.

  - APPLICATION

A.   Follow manufacturer’s recommendations and instructions carefully regarding special coating

product so as to provide the best quality work.
B.   Equipment shall be kept clean and in proper working condition to provide best quality work

as intended by this specification.

- All materials shall be applied under adequate illumination , evenly spread and smoothly

applied, free of runs, sage, holidays, lap marks, air bubbles and pinholes to assure a smooth

finish.

D.   Suction or hot spots shall be reprimed prior to applying Polomyx wall finish.

E.   Basecoat:   Apply as many coats as necessary to produce a uniform substrate appearance.

Do not exceed manufacturer's recommended coverage rate.  Allow to dry prior to application

of subsequent coats.
F.   Multicolor Finish:  Apply special coating Material by using two-step pressure differential

spray technique, with variable control to assure uniform distribution and 100% full coat

(continuous) coverage.  Slight variations in pattern and texture are normal for multi-color

coatings.
G.   FastFix( by Zolatone.  Apply multicolor finish to FastFix sheets as well as the specified

substrate.  Insert finished sheets into Zolatone Maintenance Manual or job close out package.

H.     Should any coat of coating be deemed unsatisfactory, it shall be sanded and additional coats applied.

  - INSPECTION

A    Request acceptance of each coat before applying succeeding coats.

- Touch-up and repair all work that is not acceptable to the architect and request final

acceptance.

  - CLEANING

- Remove paint spatters from adjoining surfaces.

- Repair any damage to coatings or surfaces caused by cleaning operations.

- Remove debris from job site and leave storage area clean.

  - PAINTING SCHEDULE

- Interior - As Indicated On Schedules

1.	Concrete and Masonry (filled)

Basecoat: SP206 High Solids Block Filler

Second Coat: SP202 Drywall Basecoat or

SP92 High Performance Acrylic Sealer

Third Coat: Polomyx

PART  4   REPAIR / MAINTENANCE

  - MAINTENANCE

- When necessary, the surface can be washed down with a mild solution of detergent and

water.  (This is to be done when film of dust, dirt or smoke appears on surface).

B.    Stubborn stains can be removed with a mild abrasive cleanser.

  - NECESSARY EQUIPMENT:

A.   Finished sheets of FastFix( by Zolatone.

- An option to contractor specification is to provide five gallons of each color packed in single

cans for future repairs.

C.   Compressor - 3/4 horsepower or larger.

D.   For spot repair use a Zolatone Interior Finishes - approved Cup Gun, with an internal mix air cap.

  - SURFACE PREPARATION:

A.   Make sure area to be repaired is spackled, then sanded smooth and level.

B.    Spot prime with recommended Zolatone Interior Finishes basecoat.

  - REPAIR PROCEDURE:

- Apply self-adhering FastFix( by Zolatone path(es) for temporary repair of damaged surfaces.

- Set pressure on compressor to 50 psi.  Turn control knob on the spray gun clockwisefor sheer, then counter-clockwise for pattern step.  Carefully pattern off area and blend it into surrounding area.

END OF SECTION

Polomyx is a registered trademark of Surface Protection Industries, Inc.

Zolatone Interior Finishes markets and distributes Surface Protection Industries, Inc. products to the architectural marketplace.

CAUTION:   Class A Fire Rating does not define the hazards presented by this or any other material under actual fire conditions.

Copyright ( 2003 by Surface Protection Industries, Inc.  A limited license is extended to qualified design professionals to edit and reproduce this Guide Specification into a construction specification or purchase order, and to incorporate products manufactured by Surface Protection Industries, Inc.

Issued December 2003, Surface Protection Industries, Inc.reserves the right to revise product specifications and recommendations.  Contact manufacturer for current information.

NO WARRANTY:  We cannot reasonably anticipate or control the many different and varying conditions  under, or methods by which this information  and or  product may be used. Therefore, we do not guarantee the applicability of this information or the suitability of this product in any individual situation. All purchasers and users of this product are hereby put on notice that any advice provided is not a warranty and is not to be relied upon, and further that no one is authorized to make any representation or warranties relative to this product, including any and all sellers of this product.  This product is sold WITHOUT WARRANTY, expressed or implied, and any claim or any kind is limited to the purchase price of this product.