SECTION 12500

WINDOW TREATMENT

1. 	GENERAL:

1.1	REFERENCES:  Drawings and general provisions of Contract, including General Conditions and Division 1 specifications, apply to work in this section.

1.2	DESCRIPTION:  The extent of work shall be as shown on Drawings and called for in these Specifications.  The work under this section of Specifications includes furnishing and installing the following items:

A.	Shades for each window in residential units as described.

1.3	SUBMITTALS:  Contractor to submit product data on shades and blinds

2.  	PRODUCTS:

2.1	Window shades: Black-Out Shade

A.	12 oz. 4-ply opaque darkening shade available from Reo Window Shade Company, Portland, Maine (207) 773-7992.

1.	Construction – 4- Ply fiberglass (1 ply fiberglass, 3 ply vinyl)

521-E

REQUIREMENTS			FEDERAL SPECS					BUTLER

4-Ply Opaque

Finished weight – oz/sq										12.0

Breaking strength – lbs. in.		Warp 130					meets/ or exceed

Fill 120						meets/ or exceed

2.    Flame Resistance (U.S.  Government Specification CCC-C 521E and NFPA

701 Small Scale)

After Flame Seconds			Warp 2.0						meets/ or exceed

Fill 2.0						meets/ or exceed

Char Length Inches 			Warp 4.0						meets/ or exceed

Fill 4.0						meets/ or exceed

No evidence of holes,

breaking or cracking

Adhesion											Vinyl Films Inseparable

Meets Federal Spec. CCC-C521E

2.2	Spring wood rollers to be pine 1″ for up to 46″ wide 1 ¼″ for over 46″ wide.

3.	EXECUTION:

3.1	All work to be done by experienced craftsman in first-class manner and high-grade finish.  All installations shall be in accordance with layout shown on plans and in strict conformity with the manufacturer's recommendations.

3.2	Window Shade holding hardware shall be installed to provide level and secure system for attaching window shade and rods.  Work shall be free of dents, dings and other damage to finish (paint, etc.) and clean.

3.3	Solid backing is required for all window treatment hardware.  Hardware attached otherwise will not be acceptable.

3.4	The Contractor shall furnish all wood blocking within wall, filler pieces, angles, mouldings and other finish items necessary for complete installation of the equipment.

3.5	The Contractor shall check and make necessary adjustments to insure that all installed items operate faultlessly.

END OF SECTION