Copyright 1998, The American Institute of Architects (AIA)

SECTION 04810  - UNIT MASONRY ASSEMBLIES

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - SUMMARY

        - This Section includes unit masonry assemblies consisting of the following:

- Edit list below to suit Project.

          - Concrete masonry units.

          - Face brick.

          - Mortar and grout.

          - Reinforcing steel.

          - Masonry joint reinforcement.

          - Ties and anchors.

          - Embedded flashing.

          - Miscellaneous masonry accessories.

        - Related Sections include the following:

          - Division 1 Section “Temporary Facilities and Controls” for temporary enclosures and heating for masonry Work.

- List below only products, construction, and equipment that the reader might expect to find in this Section but are specified elsewhere.

          - Division 7 Section "Bituminous Dampproofing" for dampproofing applied to cavity face of backup wythes of cavity walls.

          - Division 7 Section "Firestopping" for Firestopping at tops of masonry walls and at openings in masonry walls.

        - Products installed, but not furnished, under this Section include the following:

- Subparagraphs below are examples only.  Revise to suit Project.

          - Steel lintels for brick masonry, furnished under Division 5 Section "Metal Fabrications."

- Retain paragraph below if allowances are specified for brick selection or for masonry testing.  Include separate brick allowances for special shapes if required.

      - SUBMITTALS

        - Product Data:  For each different masonry unit, accessory, and other manufactured product specified.

- Delete subparagraph below if flashing material selected is not specially fabricated for corners, end dams, etc.

        - Samples for Selection:  For the following:

- Delete paragraph and subparagraphs above if colors and textures are preselected and specified or scheduled.  Retain paragraph and subparagraphs below with or without above.

- Revise or expand subparagraphs below to suit Project.

          - Full-size units for each different exposed masonry unit required, showing the full range of exposed colors, textures, and dimensions to be expected in the completed construction.

- Delete subparagraph below if colored mortar is not used.

          - Colored mortar Samples for each color required, showing the full range of colors expected in the finished construction.

- Delete subparagraph below if stone trim is not used.

          - Weep holes/vents in color to match mortar color.

          - Accessories embedded in the masonry.

- Retain paragraph and subparagraph below for critical work where record of mockup materials is desired.

- See Editing Instruction No. 3 in the Evaluations for information on material test reports.

        - Material Test Reports:  From a qualified testing agency indicating and interpreting test results of the following for compliance with requirements indicated:

          - Each type of masonry unit required.

            - Include size-variation data for brick, verifying that actual range of sizes falls within specified tolerances.

- See Editing Instruction No. 3 in the Evaluations for information on material certificates.

        - Material Certificates:  Signed by manufacturers certifying that each of the following items complies with requirements:

          - Each type of masonry unit required.

            - Include size-variation data for brick, verifying that actual range of sizes falls within specified tolerances.

          - Each cement product required for mortar and grout, including name of manufacturer, brand, type, and weight slips at time of delivery.

          - Each material and grade indicated for reinforcing bars.

          - Each type and size of joint reinforcement.

          - Each type and size of anchor, tie, and metal accessory.

- Delete below if not required.

        - Cold-Weather Procedures:  Detailed description of methods, materials, and equipment to be used to comply with cold-weather requirements. Coordinate with General Contractor’s procedures for enclosures and heating.

      - QUALITY ASSURANCE

- Retain paragraph below to establish qualifications for testing agencies employed by Contractor or Owner.

        - Testing Agency Qualifications:  An independent testing agency, acceptable to authorities having jurisdiction, qualified according to ASTM C 1093 to conduct the testing indicated, as documented according to ASTM E 548.

        - Source Limitations for Masonry Units:  Obtain exposed masonry units of a uniform texture and color, or a uniform blend within the ranges accepted for these characteristics, through one source from a single manufacturer for each product required.

        - Source Limitations for Mortar Materials:  Obtain mortar ingredients of a uniform quality, including color for exposed masonry, from one manufacturer for each cementitious component and from one source or producer for each aggregate.

- Delete paragraph below if fire-rated masonry is not used.

- Retain paragraph above if mockup is only for establishing appearance factors.  Retain paragraph below if mockup also establishes material and workmanship qualities of concealed construction.

- Delete subparagraph above or below.  Below is applicable only if mockups are erected as part of building rather than separately.

- Delete below if work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

      - DELIVERY, STORAGE, AND HANDLING

        - Store masonry units on elevated platforms in a dry location.  If units are not stored in an enclosed location, cover tops and sides of stacks with waterproof sheeting, securely tied.  If units become wet, do not install until they are dry.

- Delete subparagraph below if Type I concrete masonry units are not required.

          - Protect Type I concrete masonry units from moisture absorption so that, at the time of installation, the moisture content is not more than the maximum allowed at the time of delivery.

        - Store cementitious materials on elevated platforms, under cover, and in a dry location.  Do not use cementitious materials that have become damp.

        - Store aggregates where grading and other required characteristics can be maintained and contamination avoided.

- Delete two paragraphs above and retain paragraph below if preblended, dry mortar mix is required.

        - Deliver preblended, dry mortar mix in moisture-resistant containers designed for lifting and emptying into dispensing silo.  Store preblended, dry mortar mix in delivery containers on elevated platforms, under cover, and in a dry location or in a metal dispensing silo with weatherproof cover.

        - Store masonry accessories, including metal items, to prevent corrosion and accumulation of dirt and oil.

      - PROJECT CONDITIONS

        - Protection of Masonry:  During construction, cover tops of walls, projections, and sills with waterproof sheeting at end of each day's work.  Cover partially completed masonry when construction is not in progress.

- Increase extent of cover in subparagraph below as needed to suit local climatic conditions.

          - Extend cover a minimum of 24 inches (600 mm) down both sides and hold cover securely in place.

          - Where one wythe of multiwythe masonry walls is completed in advance of other wythes, secure cover a minimum of 24 inches (600 mm) down face next to unconstructed wythe and hold cover in place.

        - Do not apply uniform floor or roof loads for at least 12 hours and concentrated loads for at least 3 days after building masonry walls or columns.

        - Stain Prevention:  Prevent grout, mortar, and soil from staining the face of masonry to be left exposed or painted.  Immediately remove grout, mortar, and soil that come in contact with such masonry.

          - Protect base of walls from rain-splashed mud and from mortar splatter by coverings spread on ground and over wall surface.

          - Protect sills, ledges, and projections from mortar droppings.

          - Protect surfaces of window and door frames, as well as similar products with painted and integral finishes, from mortar droppings.

          - Turn scaffold boards near the wall on edge at the end of each day to prevent rain from splashing mortar and dirt onto completed masonry.

        - Cold-Weather Requirements:  Do not use frozen materials or materials mixed or coated with ice or frost.  Do not build on frozen substrates or setting beds.  Remove and replace unit masonry damaged by frost or by freezing conditions.  Comply with the following requirements:

          - Cold-Weather Construction:  When the anticipated daytime low temperature is within the limits indicated, use the following procedures:

            - 40 to 32F (4 to 0C):  Heat mixing water or sand to produce mortar temperatures between 40 and 120F (4 and 49C).

            - 32 to 25 F (0 to -4C):  Heat mixing water and sand to produce mortar temperatures between 40 and 120F (4 and 49C). Heat grout materials to produce grout temperatures between 40 and 120 F (4 and 49C).  Maintain mortar and grout above freezing until used in masonry. Use heat on both sides of walls under construction. Coordinate with General Contractor for heating both sides of walls under construction.

            - 25 to 20F (-4 to -7C):  Heat mixing water and sand to produce mortar temperatures between 40 and 120F (4 and 49C).  Heat grout materials to produce grout temperatures between 40 and 120F (4 and 49C).  Maintain mortar and grout above freezing until used in masonry.  Heat masonry units to 40F (4C) if grouting. Coordinate with General Contractor to provide enclosures and heat both sides of walls under construction to maintain temperatures above 32F (0C) within the enclosures.

            - 20F (-7C) and Below:  Heat mixing water and sand to produce mortar temperatures between 40 and 120F (4 and 49C).  Heat grout materials to produce grout temperatures between 40 and 120 F (4 and 49C).  Maintain mortar and grout above freezing until used in masonry.  Heat masonry units to 40F (4C).  Coordinate with General Contractor to provide enclosures and heat both sides of walls under construction to maintain temperatures above 32F (0C) within the enclosures.

          - Cold-Weather Protection:  When the anticipated daytime low temperature is within the limits indicated, coordinate with the General Contractor to provide the following protection. This is in addition to construction procedures specified above:

            - 40 to 32F (4 to 0C):  Cover masonry insulating blankets for 48 hours after construction.

            - 32F (0C) and Below:  Provide enclosure and heat to maintain temperatures above 32F (0C) within the enclosure for 72 hours after construction.

          - Cold-Weather Cleaning:  Use liquid cleaning methods only when air temperature is 40F (4C) and above and will remain so until masonry has dried out, but not less than 7 days after completion of cleaning.

        - Hot-Weather Requirements:  Coordinate with the General Contractor to protect unit masonry work when temperature and humidity conditions produce excessive evaporation of water from mortar and grout.  Provide artificial shade and wind breaks and use cooled materials as required.

          - When ambient temperature exceeds 100F (38C), or 90F (32C) with a wind velocity greater than 8 mph (13 km/h), do not spread mortar beds more than 48 inches (1200 mm) ahead of masonry.  Set masonry units within one minute of spreading mortar.

- PRODUCTS

      - CONCRETE MASONRY UNITS

        - General:  Provide shapes indicated and as follows:

- Show details on Drawings of special conditions and special shapes needed.  Revise subparagraph below to suit Project.

          - Provide special shapes for lintels, corners, jambs, sash, control joints, headers, bonding, and other special conditions.

- Delete subparagraph above or below, or both.

        - Concrete Masonry Units:  ASTM C 90 and as follows:

- See Editing Instructions No. 2 and No. 4 in the Evaluations before retaining unit compressive strengths and weight classifications in subparagraphs below.  Delete subparagraph below if "Performance Requirements" Article was retained.  Minimum average net-area compressive strength per ASTM C 90 is 1900 psi (13.1 MPa).

          - Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of 1900 psi (13.1 MPa).

- Select one of three weights below or delete subparagraph for Contractor's option.  Retain ", unless otherwise indicated" for default requirement if more than one weight is used.

          - Weight Classification: Normal weight.

          - Provide Type I, moisture-controlled units.

- Select subparagraph above or below.  Verify local availability of Type I units before retaining.

          - Size (Width):  Manufactured to the following dimensions:

            - 6 inches (152 mm) nominal; 5-5/8 inches (142 mm) actual.

            - 8 inches (203 mm) nominal; 7-5/8 inches (194 mm) actual.

- Retain and edit list above for IP sizes with equivalent metric dimensions or list below for products manufactured to metric sizes.  If retaining below, verify availability of sizes.

          - Exposed Faces:  Manufacturer's standard color and texture, unless otherwise indicated.

- Delete subparagraph below if direct application of plaster is not used.

- Insert ASTM C 129 or UBC Standard 21-5 for non-load-bearing concrete masonry units, if desired; they are not usually an inventory item and may have to be ordered in large quantities.  Drawings will have to identify load-bearing and non-load-bearing units if both are specified.

      - BRICK

        - General:  Provide shapes indicated and as follows for each form of brick required:

- Show details on Drawings of special conditions and special shapes required.  Revise paragraph and subparagraphs below to suit Project.

        - Provide special shapes for applications requiring brick of size, form, color, and texture on exposed surfaces that cannot be produced by sawing.

          - Provide special shapes for applications where stretcher units cannot accommodate special conditions, including those at corners, movement joints, bond beams, sashes, and lintels.

          - Provide special shapes for applications where shapes produced by sawing would result in sawed surfaces being exposed to view.

          - Use of existing brick requires express permission of the engineer.

- See Editing Instruction No. 5 in the Evaluations before selecting grade from paragraph below.  Retain one of three types to match brick selected.  FBS is brick with normal variation in size; FBX is more uniform; FBA is nonuniform in size and texture and is used for special architectural effects.

        - Face Brick:  ASTM C 216, Grade  SW, Type  FBS (extruded), and as follows:

- See Editing Instruction No. 2 in the Evaluations before retaining unit compressive strength in subparagraph below.  Delete below if "Performance Requirements" Article was retained.  Below is based on net area, as in Table 1 of MSJC Specification, rather than gross area reported by ASTM C 67.  Minimum average gross-area compressive strength per ASTM C 216 is 3000 psi (20.7 MPa) for Grade SW and 2500 psi (17.2 MPa) for Grade MW.

          - Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of 8000 psi (55.2 MPa).

- Subparagraph below helps ensure good mortar bond without wetting brick.  Before retaining, verify that brick selected complies.

          - Initial Rate of Absorption:  Less than 20 g/30 sq. in. (20 g/194 sq. cm) per minute when tested per ASTM C 67.

          - Efflorescence:  Provide brick that has been tested according to ASTM C 67 and is rated "not effloresced."

- Delete subparagraph below if surface-colored brick is not used.

          - Surface Coloring:  Brick with surface coloring, other than flashed or sand-finished brick, shall withstand 50 cycles of freezing and thawing per ASTM C 67 with no observable difference in the applied finish when viewed from 10 feet (3 m).

          - Size:  Manufactured to the following actual dimensions:

- Five sizes below are examples only, based on BIA designations.  Verify sizes with local suppliers and modify to suit Project.

            - Closure Modular (Econo):  3-1/2 to 3-5/8 inches (89 to 92 mm) wide by 3-1/2 to 3-5/8 inches (89 to 92 mm) high by 7-1/2 to 7-5/8 inches (190 to 194 mm) long.

- Select from subparagraphs above for IP sizes with equivalent metric dimensions or from subparagraphs below for products manufactured to metric sizes.  If retaining below, verify availability of sizes.

          - Application:  Use where brick is exposed, unless otherwise indicated.

- Subparagraphs below are three examples of descriptive requirements for appearance where proprietary Specifications and allowances cannot be used.  Edit to suit Project, or delete if brick is specified by product name or if subparagraph above is retained.

- Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary Specification.  Refer to Division 1 Section "Materials and Equipment."

          - Products:  Subject to compliance with requirements, provide one of the following:

- See Editing Instruction No. 1 in the Evaluations for cautions about naming products and manufacturers.

            - Match existing brick in color and texture as closely as possible.

            - Provide solid modular blocks at window sills.

- See Editing Instruction No. 6 in the Evaluations before selecting grade from paragraph below.

- Note that hollow brick is not simply face brick with the usual cores (holes); it is brick that has voids (cores and cells) exceeding 25 percent of the gross cross-sectional area.  See Evaluations.

- If retaining paragraph below, select one grade, class, and type.  See Editing Instruction No. 7 in the Evaluations before selecting grade.  Retain one of four types to match brick selected.  HBS is brick with normal variation in size; HBX is more uniform; HBA is nonuniform in size and texture and is used for special architectural effects; HBB is for use where appearance and uniformity are not a consideration.

- Insert calcium silicate (sand-lime) brick if required.  See Evaluations.

      - MORTAR AND GROUT MATERIALS

- Coordinate requirements in this Article with those in "Mortar and Grout Mixes" Article.

- Retain one or more of first five paragraphs below.  Delete masonry cement if not allowed by "Mortar and Grout Mixes" Article below.  See Evaluations for discussion of masonry cement and mortar cement.

        - Portland Cement:  ASTM C 150, Type I or II, except Type III may be used for cold-weather construction.  Provide natural color or white cement as required to produce mortar color to match existing mortar as closely as possible.

        - Hydrated Lime:  ASTM C 207, Type S.

- Mix below allows better control of color than does job-mixed, portland cement-lime mortar with pigment added.

        - Portland Cement-Lime Mix:  Packaged blend of Portland cement complying with ASTM C 150, Type I or Type III, and hydrated lime complying with ASTM C 207.

          - Blue Circle Cement, Inc.: Eaglebond High Strength Type "S".

          - Ciment Quebec, Inc.: Portland and Lime / Type S.

        - Aggregate for Mortar:  ASTM C 144; except for joints less than 1/4 inch (6.5 mm) thick, use aggregate graded with 100 percent passing the No. 16 (1.18-mm) sieve.

- Retain subparagraph below for white mortar.

- Retain subparagraph below for colored-aggregate mortar.

        - Aggregate for Grout:  ASTM C 404.

- Retain paragraph below for colored cement or for pigments added at Project site.

- Retain paragraph below if firebox brick and clay flue linings are used.

- Paragraph below is an example requirement for a concrete admixture often used in cold weather as an antifreeze.  ASTM C 270 appendix and BIA recommend against using any admixtures.

- Retain paragraph below if integral water repellent is used in concrete masonry units.

        - Water:  Potable.

      - REINFORCING STEEL

- Retain required products below.

        - Uncoated Steel Reinforcing Bars:  ASTM A 615/A 615M; ASTM A 616/A 616M, including Supplement 1; or ASTM A 617/A 617M, Grade 60 (Grade 400).

- Select paragraph above or below or both; if retaining both, show locations of each on plans or revise below to indicate where epoxy-coated bars are required.  Revise below to specify galvanized bars complying with ASTM A 767/A 767M if required.  Revise either or both paragraphs if another grade of steel is required.

      - MASONRY JOINT REINFORCEMENT

        - Interior Block Wall Reinforcement: Ladder type, ASTM A641, mill galvanized, No. 9 wire.

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

            - Duro-wall; D/A 320 Ladur.

            - Hohmann & Barnard;  Ladder-Mesh, #220.

            - Wire-Bond;   Series 200, Single Wythe.

        - Exterior Block Wall Reinforcement:	Ladder type, ASTM A153 B2, hot dipped galvanized, with 3/16 inch side and cross rods.

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

            - Duro-wall; D/A 320 Ladur.

            - Hohmann & Barnard;  Ladder-Mesh, #220.

            - Wire-Bond;   Series 200, Single Wythe.

        - Multiple Wythe Joint Reinforcement:  Ladder type, ASTM A153 B2, hot dipped galvanized, with 3/16 inch side and cross rods.

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

            - Duro-wall; D/A 360 Ladur-eye.

            - Hohmann & Barnard;  Lox-All Adjustable Eye-Wire, #270.

            - Wire-Bond;   Series 800, Composite Hook and Eye.

        - Steel:  ASTM A615, 60 ksi (414 MPa) yield grade, deformed billet bars, uncoated finish.

        - Strap Anchors:  12 gage bent steel shape, uncoated finish.

      - MISCELLANEOUS ANCHORS

- Revise paragraph below if ASTM A 325 (ASTM A 325M) bolts are required.

        - Anchor Bolts:  Steel bolts complying with ASTM A 307, Grade A (ASTM F 568, Property Class 4.6); with ASTM A 563 (ASTM A 563M) hex nuts and, where indicated, flat washers; hot-dip galvanized to comply with ASTM A 153, Class C; of diameter and length indicated and in the following configurations:

          - Nonheaded bolts, bent in manner indicated, typical unless headed bolts are indicated.

          - Headed bolts, where indicated.

- Usually delete paragraph below and include in Sections covering items anchored.

        - Postinstalled Anchors:  Anchors as described below, with capability to sustain, without failure, load imposed within factors of safety indicated, as determined by testing per ASTM E 488, conducted by a qualified independent testing agency.

          - Type:  Expansion anchors.

          - Corrosion Protection:  Carbon-steel components zinc plated to comply with ASTM B 633, Class Fe/Zn 5 (5 microns) for Class SC 1 service condition (mild), use at interior walls.

- Subparagraphs above and below are examples only.  Above protects against corrosion from an indoor atmosphere; revise to suit other service conditions after verifying availability of thicker coatings.

- Subparagraphs below are examples only; verify safety factors to suit anchorage conditions and types of anchors indicated.  Overhead, vibratory, and other critical loads generally require higher safety factors.

          - For Postinstalled Anchors in Concrete:  Capability to sustain, without failure, a load equal to four times the loads imposed.

          - For Postinstalled Anchors in Masonry Units:  Capability to sustain, without failure, a load equal to six times the loads imposed.

- See Evaluations and BIA Technical Notes No. 28B for use of stainless-steel screws.

- Usually delete paragraph above and below and include in the concrete section if required.  Heckman's "Wedge Insert 425" is an example of inserts above.

- Insert other kinds of anchors as required.

      - EMBEDDED FLASHING MATERIALS

- See discussion of flashing materials in Evaluations before editing this Article.

- Delete paragraph and choices for flexible flashing below if only metal flashing is allowed.  If concealed metal flashing is required at certain locations, indicate those locations on Drawings or revise paragraph below.

        - Masonry Flashing (Fabric Flashing):  For base flashing in veneer masonry, and for head flashing at doors and windows, use the following, unless otherwise indicated:

- Subparagraph below is an example only; revise if other laminated products are required.

          - Copper-Laminated Flashing:  Manufacturer's standard laminated flashing consisting of 5-oz./sq. ft. (1.5-kg/sq. m) sheet copper bonded with asphalt between 2 layers of glass-fiber cloth.

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

            - Copper Fabric; AFCO Products, Inc.

            - H & B C-Fab Flashing; Hohmann & Barnard, Inc.

            - Copper Fabric Flashing; Polytite Manufacturing Corp.

            - Copper Fabric Flashing; Sandell Manufacturing Co., Inc.

            - York Copper Fabric Flashing; York Manufacturing, Inc.

- Retain above for nonproprietary or below for semiproprietary Specification.  Refer to Division 1 Section "Materials and Equipment."

      - MISCELLANEOUS MASONRY ACCESSORIES

- Revise two paragraphs below if a specific product is required.

        - Compressible Filler:  Premolded filler strips complying with ASTM D 1056, Grade 2A1; compressible up to 35 percent; of width and thickness indicated; formulated from neoprene urethane or PVC.

          - Holmann & Barnard: #NS – Closed Cell Neoprene.

          - Wire Bond:  3000 Horizontal.

        - Preformed Control-Joint Gaskets:  Material as indicated below, designed to fit standard sash block and to maintain lateral stability in masonry wall; size and configuration as indicated.

          - Styrene-Butadiene-Rubber Compound:  ASTM D 2000, Designation M2AA-805.

- Delete subparagraph above or below.

          - PVC:  ASTM D 2287, Type PVC-65406.

        - Bond-Breaker Strips:  Asphalt-saturated, organic roofing felt complying with ASTM D 226, Type I (No. 15 asphalt felt).

- Retain one or more of first six paragraphs below, or delete all if open-head joints are used for weep holes and vents.

        - Cavity Vents:  Medium-density polyethylene, 3/8-inch (9-mm) OD by 4 inches (100 mm) long.

- Mortar will corrode product below unless protected with paint.

        - Weep Hole/Vent:  One-piece, flexible extrusion made from UV-resistant polypropylene copolymer, designed to fill head joint with outside face held back 1/8 inch (3 mm) from exterior face of masonry, in color selected from manufacturer's standard.

          - Available Products:  Subject to compliance with requirements, cavity drainage materials that may be incorporated into the Work include, but are not limited to, the following:

            - Cell Vent; Dur-O-Wal, Inc.

            - #QV-Quadro-Vent; Hohmann & Barnard.

- Product below can be used at weep holes to keep them clear or used throughout cavity to keep it free draining.  If used throughout cavity, delete last phrase.

        - Cavity Drainage Material: 2-inch- (50-mm-) thick, free-draining mesh; made from polyethylene strands and shaped to avoid being clogged by mortar droppings.

          - Available Products:  Subject to compliance with requirements, cavity drainage materials that may be incorporated into the Work include, but are not limited to, the following:

            - Mortar Net by Mortar Net USA, LTD.;  Model MN10-2.

            - Mortar Maze by Advanced Building Products; Mortar Maze 2”.

        - Reinforcing Bar Positioners:  Wire units designed to fit into mortar bed joints spanning masonry unit cells with loops for holding reinforcing bars in center of cells.  Units are formed from 0.142-inch (3.6-mm) steel wire, hot-dip galvanized after fabrication. Provide units with either two loops or four loops as needed for number of bars indicated.

          - Available Products:  Subject to compliance with requirements, cavity drainage materials that may be incorporated into the Work include, but are not limited to, the following:

- Retain above for nonproprietary or below for semiproprietary Specification.  Refer to Division 1 Section "Materials and Equipment."

            - D/A 811; Dur-O-Wal, Inc.

            - D/A 816; Dur-O-Wal, Inc.

            - No. 376 Rebar Positioner; Heckman Building Products, Inc.

            - #RB Rebar Positioner; Hohmann & Barnard, Inc.

            - #RB-Twin Rebar Positioner; Hohmann & Barnard, Inc.

            - Double O-Ring Rebar Positioner; Masonry Reinforcing Corporation of America.

            - O-Ring Rebar Positioner; Masonry Reinforcing Corporation of America.

          - Damp Proofing: Follow Section 07115 Bituminous Damp Proofing.  .

- Insert other masonry accessories as required for Project.

      - CAVITY-WALL INSULATION

- Example below describes Dow's "Cavitymate Ultra."

        - Cavity-Wall Insulation:  Polyisocyanurate Board Insulation.  Aluminum-foil-faced, glass-fiber-reinforced, rigid, cellular, polyisocyanurate thermal insulation complying with ASTM C 1289, Type I, Class 2.

          - Available Products:  Subject to compliance with requirements, cavity insulation that may be incorporated into the Work include, but are not limited to, the following:

            - Celotex

- Revise below to suit insulation selected, if desired, or delete if adhesive is not used.  See Evaluations.

        - Adhesive:  Type recommended by insulation board manufacturer for application indicated.

      - MASONRY CLEANERS

- Tetrasodium polyphosphate is the cleaning agent in "Spic and Span," replacing the previous cleaning agent trisodium phosphate.  The new agent is less damaging to the environment.

- Verify acceptability of paragraph below for cleaning masonry with pigmented mortar joints and for kinds of masonry units specified.

        - Proprietary Acidic Cleaner:  Manufacturer's standard-strength cleaner designed for removing mortar/grout stains, efflorescence, and other new construction stains from new masonry without discoloring or damaging masonry surfaces.  Use product expressly approved for intended use by cleaner manufacturer and manufacturer of masonry units being cleaned.

          - Available Products:  Subject to compliance with requirements, products that may be used to clean unit masonry surfaces include, but are not limited to, the following:

            - 202V Vana-Stop; Diedrich Technologies, Inc.

            - Sure Klean Vana Trol; ProSoCo, Inc.

      - MORTAR AND GROUT MIXES

        - General:  Do not use admixtures, including pigments, air-entraining agents, accelerators, retarders, water-repellent agents, antifreeze compounds, or other admixtures, unless otherwise indicated.

          - Do not use calcium chloride in mortar or grout.

- Delete subparagraph below if cold-weather admixture is not retained.

- Retain paragraph below if preblended mix is required.

- Retain and edit one of two paragraphs below.  See Evaluations.

        - Mortar for Unit Masonry:  Comply with ASTM C 270, Property Specification.

- Retain subparagraph below to allow use of extended-life (ready-mixed) mortar if acceptable and available in Project location.  Usually select property specification above if retaining below.

- Select subparagraph above or below, or delete both if masonry cement is acceptable.  Retain below if masonry cement is acceptable for unreinforced interior masonry.

- For each masonry condition below applicable to Project, retain one mortar type or revise to suit Project.  See Editing Instruction No. 8 in the Evaluations before making selections.

- Delete subparagraph below if no masonry is grouted and reinforced with steel reinforcing bars.

          - For reinforced masonry and where indicated, use Type  S.

          - For exterior, above-grade, load-bearing and non-load-bearing walls and parapet walls; for interior load-bearing walls; for interior non-load-bearing partitions; and for other applications where another type is not indicated, use Type S.

- Delete subparagraph below if not allowed.

          - For interior non-load-bearing partitions, Type S.

- Delete paragraph and subparagraphs below if colored cement was required in "Mortar and Grout Materials" Article above.

- Delete subparagraph below if mortar pigments are limited to mineral oxides.

- Delete two subparagraphs below if masonry cement and mortar cement are not used.

        - Grout for Unit Masonry:  Comply with ASTM C 476.

          - Use grout of type indicated or, if not otherwise indicated, of type (fine or coarse) that will comply with Table 5 of ACI 530.1/ASCE 6/TMS 602 for dimensions of grout spaces and pour height.

          - Provide grout with a slump of 8 to 11 inches (200 to 280 mm) as measured according to ASTM C 143.

- EXECUTION

      - EXAMINATION

        - Examine conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance.

          - For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance.

- Delete subparagraph below if not required.

          - Verify that foundations are within tolerances specified.

- Delete subparagraph below if not applicable.

          - Verify that reinforcing dowels are properly placed.

          - Proceed with installation only after unsatisfactory conditions have been corrected.

        - Before installation, examine rough-in and built-in construction to verify actual locations of piping connections.

      - PREPARATION

        - Damp Proofing:

          - Provide access to personnel performing Bituminous Damp Proofing under Section 07115 Bituminous Damp Proofing.

          - Allow adequate time for the masonry back up to set prior to allowing application of damp proofing.

        - Coordinate with General Contractor for enclosures and heating requirements.

      - INSTALLATION, GENERAL

        - Thickness:  Build cavity and composite walls and other masonry construction to the full thickness shown.  Build single-wythe walls to the actual widths of masonry units, using units of widths indicated.

        - Build chases and recesses to accommodate items specified in this Section and in other Sections of the Specifications.

        - Where cutting and patching existing CMU, tooth in new work only where exposed to view.

        - Leave openings for equipment to be installed before completing masonry.  After installing equipment, complete masonry to match the construction immediately adjacent to the opening.

        - Cut masonry units with motor-driven saws to provide clean, sharp, unchipped edges.  Cut units as required to provide a continuous pattern and to fit adjoining construction.  Where possible, use full-size units without cutting.  Allow units cut with water-cooled saws to dry before placing, unless wetting of units is specified.  Install cut units with cut surfaces and, where possible, cut edges concealed.

        - Select and arrange units for exposed unit masonry to produce a uniform blend of colors and textures.

- Subparagraph below is "means and methods" but does help ensure uniformity of blend.

          - Mix units from several pallets or cubes as they are placed.

- Delete paragraph below if not applicable.

        - Matching Existing Masonry:  Match coursing, bonding, color, and texture of existing masonry.

- Retain below for high-suction brick.  A simple test to determine if wetting is required consists of drawing a circle the size of a quarter on a brick and placing 20 drops of water in the circle; if water is absorbed within 1-1/2 minutes, the brick requires wetting.

        - Wetting of Brick:  Wet brick before laying if the initial rate of absorption exceeds 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested per ASTM C 67.  Allow units to absorb water so they are damp but not wet at the time of laying.

      - CONSTRUCTION TOLERANCES

        - Comply with tolerances in ACI 530.1/ASCE 6/TMS 602 and the following:

        - For conspicuous vertical lines, such as external corners, door jambs, reveals, and expansion and control joints, do not vary from plumb by more than 1/4 inch in 20 feet (6 mm in 6 m), nor 1/2 inch (12 mm) maximum.

        - For vertical alignment of exposed head joints, do not vary from plumb by more than 1/4 inch in 10 feet (6 mm in 3 m), nor 1/2 inch (12 mm) maximum.

        - For conspicuous horizontal lines, such as exposed lintels, sills, parapets, and reveals, do not vary from level by more than 1/4 inch in 20 feet (6 mm in 6 m), nor 1/2 inch (12 mm) maximum.

- If Type FBS Rough or Type FBA brick is used, revise tolerances below to allow for variation in brick size.  Consider restricting tolerances if Type FBX brick is used.

        - For exposed bed joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm), with a maximum thickness limited to 1/2 inch (12 mm).  Do not vary from bed-joint thickness of adjacent courses by more than 1/8 inch (3 mm).

        - For exposed head joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm).  Do not vary from adjacent bed-joint and head-joint thicknesses by more than 1/8 inch (3 mm).

      - LAYING MASONRY WALLS

        - Lay out walls in advance for accurate spacing of surface bond patterns with uniform joint thicknesses and for accurate location of openings, movement-type joints, returns, and offsets.  Avoid using less-than-half-size units, particularly at corners, jambs, and, where possible, at other locations.

        - Bond Pattern for Exposed Masonry:  Lay exposed masonry in the following bond pattern; do not use units with less than nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

- Pattern is usually running bond.  If other bond patterns are required, they must be specified below or indicated on Drawings.

          - One-half running bond with vertical joint in each course centered on units in courses above and below.

        - Lay concealed masonry with all units in a wythe in running bond or bonded by lapping not less than 2 inches (50 mm).  Bond and interlock each course of each wythe at corners.  Do not use units with less than nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

        - Stopping and Resuming Work:  In each course, rack back one-half-unit length for one-half running bond or one-third-unit length for one-third running bond; do not tooth.  Clean exposed surfaces of set masonry, wet clay masonry units lightly if required, and remove loose masonry units and mortar before laying fresh masonry.

        - Built-in Work:  As construction progresses, build in items specified under this and other Sections of the Specifications.  Fill in solidly with masonry around built-in items.

- Revise paragraph below if flexible perimeter joint or thermal break is required.

        - Fill space between hollow-metal frames and masonry solidly with mortar, unless otherwise indicated.

- Delete paragraph above and below if not applicable.

        - Where built-in items are to be embedded in cores of hollow masonry units, place a layer of metal lath in the joint below and rod mortar or grout into core.

        - Fill cores in hollow concrete masonry units with grout 24 inches (600 mm) under bearing plates, beams, lintels, posts, and similar items, unless otherwise indicated.

        - Build non-load-bearing interior partitions full height of story to underside of solid floor or roof structure above, unless otherwise indicated.

- Select one or more of three subparagraphs below or revise to suit Project.  Coordinate with firestopping requirements.  Select first subparagraph if live-load deflection of structure above will produce stress in masonry.  See Editing Instruction No. 9 in the Evaluations.

          - Install compressible filler in joint between top of partition and underside of structure above.

          - Install partition top anchors, 4 foot on center, at tops of masonry partitions.

          - At fire-rated partitions, coordinate joint between top of partition and underside of structure above to comply with requirements of Division 7 Section "Firestopping."

        - Fill cores with sand where indicated on the drawings for sound control.

      - MORTAR BEDDING AND JOINTING

- Delete paragraph and subparagraphs below if no hollow concrete masonry units are required.  Mortar bedding of cross webs should be added if required.

        - Lay hollow masonry units as follows:

          - With full mortar coverage on horizontal and vertical face shells.

          - Bed webs in mortar in starting course on footings and in all courses of piers, columns, and pilasters, and where adjacent to cells or cavities to be filled with grout.

          - For starting course on footings where cells are not grouted, spread out full mortar bed, including areas under cells.

        - Lay solid brick-size masonry units with completely filled bed and head joints; butter ends with sufficient mortar to fill head joints and shove into place.  Do not deeply furrow bed joints or slush head joints.

- Delete subparagraph below if no cavity walls.

          - At cavity walls, bevel beds away from cavity, to minimize mortar protrusions into cavity.  As work progresses, trowel mortar fins protruding into cavity flat against the cavity face of the brick.

- Delete paragraph above and below if no fireplaces.

- Delete paragraph below if no stone trim.  Below is an example based on limestone specified in Part 2.

- If another joint profile is used, revise paragraph below or show on Drawings.

        - Tool exposed joints slightly concave when thumbprint hard, using a jointer larger than the joint thickness, unless otherwise indicated.

- Retain all text in paragraph below if full collar joints are required for all walls and partitions, or edit for limited requirements.  Retain below if all wythes are needed to meet height-to-thickness ratio of codes.

      - BONDING OF MULTIWYTHE MASONRY

- Retain paragraph below if main bonding between wythes is by individual metal ties.  Revise spacings as required by authorities having jurisdiction or by office practice.  Spacings are for wire ties 0.188 inch 4.8 mm in diameter, wire ties 0.148 inch 3.8 mm in diameter, and adjustable two-piece ties, respectively.

        - Use individual metal ties installed in horizontal joints to bond wythes together.  Provide ties as shown, but not less than one metal tie for 1.77 sq. ft. (0.16 sq. m) of wall area spaced not to exceed 16 inches (406 mm) o.c. horizontally and 16 inches (406 mm) o.c. vertically.  Stagger ties in alternate courses.  Provide additional ties within 12 inches (305 mm) of openings and space not more than 36 inches (915 mm) apart around perimeter of openings.  At intersecting and abutting walls, provide ties at no more than 24 inches (610 mm) o.c. vertically.

- Retain paragraph below if masonry joint reinforcement is main bond tie.  See Evaluations.

        - Corners:  Provide interlocking masonry unit bond in each wythe and course at corners, unless otherwise indicated.

- Delete subparagraph below if masonry joint reinforcement is not used.

          - Provide continuity with masonry joint reinforcement at corners by using prefabricated "L" units as well as masonry bonding.

        - Intersecting and Abutting Walls:  Unless vertical expansion or control joints are shown at juncture, bond walls together as follows:

- Select one of three subparagraphs below and edit to suit Project.  If more than one type of bonding is required, modify subparagraphs below and show locations on Drawings.

          - Provide individual metal ties not more than 16 inches (406 mm) o.c.

          - Provide continuity with masonry joint reinforcement by using prefabricated "T" units.

          - Provide rigid metal anchors not more than 48 inches (1220 mm) o.c.  If used with hollow masonry units, embed ends in mortar-filled cores.

      - CAVITIES

- Delete this Article if cavity walls are not used.

- Striking joints on cavity face may cause mortar to drop into cavity.  Delete second sentence in paragraph below if not required.

        - Keep cavities clean of mortar droppings and other materials during construction.  Strike joints facing cavities flush.

- Procedures in subparagraphs below help eliminate clogging of weep holes.  Wood strips usually rest on ties and have wires attached for lifting.

- Delete subparagraph above or below.

          - Install cavity drainage material above base flashing, lintel flashing, whether indicated or not on the drawings.

- Delete paragraph above or below, or both.

- Delete below if cavities are not insulated; revise if adhesive is not used.

        - Installing Cavity-Wall Insulation:  Place small dabs of adhesive, spaced approximately 12 inches (300 mm) o.c. both ways, on inside face of insulation boards, or attach with plastic fasteners designed for this purpose.  Fit courses of insulation between wall ties and other confining obstructions in cavity, with edges butted tightly both ways.  Press units firmly against inside wythe of masonry or other construction as shown.

          - Fill cracks and open gaps greater than 1/4 inch (6 mm) in insulation with foam insulation specified in Division 7 section “Building Insulation”.

      - MASONRY JOINT REINFORCEMENT

        - General:  Provide continuous masonry joint reinforcement as indicated.  Install entire length of longitudinal side rods in mortar with a minimum cover of 5/8 inch (16 mm) on exterior side of walls, 1/2 inch (13 mm) elsewhere.  Lap reinforcement a minimum of 6 inches (150 mm).

- Revise subparagraph below if different spacing is required.  Delete if shown on Drawings.

          - Space reinforcement not more than 16 inches (406 mm) o.c. unless noted otherwise.

- Delete subparagraphs below if not required.

          - Provide reinforcement not more than 8 inches (203 mm) above and below wall openings and extending 12 inches (305 mm) beyond openings.

- Delete subparagraph below if not required.

            - Reinforcement above is in addition to continuous reinforcement.

        - Cut or interrupt joint reinforcement at control and expansion joints, unless otherwise indicated.

        - Provide continuity at corners and wall intersections by using prefabricated "L" and "T" sections.  Cut and bend reinforcing units as directed by manufacturer for continuity at returns, offsets, column fireproofing, pipe enclosures, and other special conditions.

      - LINTELS

- Delete this Article if steel and masonry lintels are not required.  Delete types of lintels not required.  Coordinate with Division 5 Section "Metal Fabrications."

        - Install steel lintels where indicated.

        - Provide masonry lintels where shown and where openings of more than 12 inches (305 mm) for brick-size units and 24 inches (610 mm) for block-size units are shown without structural steel or other supporting lintels.

- Retain one of three subparagraphs below, depending on appearance desired.

          - Provide built-in-place masonry lintels.  Use specially formed bond beam units with reinforcing bars placed as indicated and filled with coarse grout.  Temporarily support built-in-place lintels until cured.

          - Extend horizontal reinforcement beyond the opening a minimum of 40 bar diameters, but not less than 24 inches.

          - Where steel lintels are utilized in concrete masonry openings, construct a bond beam above the steel with 2 #4 bars.  Extend 24 inches beyond the opening.

- Delete below if bearing is shown on Drawings.

        - Provide minimum bearing of 8 inches (200 mm) at each jamb, unless otherwise indicated.

      - FLASHING, WEEP HOLES, AND VENTS

        - General:  Install embedded flashing, cavity drainage materials, and weep holes in masonry at shelf angles, lintels, ledges, other obstructions to downward flow of water in wall, and where indicated.

        - Prepare masonry surfaces so they are smooth and free from projections that could puncture flashing.  Unless otherwise indicated, place through-wall flashing on sloping bed of mortar and cover with mortar.  Before covering with mortar, seal penetrations in flashing with adhesive, sealant, or tape as recommended by flashing manufacturer.

        - Install masonry flashing as follows:

          - At multiwythe masonry walls, including cavity walls, extend flashing from exterior face of outer wythe of masonry, through outer wythe, turned up a minimum of 8 inches (200 mm), and through inner wythe 1 inch (25 mm).  Fold flashing back over itself 1/2 inch (13 mm) to form hem.

- Delete subparagraph below if no masonry-veneer walls with sheathing behind them.

          - At masonry-veneer walls, extend flashing from exterior face of veneer, through veneer, up face of sheathing at least 8 inches (200 mm), and behind felt paper.

          - At lintels and shelf angles, extend flashing a minimum of 4 inches (100 mm) into masonry at each end.  At heads and sills, extend flashing 4 inches (100 mm) at ends and turn flashing up not less than 2 inches (50 mm) to form a pan.

- Delete subparagraph below if ribbed sheet metal flashing is not used.

          - Cut flashing off 3/8 inch (10 mm) beyond face of wall after masonry wall construction is completed and turn flashing down to form a drip.

        - Install weep holes in the head joints in exterior wythes of the first course of masonry immediately above embedded flashing and as follows:

          - Use plastic weep hole/vents to form weep holes.

          - Space weep holes 24 inches (600 mm) o.c.

- Delete subparagraph above and retain subparagraph below if plastic tubes or wicking is retained for weep holes in Part 2.

- Delete subparagraph above and below if cavity walls are not used.  Retain product in Part 2 if below is retained.  Delete both subparagraphs if cavity drainage material is shown throughout cavity on Drawings.

          - Place cavity drainage material immediately above flashing in cavities.

- Delete subparagraph below if loose-fill insulation is not used or if weep holes do not require screening.

- Delete paragraph below if wicking is not used.

- Retain vents if wall is designed on rain-screen principle with vents acting to equalize air-pressure differential between cavity and exterior.  Indicate spacing of vents and blocking on Drawings.  See Evaluations.

        - Install vents in vertical head joints at the top of each continuous cavity.  Use round plastic tubing to form vents.

          - Space weep holes 32 inches (900 mm) o.c.

- Delete below if built-in reglets and nailers are not used.

      - REINFORCED UNIT MASONRY INSTALLATION

- Usually retain paragraph and subparagraphs below only if reinforced masonry beams, slabs, soffits, and similarly formed elements are required.

        - Temporary Formwork and Shores:  Construct formwork and shores to support reinforced masonry elements during construction.

          - Construct formwork to conform to shape, line, and dimensions shown.  Make it sufficiently tight to prevent leakage of mortar and grout.  Brace, tie, and support forms to maintain position and shape during construction and curing of reinforced masonry.

          - Do not remove forms and shores until reinforced masonry members have hardened sufficiently to carry their own weight and other temporary loads that may be placed on them during construction.

        - Placing Reinforcement:  Comply with requirements of ACI 530.1/ASCE 6/TMS 602.

          - Layout vertical reinforcement with specified jamb reinforcement 4" from each corner, control joint, and opening jamb.  Space bars between at a uniform spacing that does not exceed the spacing specified, rounded to the nearest 8".  Maximum spacing shall not exceed 48" in any location.

          - Minimum splice length for deformed bar reinforcement shall be 48 bar diameters.  Secure lap splices by tying with wire.

          - Secure reinforcement in place before placing grout,  For vertical reinforcement, use one of the following methods:

            - Secure bar at the bottom of each grout lift by tying to dowels.  Build masonry around reinforcement.  Install rebar positioners at the top of each bar and at a maximum spacing of 192 bar diameters.

            - Install rebar positioner at the bottom course of the grout lift, located within 4 inches of the dowel to be spliced.  Lay up masonry units.  Set vertical bar in the rebar positioner.  Install additional rebar positioners at the top of the bar, and at a maximum spacing of 192 bar diameters.

        - Grouting:  Do not place grout until entire height of masonry to be grouted has attained sufficient strength to resist grout pressure.

          - Comply with requirements of ACI 530.1/ASCE 6/TMS 602 for cleanouts and for grout placement, including minimum grout space and maximum pour height.

          - Definitions:

            - Grout Lift - Grout placed in one continuous operation.  The maximum time span for the grout placement in one lift is 1-1/2 hours measured from the time water is added to the grout mix.  The minimum time span between successive grout lifts is one hour.

            - Grout Pour - The height of masonry to be grouted prior to the erection of additional masonry.

          - Provide cleanout holes at least 3 inches (76 mm) in least dimension for grout pours over 60 inches (1524 mm) in height.

            - Provide cleanout holes at each vertical reinforcing bar.

          - Where grouting of cells does not extend the full height of the wall, install specified grout stop at the bottom of lift.

          - Consolidate grout with a mechanical vibrator.

            - Use a low velocity vibrator with a 3/4 inch head.

            - Vibrate each cell in concrete masonry units twice.  Insert vibrator to bottom of lift and activate for 1 to 2 seconds.

            - Perform initial consolidation at each cell immediately after grout placement.

            - Perform reconsolidation in each cell by reinserting vibrator when grout is still plastic.

      - REPAIRING, POINTING, AND CLEANING

        - Remove and replace masonry units that are loose, chipped, broken, stained, or otherwise damaged or that do not match adjoining units.  Install new units to match adjoining units; install in fresh mortar, pointed to eliminate evidence of replacement.

        - Pointing:  During the tooling of joints, enlarge voids and holes, except weep holes, and completely fill with mortar.  Point up joints, including corners, openings, and adjacent construction, to provide a neat, uniform appearance.  Prepare joints for sealant application.

        - In-Progress Cleaning:  Clean unit masonry as work progresses by dry brushing to remove mortar fins and smears before tooling joints.

        - Final Cleaning:  After mortar is thoroughly set and cured, clean exposed masonry as follows:

          - Remove large mortar particles by hand with wooden paddles and nonmetallic scrape hoes or chisels.

          - Test cleaning methods on sample wall panel; leave one-half of panel uncleaned for comparison purposes.  Obtain Engineer's approval of sample cleaning before proceeding with cleaning of masonry.

          - Protect adjacent stone and nonmasonry surfaces from contact with cleaner by covering them with liquid strippable masking agent, polyethylene film, or waterproof masking tape.

- Delete subparagraph above and below if no cleaners are specified in Part 2 or if no cleaners are allowed.

          - Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing the surfaces thoroughly with clear water.

- Select subparagraph above or below.  Coordinate with products retained in Part 2.  If high-pressure water cleaning or other methods are acceptable, delete or revise below and insert applicable requirements.

          - Clean concrete masonry by cleaning method indicated in NCMA TEK 8-2 applicable to type of stain on exposed surfaces.

          - Clean brick masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

          - Clean brick masonry by the bucket-and-brush hand-cleaning method described in BIA Technical Notes No. 20 Revised and the cleaning compound manufacturer’s written instructions.

- Delete below if no limestone trim.

      - MASONRY WASTE DISPOSAL

- Retain this Article if clean masonry waste can be used as fill.  This diverts some material from the waste stream, conserving landfill space.

        - Recycling:  Unless otherwise indicated, excess masonry materials are Contractor's property.  At completion of unit masonry work, remove from Project site.

        - Excess Masonry Waste:  Remove excess, clean masonry waste that cannot be used as fill, as described above, and other masonry waste, and legally dispose of off Owner's property.

END OF SECTION 04810