Copyright 1996, The American Institute of Architects (AIA)

SECTION 04901 - CLAY MASONRY RESTORATION AND CLEANING

This Section uses the term Architect.  Change this term as necessary to match the actual term used to identify the design professional as defined in the General and Supplementary Conditions.

- GENERAL

      - SUMMARY

        - This Section includes the following:

- Edit below to suit Project.

          - Repointing mortar joints.

            - Carry in the base bid 150 SF of area to be repointed as and allowance in areas required at the discretion of the engineer.

            - Include on the bid form a square foot unit cost for repointing of brick mortar joints.  The cost shall be the same if added or deducted from the allowance.

        - Related Sections include the following:

          - Division 1 Section “Allowances” for information on allowances pertaining to this section.

          - Division 1 Section “Unit Prices” for information on unit pricing pertaining to this section.

- List below only products, construction, and equipment for this Project that the reader might expect to find in this Section but are specified elsewhere.  Verify that Section titles listed below are correct for this Project's Specifications because Section titles may have changed since this Section was updated.

          - Division 4 Section "Unit Masonry Assemblies" for new clay masonry construction.

          - Division 7 Section "Joint Sealants" for sealing joints in restored clay masonry.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver other materials to Project site in manufacturer's original and unopened containers, labeled with type and name of products and manufacturers.

        - Store cementitious materials off the ground, under cover, and in a dry location.

        - Store aggregates, covered and in a dry location, where grading and other required characteristics can be maintained and contamination avoided.

        - Comply with manufacturer's written instructions for minimum and maximum temperature requirements for storage.

      - PROJECT CONDITIONS

- Retain this Article for extensive exterior masonry restorations or revise to suit Project.

        - Do not repoint mortar joints or repair masonry unless air temperature is between and 40 and 80 deg F (4 and 27 deg C) and will remain so for at least 48 hours after completion of Work.

- Delete paragraph above and retain paragraph below if cold-weather construction is allowed for pointing and repair work.

        - Cold-Weather Requirements:  Comply with the following procedures for masonry repair and mortar-joint pointing:

          - When air temperature is below 40 deg F (4 deg C), heat mortar ingredients, masonry repair materials, and existing masonry walls to produce temperatures between 40 and 120 deg F (4 and 49 deg C).

          - When mean daily air temperature is between 25 and 40 deg F (minus 4 and 4 deg C), cover completed Work with weather-resistant, insulating blankets for 48 hours after repair and pointing.

          - When mean daily air temperature is below 25 deg F (minus 4 deg C), provide enclosure and heat to maintain temperatures above 32 deg F (0 deg C) within the enclosure for 48 hours after repair and pointing.

        - Hot-Weather Requirements:  Protect restoration work when temperature and humidity conditions produce excessive evaporation of water from mortar and patching materials.  Provide artificial shade and wind breaks and use cooled materials as required.  Do not apply mortar to substrates with temperatures of 90 deg F (32 deg C) and above.

- Extend period below, if necessary, to ensure masonry does not freeze before it dries out.

        - Prevent grout or mortar used in repointing and repair work from staining face of surrounding masonry and other surfaces.  Immediately remove grout and mortar in contact with exposed masonry and other surfaces.

        - Protect sills, ledges, and projections from mortar droppings.

- If windows are to be replaced, add to sequence here to ensure new windows will not be damaged by cleaning process.

- PRODUCTS

      - MORTAR MATERIALS

- Add specific requirements to suit Project.

        - Portland Cement:  ASTM C 150, Type I or Type II.

- Delete subparagraph below if not applicable or required.

          - Provide white cement containing not more than 0.60 percent total alkali when tested according to ASTM C 114.

        - Hydrated Lime:  ASTM C 207, Type S.

- Usually delete paragraph below and retain paragraph above.

        - Aggregate for Mortar:  ASTM C 144, unless otherwise indicated.

- Revise subparagraph below to produce mortar quality and appearance required for Project.  See Evaluations.

          - Match size, texture, and gradation of existing mortar as closely as possible.

- If known, indicate source of sand and size and gradation.

- Delete paragraph below if pigmented mortar is not used.

        - Mortar Pigments:  Natural and synthetic iron oxides and chromium oxides, compounded for mortar mixes.  Use only pigments with a record of satisfactory performance in masonry mortars.

        - Water:  Potable.

      - CLEANING MATERIALS

- If local water is known to be unsuitable, consider informing Contractor in paragraph below.  Hard or softened water may be unsuitable even though potable.

        - Water for Cleaning:  Potable.

- Delete paragraph below if heated water is not required.

- Insert other types of products or masking agents, including tapes, sheets, etc., as required.

        - Proprietary Acidic Cleaner:  Manufacturer's standard-strength cleaner designed for removing mortar/grout stains, efflorescence, and other new construction stains from new masonry without discoloring or damaging masonry surfaces.  Use product expressly approved for intended use by cleaner manufacturer and manufacturer of masonry units being cleaned.

          - Available Products:  Subject to compliance with requirements, products that may be used to clean unit masonry surfaces include, but are not limited to, the following:

            - 202V Vana-Stop; Diedrich Technologies, Inc.

            - Sure Klean Vana Trol; ProSoCo, Inc.

      - MORTAR MIXES

- Delete paragraph below if hydrated lime is used.

        - Measurement and Mixing:  Measure cementitious and aggregate material in a dry condition by volume or equivalent weight.  Do not measure by shovel; use known measure.  Mix materials in a clean, mechanical batch mixer.

- Delete subparagraph below if pointing mortar is not used or if prehydration is not required.

          - Mixing Pointing Mortar:  Thoroughly mix cementitious and aggregate materials together before adding any water.  Then mix again adding only enough water to produce a damp, unworkable mix that will retain its form when pressed into a ball.  Maintain mortar in this dampened condition for 1 to 2 hours.  Add remaining water in small portions until reaching mortar of the desired consistency.  Use mortar within 30 minutes of final mixing; do not retemper or use partially hardened material.

        - Colored Mortar:  Produce mortar of color required by using selected ingredients.  Do not adjust proportions without Engineer's approval.

- Delete subparagraph below if none.

          - Mortar Pigments:  Where mortar pigments are indicated, do not exceed a pigment-to-cement ratio of 1:10 by weight.

        - Do not use admixtures of any kind in mortar, unless otherwise indicated.

        - Mortar Proportions:  Mix mortar materials in the following proportions:

- Mix proportions below are examples only and must be revised to suit Project.  See Evaluations.

          - Pointing Mortar for Brick:  1 part portland cement, 1 part lime, and 6 parts natural-mortar aggregate.

- EXECUTION

      - REPOINTING MASONRY

- Delete this Article if no repointing is required.

        - Rake out joints as follows:

- Unless all joints on Project are repointed, indicate location of repointing work here by insert or on Drawings.  Investigate depth required to rake out joints for Project and revise below accordingly.

          - Rake out mortar from joints to depths equal to 2-1/2 times their widths, but not less than 1/2 inch (13 mm) or not less than that required to expose sound, unweathered mortar.

          - Remove mortar from masonry surfaces within raked-out joints to provide reveals with square backs and to expose masonry for contact with pointing mortar.  Brush, vacuum, or flush joints to remove dirt and loose debris.

          - Do not spall edges of masonry units or widen joints.  Replace damaged masonry units.

- Revise subparagraph below if power tools are not allowed.

            - For bed joints, power-operated grinders will be allowed with Engineer's approval based on mockup by Contractor of a satisfactory ability of operators to use tools without damaging masonry.

            - For head joints, cut out old mortar by hand with a chisel and mallet.

        - Point joints as follows:

          - Rinse masonry-joint surfaces with water to remove dust and mortar particles.  Time rinsing application so, at the time of pointing, excess water has evaporated or run off and joint surfaces are damp but free of standing water.

          - Apply the first layer of pointing mortar to areas where existing mortar was removed to depths greater than surrounding areas.  Apply in layers not greater than 3/8 inch (9 mm) until a uniform depth is formed.  Compact each layer thoroughly and allow it to become thumbprint hard before applying the next layer.

          - After joints have been filled to a uniform depth, place remaining pointing mortar. Take care not to spread mortar over edges onto exposed masonry surfaces or to featheredge mortar.

          - When mortar is thumbprint hard, tool joints to match original appearance of joints, unless otherwise indicated.  Remove excess mortar from edge of joint by brushing.

          - Cure mortar by maintaining in a damp condition for at least 72 hours.

          - Where repointing work precedes cleaning of existing masonry, allow mortar to harden at least 30 days before beginning cleaning work.

      - FINAL CLEANING

- Delete this Article only if overall cleaning of existing masonry occurs after pointing work is completed.

- Revise below if chemical cleaning of rebuilt masonry work is allowed or if overall cleaning of rebuilt and existing masonry can be accomplished using new masonry chemical cleaning techniques.  See Division 4 Section "Unit Masonry."

        - After mortar is thoroughly set and cured, clean exposed masonry as follows:

          - Remove large mortar particles by hand with wooden paddles and nonmetallic scrape hoes or chisels.

          - Protect adjacent stone and nonmasonry surfaces from contact with cleaner by covering them with liquid strippable masking agent, polyethylene film, or waterproof masking tape.

- Delete subparagraph above and below if no cleaners are specified in Part 2 or if no cleaners are allowed.

          - Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing the surfaces thoroughly with clear water.

- Select subparagraph above or below.  Coordinate with products retained in Part 2.  If high-pressure water cleaning or other methods are acceptable, delete or revise below and insert applicable requirements.

          - Clean brick masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

          - Clean brick masonry by the bucket-and-brush hand-cleaning method described in BIA Technical Notes No. 20 Revised and the cleaning compound manufacturer’s written instructions.

END OF SECTION 04901