Copyright 1997, The American Institute of Architects (AIA)

SECTION 05500 - METAL FABRICATIONS

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - SUMMARY

        - This Section includes the following:

          - Loose bearing and leveling plates.

          - Loose steel lintels.

          - Steel framing and supports for applications where framing and supports are not specified in other Sections.

        - Related Sections include the following:

List below only products, construction, and equipment that the reader might expect to find in this Section but are specified elsewhere.

          - Division 5 Section "Structural Steel" for structural-steel framing system components.

          - Division 6 Section "Rough Carpentry" for metal framing anchors and other rough hardware.

          - Division 13 Section “Hazardous Material Remediation” for abatement of lead coatings.

Delete subparagraph above and below if pit ladders are in this Section.

      - SUBMITTALS

        - Product Data:  For the following:

Delete items below for which Product Data is not required.

          - Paint products.

        - Shop Drawings:  Detail fabrication and erection of each metal fabrication indicated.  Include plans, elevations, sections, and details of metal fabrications and their connections.  Show anchorage and accessory items.

          - Provide templates for anchors and bolts specified for installation under other Sections.

Usually delete paragraph below unless increased corrosion resistance of Type 316 stainless steel is required.

Retain paragraph below if procedures for welder certification are retained in "Quality Assurance" Article.

        - Welding Certificates:  Copies of certificates for welding procedures and personnel.

        - Qualification Data:  For firms and persons specified in "Quality Assurance" Article to demonstrate their capabilities and experience.  Include lists of completed projects with project names and addresses, names and addresses of architects and owners, and other information specified.

      - QUALITY ASSURANCE

        - Fabricator Qualifications:  A firm experienced in producing metal fabrications similar to those indicated for this Project and with a record of successful in-service performance, as well as sufficient production capacity to produce required units.

Delete paragraph below if no welding.  Retain "Welding Certificates" Paragraph in "Submittals" Article if below is retained.  AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

        - Welding:  Qualify procedures and personnel according to the following:

Retain applicable standards below.

          - AWS D1.1, "Structural Welding Code--Steel."

          - AWS D1.3, "Structural Welding Code--Sheet Steel."

          - Certify that each welder has satisfactorily passed AWS qualification tests for welding processes involved and, if pertinent, has undergone recertification.

      - PROJECT CONDITIONS

        - Field Measurements:  Where metal fabrications are indicated to fit walls and other construction, verify dimensions by field measurements before fabrication and indicate measurements on Shop Drawings.  Coordinate fabrication schedule with construction progress to avoid delaying the Work.

Delete below if not allowed.

          - Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating metal fabrications without field measurements.  Coordinate construction to ensure that actual dimensions correspond to established dimensions.  Allow for trimming and fitting.

      - COORDINATION

        - Coordinate installation of anchorages for metal fabrications.  Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors, that are to be embedded in concrete or masonry.  Deliver such items to Project site in time for installation.

        - Lead Coatings have been found in this facility and are identified in part 3 of section 13280 Hazardous Material Remediation.  It shall be the contractor’s responsibility to coordinate with section 13280 to identify the locations of required abatement.

          - The lead abatement shall be limited to areas that need to be cut apart and or will require welding of new connections, bolted connections shall be unbolted.

        - The contractor shall be responsible for all requirements under 29 CFR part 1926.62.  Although the lead coatings will be removed under section 13280, employee exposure assessment monitoring required for work under this section is the responsibility of this section.

- PRODUCTS

      - METALS, GENERAL

        - Metal Surfaces, General:  For metal fabrications exposed to view in the completed Work, provide materials with smooth, flat surfaces without blemishes.  Do not use materials with exposed pitting, seam marks, roller marks, rolled trade names, or roughness.

      - FERROUS METALS

Retain material types, qualities, and grades below that are indicated in Specifications or on Drawings for each fabrication type.  Add or delete to suit Project.

        - Steel Plates, Shapes, and Bars:  ASTM A 36/A 36M.

Revise paragraph below to hot-formed tubing (ASTM A 501), if required, only after verifying its availability.

        - Steel Tubing:  Cold-formed steel tubing complying with ASTM A 500.

Round steel tubing and pipe are sized differently.  Tubing is designated by OD and wall thickness.  Pipe is designated by nominal pipe size and weight or schedule number.  See Evaluations.

        - Steel Pipe:  ASTM A 53, standard weight (Schedule 40), unless another weight is indicated or required by structural loads.

Paragraph below describes typical component of metal channel framing systems such as that manufactured by Unistrut Corporation.

        - Malleable-Iron Castings:  ASTM A 47, Grade 32510 (ASTM A 47M, Grade 22010).

Usually select paragraph above or below if castings are required; see Evaluations.  Revise if another grade or class is required for structural reasons.

        - Gray-Iron Castings:  ASTM A 48, Class 30 (ASTM A 48M, Class 200), unless another class is indicated or required by structural loads.

Delete paragraph and subparagraph below if not applicable.  If retaining, verify safety factor with Project's structural engineer.

        - Cast-in-Place Anchors in Concrete:  Anchors of type indicated below, fabricated from corrosion-resistant materials capable of sustaining, without failure, the load imposed within a safety factor of 4, as determined by testing per ASTM E 488, conducted by a qualified independent testing agency.

          - Threaded or wedge type; galvanized ferrous castings, either ASTM A 47 (ASTM A 47M) malleable iron or ASTM A 27/A 27M cast steel.  Provide bolts, washers, and shims as needed, hot-dip galvanized per ASTM A 153/A 153M.

        - Welding Rods and Bare Electrodes:  Select according to AWS specifications for metal alloy welded.

      - PAINT

Select paragraph above or below.  Revise above if Division 9 Section "Special Coatings" is used.

        - Shop Primer for Ferrous Metal:  Fast-curing, lead- and chromate-free, universal modified-alkyd primer complying with performance requirements in FS TT-P-664; selected for good resistance to normal atmospheric corrosion, compatibility with finish paint systems indicated, and capability to provide a sound foundation for field-applied topcoats despite prolonged exposure.

Select paragraph above or below.  Above is a typical primer; provides minimum protection to steel.  Below provides better protection; is suitable for more severe environments.

Delete paragraph below if no galvanized fabrications.

        - Galvanizing Repair Paint:  High-zinc-dust-content paint for regalvanizing welds in steel, complying with SSPC-Paint 20.

        - Bituminous Paint:  Cold-applied asphalt mastic complying with SSPC-Paint 12, except containing no asbestos fibers, or cold-applied asphalt emulsion complying with ASTM D 1187.

      - FASTENERS

        - General:  Provide Type 304 or 316 stainless-steel fasteners for exterior use and zinc-plated fasteners with coating complying with ASTM B 633, Class Fe/Zn 5, where built into exterior walls.  Select fasteners for type, grade, and class required.

Delete paragraphs below if no detailed fastening requirements.  Revise first paragraph if ASTM A 325 bolts are required for connecting miscellaneous steel framing and supports.

        - High-Strength Bolts, Nuts, and Washers:  ASTM A 325 (ASTM A 325M), Type 1, heavy hex steel structural bolts; ASTM A 563 (ASTM A 563M) heavy hex carbon-steel nuts; and ASTM F 436 (ASTM F 436M) hardened carbon-steel washers.

Select one finish from options in subparagraph below.

          - Finish:  Plain.

Retain subparagraph below if applicable.

          - Direct-Tension Indicators:  ASTM F 959, Type 325 (ASTM F 959M, Type 8.8,) compressible-washer type.

Select one finish from options in subparagraph below.

            - Finish:  Plain.

If corrosion-resisting (weathering) steel is used, change Type 1 bolts to Type 3 in paragraph below. Retain option if applicable.  Indicate locations if using bolts below for some connections and ASTM A 325 (ASTM A 325M) bolts in paragraph above for others.

        - High-Strength Bolts, Nuts, and Washers:  ASTM A 490 (ASTM A 490M), Type 1, heavy hex steel structural bolts; ASTM A 563 (ASTM A 563M) heavy hex carbon-steel nuts; and ASTM F 436 (ASTM F 436M) hardened carbon-steel washers, plain.

Retain subparagraph below if applicable.

          - Direct-Tension Indicators:  ASTM F 959, Type 490 (ASTM F 959M,) Type 10.9, compressible-washer type, plain.

        - Machine Screws:  ASME B18.6.3 (ASME B18.6.7M).

        - Lag Bolts:  ASME B18.2.1 (ASME B18.2.3.8M).

        - Wood Screws:  Flat head, carbon steel, ASME B18.6.1.

        - Plain Washers:  Round, carbon steel, ASME B18.22.1 (ASME B18.22M).

        - Lock Washers:  Helical, spring type, carbon steel, ASME B18.21.1 (ASME B18.21.2M).

        - Adhesive Anchors:  Threaded anchors with a chemical capsule containing prepared amounts of liquid polyester resin, quartz aggregate, and a catalyst.  Size and embedment depth shall be as noted on the drawings, or if not noted, as required to withstand required loading.  Acceptable products include, but are not limited to:

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

            - Hilti HVA Adhesive Anchors

            - Red Head Redi-Chem Anchors

            - Rawl Needle-Capsule Anchors System

            - Fastenal Chemical Capsule Anchors

        - Sleeve Anchors:  Hilti with Hex Nut (HX).  Provide tamperproof nut as indicated.

        - Renovation Anchors:  Hilti, HIT C-20 system, female type.

      - CONCRETE FILL

Delete this Article if not required for concrete-filled bollards or wheel guards.

        - Concrete Materials and Properties:  Comply with requirements in Division 3 Section "Cast-in-Place Concrete" for normal-weight, air-entrained, ready-mix concrete with a minimum 28-day compressive strength of 3000 psi (20 MPa), unless otherwise indicated.

      - FABRICATION, GENERAL

        - Shop Assembly:  Preassemble items in shop to greatest extent possible to minimize field splicing and assembly.  Disassemble units only as necessary for shipping and handling limitations.  Use connections that maintain structural value of joined pieces.  Clearly mark units for reassembly and coordinated installation.

        - Shear and punch metals cleanly and accurately.  Remove burrs.

        - Ease exposed edges to a radius of approximately 1/32 inch (1 mm), unless otherwise indicated.  Form bent-metal corners to smallest radius possible without causing grain separation or otherwise impairing work.

        - Weld corners and seams continuously to comply with the following:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

          - At exposed connections, finish exposed welds and surfaces smooth and blended so no roughness shows after finishing and contour of welded surface matches that of adjacent surface.

        - Provide for anchorage of type indicated; coordinate with supporting structure.  Fabricate and space anchoring devices to secure metal fabrications rigidly in place and to support indicated loads.

        - Cut, reinforce, drill, and tap metal fabrications as indicated to receive finish hardware, screws, and similar items.

        - Fabricate joints that will be exposed to weather in a manner to exclude water, or provide weep holes where water may accumulate.

Paragraph below is for exterior metalwork.  Revise to suit Project conditions and metalwork exposure.

        - Allow for thermal movement resulting from the following maximum change (range) in ambient and surface temperatures by preventing buckling, opening up of joints, overstressing of components, failure of connections, and other detrimental effects.  Base engineering calculation on surface temperatures of materials due to both solar heat gain and nighttime-sky heat loss.

Differential values below (for aluminum in particular) are suitable for most of the U.S.  Revise to suit local conditions.

          - Temperature Change (Range):  120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

        - Form exposed work true to line and level with accurate angles and surfaces and straight sharp edges.

        - Remove sharp or rough areas on exposed traffic surfaces.

        - Form exposed connections with hairline joints, flush and smooth, using concealed fasteners where possible.  Use exposed fasteners of type indicated or, if not indicated, Phillips flat-head (countersunk) screws or bolts.  Locate joints where least conspicuous.

Delete subparagraph above if no exterior ladders.  Retain below, with or without above, if only selected interior ladders are galvanized and locations are indicated on Drawings.  Revise if all interior ladders are galvanized.

Delete paragraph below if no ship's ladders are galvanized.

      - LOOSE BEARING AND LEVELING PLATES

        - Provide loose bearing and leveling plates for steel items bearing on masonry or concrete construction.  Drill plates to receive anchor bolts and for grouting.

Delete below if plates are not galvanized.

      - LOOSE STEEL LINTELS

        - Fabricate loose structural-steel lintels from steel angles and shapes of size indicated for openings and recesses in masonry walls and partitions at locations indicated.

        - Weld adjoining members together to form a single unit where indicated.

Delete paragraph below if bearing lengths are indicated on Drawings or in schedules.

        - Size loose lintels to provide bearing length at each side of openings equal to one-twelfth of clear span, but not less than 8 inches (200 mm), unless otherwise indicated.

Delete below if not required.

        - Galvanize loose steel lintels located in exterior walls.

      - MISCELLANEOUS FRAMING AND SUPPORTS

        - General:  Provide steel framing and supports that are not a part of structural-steel framework as necessary to complete the Work.

Delete paragraph above and retain paragraph below if building does not have a structural-steel frame.

        - Fabricate units from structural-steel shapes, plates, and bars of welded construction, unless otherwise indicated.  Fabricate to sizes, shapes, and profiles indicated and as necessary to receive adjacent construction retained by framing and supports.  Cut, drill, and tap units to receive hardware, hangers, and similar items.

Delete three subparagraphs below if not required.

          - Fabricate units from slotted channel framing where indicated.

          - Where units are indicated to be cast into concrete or built into masonry, equip with integrally welded steel strap anchors 1-1/4 inches (32 mm) wide by 1/4 inch (6 mm) thick by 8 inches (200 mm) long at 24 inches (600 mm) o.c., unless otherwise indicated.

          - Furnish inserts if units must be installed after concrete is placed.

Below are sample requirements; revise to suit Project.  Add similar provisions for other supports, such as for ceiling hung toilet compartments, overhead doors, etc.  Base support and bracing sizes on recommendations of manufacturer of item being supported.  Insert requirements for other specific applications.

Revise paragraph and subparagraphs below if girders are spliced.  Add ASTM A 325 bolts to "Fasteners" Article if required for splicing or for connecting to pipe columns.

Retain subparagraph below with either paragraph above if required; delete if bollards are concrete filled.

Retain paragraph below if required for mounting bollards on structural slab or on existing pavement.

Add other specific items here to suit Project.

      - FINISHES, GENERAL

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

        - Finish metal fabrications after assembly.

      - STEEL AND IRON FINISHES

        - Preparation for Shop Priming:  Prepare uncoated ferrous-metal surfaces to comply with minimum requirements indicated below for SSPC surface-preparation specifications and environmental exposure conditions of installed metal fabrications:

Retain or revise subparagraphs below to suit Project service conditions of installed work.  Insert other exposures and preparation requirements where applicable.  Refer to SSPC Specification referenced.  Both subparagraphs apply to locations that would normally remain dry in service.

          - Exteriors (SSPC Zone 1B):  SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."

          - Interiors (SSPC Zone 1A):  SSPC-SP 3, "Power Tool Cleaning."

        - Apply shop primer to uncoated surfaces of metal fabrications, except those with galvanized finishes and those to be embedded in concrete, sprayed-on fireproofing, or masonry, unless otherwise indicated.  Comply with SSPC-PA 1, "Paint Application Specification No. 1," for shop painting.

Delete below if not required.  Stripe painting adds cost but helps ensure that hard-to-reach areas, such as crevices, inside corners, and welds, are thoroughly coated and that sharp edges (which are vulnerable to chipping and where the film may be thinner due to surface tension) receive adequate coverage.

          - Stripe paint corners, crevices, bolts, welds, and sharp edges.

- EXECUTION

      - INSTALLATION, GENERAL

        - Fastening to In-Place Construction:  Provide anchorage devices and fasteners where necessary for securing metal fabrications to in-place construction.  Include threaded fasteners for concrete and masonry inserts, toggle bolts, through-bolts, lag bolts, wood screws, and other connectors.

        - Cutting, Fitting, and Placement:  Perform cutting, drilling, and fitting required for installing metal fabrications.  Set metal fabrications accurately in location, alignment, and elevation; with edges and surfaces level, plumb, true, and free of rack; and measured from established lines and levels.

        - Provide temporary bracing or anchors in formwork for items that are to be built into concrete, masonry, or similar construction.

        - Fit exposed connections accurately together to form hairline joints.  Weld connections that are not to be left as exposed joints but cannot be shop welded because of shipping size limitations.  Do not weld, cut, or abrade surfaces of exterior units that have been hot-dip galvanized after fabrication and are for bolted or screwed field connections.

        - Field Welding:  Comply with the following requirements:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

          - At exposed connections, finish exposed welds and surfaces smooth and blended so no roughness shows after finishing and contour of welded surface matches that of adjacent surface.

Delete paragraph below if no aluminum.

        - Corrosion Protection:  Coat concealed surfaces of aluminum that will come into contact with grout, concrete, masonry, wood, or dissimilar metals with a heavy coat of bituminous paint.

Delete articles below not applicable to Project.  Insert others where needed to specify requirements applicable to a specific item not covered under general installation requirements above.

      - SETTING BEARING AND LEVELING PLATES

        - Clean concrete and masonry bearing surfaces of bond-reducing materials, and roughen to improve bond to surfaces.  Clean bottom surface of plates.

        - Set bearing and leveling plates on wedges, shims, or leveling nuts.  After bearing members have been positioned and plumbed, tighten anchor bolts.  Do not remove wedges or shims but, if protruding, cut off flush with edge of bearing plate before packing with grout.

Revise subparagraph below if only metallic grout is used at concealed, protected locations.

          - Use nonshrink, nonmetallic grout, unless otherwise indicated.

Delete below if not required.

          - Pack grout solidly between bearing surfaces and plates to ensure that no voids remain.

        - Where bearing plates are indicated with integral anchors, set in cement grout while grout is fluid.  Level the surface and provide temporary support while grout hardens.  Do not force anchors in partially hardened grout.

Revise subparagraph below if only metallic grout is used at concealed, protected locations.

          - Where non-shrink grout is indicated, pack between bearing surfaces as indicated above.

      - INSTALLING MISCELLANEOUS FRAMING AND SUPPORTS

        - General:  Install framing and supports to comply with requirements of items being supported, including manufacturers' written instructions and requirements indicated on Shop Drawings, if any.

        - Support steel girders on solid grouted masonry, concrete, or steel columns.  Secure girders with anchor bolts embedded in grouted masonry or concrete or with bolts through top plates of columns.

Delete subparagraph below if not required.

          - Where grout space under bearing plates is indicated at girders supported on concrete or masonry, install as specified above for setting and grouting bearing and leveling plates.

        - Install columns on concrete footings with grouted baseplates.  Position and grout column baseplates as specified above for setting and grouting bearing and leveling plates.

Delete below if no pipe columns support steel girders.

          - Do not grout baseplates of columns supporting steel girders until girders are installed and leveled.

Delete below if no removable bollards.

      - ADJUSTING AND CLEANING

        - Touchup Painting:  Immediately after erection, clean field welds, bolted connections, and abraded areas of shop paint, and paint exposed areas with the same material as used for shop painting to comply with SSPC-PA 1 for touching up shop-painted surfaces.

          - Apply by brush or spray to provide a minimum 2.0-mil (0.05-mm) dry film thickness.

Retain paragraph and subparagraph above if touchup painting is in this Section.  Retain paragraph below if it is in Division 9 Section "Painting."  Revise reference if another Division 9 Section, such as "Special Coatings," is used.

        - Touchup Painting:  Cleaning and touchup painting of field welds, bolted connections, and abraded areas of shop paint are specified in Division 9 Section "Painting."

END OF SECTION 05500