Copyright 1999, The American Institute of Architects (AIA)

SECTION 07531 - EPDM MEMBRANE ROOFING

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

Adjust list below to suit Project.

          - Adhered membrane roofing system.

          - Roof insulation.

          - Fascias/gravel stops, counter flashings, Scuppers and Downspouts.

          - Repair at existing gravel roof including new gravel stops as detailed.

Delete first paragraph below if no acoustical roof deck is required.

        - This Section includes the installation of acoustical roof deck rib insulation strips furnished under Division 5 Section "Steel Deck."

        - Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

          - Division 6 Section Rough Carpentry for wood nailers, curbs, and blocking, and for wood roof deck panels.

          - Division 7 Section "Joint Sealants”.

Unit prices may be required in bid documents.  One example is removal and replacement of wet roof insulation that may be discovered during reroofing.

If alternates or allowances apply to work of this Section, insert brief paragraphs here to alert Contractor and reference appropriate Division 1 Section for specific details.

      - DEFINITIONS

        - Roofing Terminology:  Refer to ASTM D 1079 and glossary of NRCA's "The NRCA Roofing and Waterproofing Manual" for definition of terms related to roofing work in this Section.

Retain two definitions below if design uplift pressure subparagraphs based on SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems" are retained in "Performance Requirements" Article.  The membrane roofing system must resist, at a minimum, design uplift pressure.  Design uplift pressure, multiplied by a safety factor, produces the factored design uplift pressure.

        - Design Uplift Pressure:  The uplift pressure, calculated according to procedures in SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems," before multiplication by a safety factor.

        - Factored Design Uplift Pressure:  The uplift pressure, calculated according to procedures in SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems," after multiplication by a safety factor.

      - PERFORMANCE REQUIREMENTS

        - General:  Provide installed roofing membrane and base flashings that remain watertight; do not permit the passage of water; and resist specified uplift pressures, thermally induced movement, and exposure to weather without failure.

        - Material Compatibility: Provide roofing materials that are compatible with one another under conditions of service and application required, as demonstrated by roofing membrane manufacturer based on testing and field experience.

          - All materials used shall be 100% asbestos free.

        - Regulatory Requirements:

          - OSHA Requirements - Special attention is to be given to 29 CFR 1926.500(g) - Guardrails, Handrails, and Covers - for the roofing projects.

Retain paragraph and subparagraphs below if membrane roofing system is to be designed to withstand uplift pressure established by ASCE 7.  Revise design uplift pressures in subparagraphs below if local building code requirements are more stringent than ASCE 7.  Retain with "FMG Listing" Paragraph and subparagraphs below if both ASCE 7 and FMG criteria may apply.  Delineate dimensions of corners, perimeter, and field of roof on Drawings.  Delete paragraph and subparagraphs below if a loosely laid and ballasted membrane roofing system is required.

        - Roofing System Design:  Provide a membrane roofing system that is identical to systems that have been successfully tested by a qualified testing and inspecting agency to resist uplift pressure calculated according to ASCE 7-latest revision.

          - Corner Uplift Pressure: 52-lbf/sq. ft..

          - Perimeter Uplift Pressure: 40-lbf/sq. ft..

          - Field-of-Roof Uplift Pressure: 28-lbf/sq. ft..

Retain paragraph and subparagraphs below if Project is FMG insured or if FMG requirements will set a minimum quality standard.  Coordinate requirements of FMG classification with other requirements in this Section.  Loosely laid and ballasted membrane roofing systems cannot be FMG approved but may be accepted by FMG on a project-by-project basis.

        - FMG Listing:  Provide roofing membrane, base flashings, and component materials that comply with requirements in FMG 4450 and FMG 4470 as part of a membrane roofing system and that are listed in FMG's "Approval Guide" for Class 1 or noncombustible construction, as applicable.  Identify materials with FMG markings.

Select one option in first subparagraph below based on windstorm classification of Project.  FMG Loss Prevention Data Sheet 1-28 multiplies the actual field-of-roof uplift pressure by a factor of 2 to obtain the factored pressure, the number that establishes the minimum FMG approval rating.  Verify availability of roofing systems that meet these classifications.  Other options for classifications increase in increments of 15, e.g., Class 1A-135, 1A-150, 1A-165, and higher.  "Class 1A" signifies meeting ASTM E 108, Class A fire performance for FMG-approved Class 1 roof covers.  For areas having three or more hailstorms annually, FMG recommends SH (severe hail) rated roofing systems instead of MH (moderate hail).

          - Fire/Windstorm Classification: Class 1A-90.

Retain paragraph and subparagraphs below if membrane roofing system is to be designed to withstand wind loads established from SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems."  SPRI derives design uplift pressure using ASCE 7's wind load procedure and increases this pressure by a safety factor.  Delete below if a loosely laid and ballasted membrane roofing system is required.

SPRI requires the calculated design uplift pressure for each roof area to be multiplied by a safety factor to arrive at uplift resistance required of the membrane roofing system.  Delineate dimensions of corners, perimeter, and field of roof on Drawings.

      - SUBMITTALS

        - Product Data:  For each type of product indicated. Submit copies of descriptive literature to the Engineer for approval.  The literature shall include information on the roofing membrane with all ancillary materials required, roof insulation, fascia systems, coping system, scuppers, downspouts, gravel stops, expansion joints, application methods and a copy of the roof system manufacturers standard “Total System Warranty”.

        - Shop Drawings: For roofing system, submit copies of literature to Engineer for approval. Include plans, elevations, sections, details, and attachments to other Work.

Adjust list below to suit Project.

          - Check field dimensions and make fabricated work correspond to approved shop drawings and conditions.

          - Fascia system, coping system, scuppers, downspouts and sheet metal work indicating materials, thickness, weights and methods of installation.

          - Sheet sizes and splice locations.

          - Base flashings and membrane terminations.

          - Tapered insulation, including slopes.

          - Insulation fastening patterns.

          - Special details.

          - Adjacent work of other trades

        - Manufacturer’s Standard Details and Shop Drawings: Shop drawings are required for final inspection of the warranted roof.  All shop drawings must include as-built conditions of the following:

          - Outline of the roof and roof size.

          - Location and type of penetrations.

          - Perimeter and penetration details.

          - Special details.

          - Bill of material.

          - Manufacturer's assigned number.

        - Post Submittals:

          - The roof system manufacturer’s standard “Total System Warranty” with the shop drawings as required in paragraph C above. .

          - A Copy of roofing system manufacturer's inspection report of completed roofing installation.

        - Approval: Roof system manufacturer shall approve all details relating to the installation of the roof system.

        - Samples for Verification:  For the following products:

Adjust list below to suit Project.

          - 12-by-12-inch square of sheet roofing, of color specified, including T-shaped side and end lap seam.

          - 6-by-6-inch square of roof insulation.

          - 6 inch long  piece of fascia, coping, scuppers, downspouts .

          - 12-by-12-inch square of walkway pads or rolls.

          - 12-inch length of metal termination bars.

          - 12-inch length of battens.

          - One insulation fasteners of each type, and finish.

          - One roof cover fasteners of each type, length, and finish.

Retain paragraph below if Installer certification is required in "Quality Assurance" Article or a special warranty is required.

        - Installer Certificates:  Signed by roofing system manufacturer certifying that Installer is approved, authorized, or licensed by manufacturer to install roofing system.

Retain paragraph and subparagraph below if "Performance Requirements" Article and either "FMG Listing" or "Roofing System Design" Paragraph are retained.

        - Manufacturer Certificates:  Signed by roofing manufacturer certifying that roofing system complies with requirements specified in "Performance Requirements" Article.

          - Submit evidence of meeting performance requirements.

          - Include name and location of contract, reference to specific material usage, and related reference standards.

          - Include related current test reports performed in accordance with specified standards.  The testing shall have been performed by an approved independent laboratory.  Test reports on previously tested materials shall be accompanied by notarized certificates from the manufacturers attesting that the previously tested material is of the same type, quality, manufacturer, and make as that submitted for this project.

          - Furnish a certificate that the system used will have a U.L. Class A label

        - Letter of Suitability: Signed by roofing manufacturer stating that the insulation is suitable for use in the specified system.

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

Insert specific model code organization in first paragraph below or revise if report must be from another source.

        - Maintenance Data: For roofing system to include in maintenance manuals.

Retain paragraph below if desired.  Submittal of sample warranty provides Architect or Owner an opportunity to further verify that warranty coverage meets requirements.

Retain below if manufacturer's final roof inspection report is required.

      - QUALITY ASSURANCE

FMG is launching a certified roofing installer program.  Add certification requirements to first paragraph below if Project is FMG insured and a certified roofing installer is required.

        - Installer Qualifications:  A qualified firm that is approved, authorized, or licensed by roofing system manufacturer to install manufacturer's product and that is eligible to receive manufacturer's warranty.

            - The Roofing Contractor shall use only competent and skilled workmen completely familiar with the products and the manufacturer's currently recommended methods of installation.

            - The Roofing Contractor shall be able to substantiate they have installed a minimum of 500,000 square feet of roofing of this type and have a manufacturer’s installation rating of 9.0 or better.

Retain paragraph below if Contractor selects testing agency.

Retain first paragraph below if required to meet provisions of special manufacturer's warranty.  Consult manufacturer's literature for requirements because they vary.

        - Fire-Test-Response Characteristics: Provide membrane roofing materials with the fire-test-response characteristics indicated as determined by testing identical products per test method below by UL, FMG, or another testing and inspecting agency acceptable to authorities having jurisdiction.  Materials shall be identified with appropriate markings of applicable testing and inspecting agency.

Retain one of three options in subparagraph below based on fire classification of roof assembly and roof covering.  Delete subparagraph if exterior fire-test exposure is included in FMG class designation in "Performance Requirements" Article above.

          - Exterior Fire-Test Exposure: Class A; ASTM E 108, for application and roof slopes indicated.

Delete subparagraph below if fire-resistance rating of roof assembly is not applicable.  Indicate rating, testing agency, and testing agency's design designation on Drawings.

Consider retaining paragraph below if roofing installation is large and complicated.  A preliminary roofing conference would precede a preinstallation conference and focus on roof deck construction and planning activities of roofing Installer.

Delete subparagraphs below not required.  If retaining, revise to include Project-specific requirements.  Insert additional requirements to suit Project.

Preinstallation conference below is recommended with or without preliminary roofing conference above.

        - Preinstallation Conference: Before installing any components of the roof system, conduct conference at Project site " Provide at least 5 working days notice before the conference.  Review methods and procedures related to roofing system including, but not limited to, the following:

Delete subparagraphs below not required.  If retaining, revise to include Project-specific requirements.  Insert additional requirements to suit Project.

          - Meet with Owner; Architect; Owner's insurer if applicable; testing and inspecting agency representative; roofing Installer; roofing system manufacturer's representative; deck Installer; and installers whose work interfaces with or affects roofing, including installers of roof accessories and roof-mounted equipment.

          - Review methods and procedures related to roofing installation, including manufacturer's written instructions.

          - Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

          - Examine deck substrate conditions and finishes for compliance with requirements, including flatness and fastening.

          - Review structural loading limitations of roof deck during and after roofing.

          - Review base flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that will affect roofing system.

          - Review governing regulations and requirements for insurance and certificates if applicable.

          - Review temporary protection requirements for roofing system during and after installation.

          - Review roof observation and repair procedures after roofing installation.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver roofing materials to Project site in original containers with seals unbroken and labeled with manufacturer's name, product brand name and type, date of manufacture, and directions for storing and mixing with other components.

          - All materials furnished by the systems manufacturer, other than membrane, shall be stored between 60 degrees F and 80 degrees F.  Should they be exposed at lower temperatures, restore to above  temperature prior to use.  Do not use materials damaged in handling or storage.  All cardboard containers shall be stored in a dry area.

        - Store liquid materials in their original undamaged containers in a clean, dry, protected location and within the temperature range required by roofing system manufacturer.  Protect stored liquid material from direct sunlight.

          - Discard and legally dispose of liquid material that cannot be applied within its stated shelf life.

        - Protect roof insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources.  Store in a dry location.  Comply with insulation manufacturers written instructions for handling, storing, and protecting during installation.

        - Handle and store roofing materials and place equipment in a manner to avoid permanent deflection of deck.

      - PRODUCT HANDLING

        - The Roofing and Flashing Subcontractor shall furnish and maintain his own scaffolding, mechanical hoisting equipment and operating personnel, and all required rigging.

        - No materials weighing in bulk over 1,000 pounds shall be hoisted upon any roof deck without the prior supervision and approval of the Engineer or his Representative.

      - INSPECTION

        - Upon completion of the installation, an inspection shall be made by a representative of the roof system manufacturer to ascertain that the roofing system has been installed according to published specifications and details.  Warranty shall be issued to the Owner upon manufacturer's approval of the installation.

      - DEVIATION

        - The latest printed specifications of the approved roofing materials manufacturer shall govern the work unless a more stringent requirement is specified herein.

      - PROJECT CONDITIONS

        - Weather Limitations:  Proceed with installation only when existing and forecasted weather conditions permit roofing system to be installed according to manufacturer's written instructions and warranty requirements.

      - WARRANTY

        - A manufacturer's sole source 15 year Total Roofing System Warranty shall be provided with a peak gust wind speed limitation of 80 mph (measured 30 feet above the ground). Warranty shall cover both labor and materials with no dollar limitation and shall state that the Total Roofing System will remain in a watertight condition. The contractor shall provide as part of the shop drawing submittal process, certification indicating that the manufacturer has reviewed and has agreed to such wind coverage indicated.

          - Total Roofing System is defined as the following materials and provided by the roof system manufacturer:  membrane, flashings, counterflashings, adhesives, sealants, insulation, overlayment, fasteners, fastener plates, fastener strips, hard rubber, metal edging, preformed fascia system, metal termination anchor bars, roof drain flashing and sealants, and any other product utilized in this system installation.

          - The warranty shall also provide without any limitations that the insulation shall retain at least 80% of its thermal resistance.

          - The warranty shall be for fifteen (15) years starting after final acceptance of the total roofing system by the roof system manufacturer.  Defective materials or installation shall be removed, properly disposed of, and replaced at the manufacturer's expense.

          - The warranty shall provide that if within the warranty period the roofing system becomes non-watertight or if the elastomeric sheet splits, tears, or separates at the seams because of defective materials and/or workmanship that correction of defective workmanship and/or material and cost thereof shall be the responsibility of the manufacturer.  Should the manufacturer or his approved applicator fail to perform repairs within 72 hours of notification, the warranty will not be voided because of work being performed by others to repair the roofing regardless of the manufacturer's warranty to the contrary.

          - The Total Roofing System shall be applied by a Roofing Contractor approved by the system manufacturer.  After inspection and acceptance of the installed roof system, the warranty will be issued.

When warranties are required, verify with Owner's counsel that special warranties stated in this Article are not less than remedies available to Owner under prevailing local laws.  Coordinate with Division 1 Section "Product Requirements."

Retain paragraph below if manufacturer's labor-and-materials warranty, covering roofing system, is required.  Verify coverage offered by manufacturers because roof insulation, fasteners, and other roofing components may be excluded unless part of a roofing membrane manufacturer's roofing system warranty.  If adding special provisions, retitle paragraph "Special Roofing Manufacturer's Warranty."  Verify warranty availability and coordinate choice of manufacturers in Part 2 accordingly.

Retain options in subparagraph below based on those used on Project.  Verify availability of manufacturer's total-system warranty and components included.

Revise warranty to period required and verify availability; 10- and 15-year periods predominate.  Standard manufacturers' warranties begin on completion of roofing system.  AIA Document A201 establishes that the period begins with Substantial Completion.

Usually delete below if retaining manufacturer's warranty above.  Manufacturer's labor-and-materials warranty typically binds Installer for the first two or three years.  If retaining special Project warranty below, use or modify sample roofing Installer's warranty form at end of this Section.  Alternately, insert copy of local roofing contractor association's warranty form or use another form as advised by Owner's counsel.  Revise below to reflect scope of special Project warranty.

- PRODUCTS

      - MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations in Division 7 Section "Elastomeric Membrane Roofing" for cautions about naming manufacturers and products.

Edit this Article with other Part 2 articles in which manufacturers and products, or manufacturers only, are named.  See Division 1 Section "Product Requirements" for an explanation of the terms "Available Products," "Products," "Available Manufacturers," and "Manufacturers" and the effect these terms have on "Comparable Product" and "Product Substitution" requirements.

        - Manufacturers: Subject to compliance with requirements of this section, provide products by one of the following:

          - EPDM Sheet

            - Carlisle Syntec Systems; Carlisle Corp

            - Firestone Building Products Company

            - Versico Inc.

          - Rigid/tapered insulation: Manufacturer as required by the roofing system manufacturer for total system warranty.

          - Fascia, scuppers, counter flashings and down spouts: Shop fabricated by roofing installer.

      - EPDM ROOFING MEMBRANE

Class A exterior fire-test rating for either an adhered or mechanically fastened EPDM roofing system may require a specially formulated fire-retardant sheet; verify with manufacturer.

        - EPDM Roofing Membrane:  ASTM D 4637, Type I, nonreinforced] uniform, flexible sheet made from EPDM, and as follows:

Select thickness from options in subparagraph below.  First two thicknesses predominate.

          - Thickness: .060”, nominal.

Select color from options in subparagraph below.

          - Exposed Face Color: Black.

          - Backing: unbacked.

Retain product below if specifying Carlisle's proprietary fleece-backed EPDM.

      - AUXILIARY MATERIALS

        - General:  Auxiliary materials recommended by roofing system manufacturer for intended use and compatible with membrane roofing.

          - Liquid-type auxiliary materials shall meet VOC limits of authorities having jurisdiction.

        - Sheet Flashing: .060”- thick EPDM, partially cured or cured, according to application.

Delete first paragraph and subparagraphs below if not required.  Available from Carlisle, epichlorohydrin is intended to protect EPDM from hydrocarbons, non-aromatic solvents, grease, and oil.  Delete this sheet and replace with another sheet if applicable.

        - Bonding Adhesive: Manufacturer’s standard bonding adhesive.

Retain paragraph below if fleece-backed roofing membrane is required to be set in cold fluid-applied adhesive.

Select one option in first paragraph below based on method of seaming required.  Retain both options if choice of seaming method is Contractor's option.

        - Seaming Material: Manufacturer's standard synthetic-rubber polymer primer and 3-inch- wide minimum, butyl splice tape with release film].

        - Lap Sealant: Manufacturer’s standard single-component sealant, color to match roofing membrane.

        - Water Cutoff Mastic:  Manufacturer's standard butyl mastic sealant.

        - Metal Termination Bars:  Manufacturer's standard predrilled stainless-steel or aluminum bars, approximately 1 by 1/8 inch thick; with anchors.

        - Fasteners:  Factory-coated steel fasteners and metal or plastic plates meeting corrosion-resistance provisions in FMG 4470, designed for fastening membrane to substrate, and acceptable to membrane roofing system manufacturer.

        - Miscellaneous Accessories: Provide pourable sealers, preformed cone and vent sheet flashings, preformed inside and outside corner sheet flashings, T-joint covers, in-seam sealants, termination reglets, and other accessories recommended by roofing system manufacturer for intended use.

Delete paragraph below unless a color coating of roofing membrane or base flashing is required for aesthetic reasons or improved reflectance.

Select coating from options in subparagraph below.

Select color from below.  Verify availability with manufacturer.

Select one of three substrate boards below if required or delete this Article.  Substrate boards may serve as model building code-required thermal barriers, separating foam insulation from steel or wood deck.  They may also be used over steel deck as part of a fire-resistance-rated roofing system or to provide a smooth substrate for a vapor retarder.

        - Cover Board:  Cellulostic-fiber insulating board, ASTM C 208, Type II, Grade 2, ½ inch thick.

Retain below with substrate board selected from paragraphs above.

Delete this Article if vapor retarders are not required.  Review compatibility of vapor retarder with other membrane roofing system materials.  A substrate board or layer of insulation will be needed because vapor retarders cannot be placed directly over a steel deck.  Retitle Article "Air Retarder" or "Vapor/Air Retarder" depending on function of retarder.

Retain one of two subparagraphs below with paragraph above.

Delete vapor-retarder options above and add other products, such as self-adhering rubberized asphalt sheets, if required.

      - ROOF INSULATION

Delete from this Article insulation materials not required.  If retaining more than one insulation material, show location of each on Drawings or indicate where each layer is used in roofing system.  If allowing Contractor to select from more than one insulation material, limit options to insulations that will meet Project requirements and limitations.  Coordinate insulation selection and thicknesses indicated on Drawings with adjoining construction as well as HVAC design and energy program.

Roofing system manufacturers may require use of their own insulations or limit approvals to some insulation manufacturers.  Correlate lists of insulation manufacturers in subparagraphs below with insulation manufacturers approved by roofing system manufacturers, or delete lists altogether for total-system warranties.

        - General:  Provide preformed roof insulation boards that comply with requirements and referenced standards, selected from manufacturer's standard sizes and of thicknesses indicated with a maximum thickness of each layer of 2”.

        - Roof Insulation (Rigid):  Glass fiber reinforced facers integrally laminated to the rigid polyisocyanurate foam core on both sides.  Insulation to be compatible with the membrane used and supplied by the membrane manufacturer.  Tapered as required, to form crickets.

          - The insulation system shall consist of polyisocyanurate foam panels, chemically bonded during the foaming process to facers on the top and bottom surfaces, and shall conform to the following:

Property						Test Method			Specification

*Thermal Performances			ASTM C 518				as required

Water Absorption % Volume		ASTM C 209				 1

Dimensional Stability			70 degrees C/100% RH		1%

Compressive Strength			ASTM D 1621				18 psi

Foam Core Density				ASTM D 1622				2.0 lbs/cu. ft.

Moisture Vapor Transmission		ASTM C 355				   1

Service Temperature				----------					-100 degrees F to

+250 degrees F

Flame Spread					ASTM E 84				  25

*Thermal values for the installed tapered insulation system shall be "LTTR" values and determined in accordance with CAN/ULC-S770 test method.

          - Insulation system facers shall be glass fiber reinforced mat asphaltic.

          - The tapered insulation system used for crickets shall have a minimum slope of 1/4" per foot unless indicated otherwise on the drawings.

          - The insulation system, not counting the ½” cover board, shall have a minimum thickness of 2" and a minimum average "LTTR" value of 30 unless indicated otherwise on the drawings.

          - Insulation to be compatible with the membrane used and supplied by the membrane manufacturer.

Select one of two "Facer" subparagraphs below, or revise to another board facer if required.  An example of the first product is "Perform Plus" by AFM Corp., and of the second, "R-Control SpecLam" by AFM Corp.  If a field-installed cover board is required, see "Insulation Accessories" Article for options.

Retain below with or without tapered insulation above.  Delete if not required.

        - Provide preformed saddles, crickets, tapered edge strips, and other insulation shapes where indicated for sloping to drain.  Fabricate to slopes indicated.

      - INSULATION ACCESSORIES

        - General:  Furnish roof insulation accessories recommended by roof system manufacturer for intended use and compatible with membrane roofing.

Retain first paragraph below if insulation requires mechanical fastening.

        - Fasteners:  Factory-coated steel fasteners and metal or plastic plates meeting corrosion-resistance provisions in FMG 4470, designed for fastening roof insulation to substrate, and acceptable to roofing system manufacturer.

Select one of three cover boards below if required.  Cover or overlay boards are usually needed over noncomposite foam insulation or over existing roofing before installing new roofing.

        - Overlayment:  Meeting ASTM C 208, Class E, ASTM 209, Roof Insulating Board Grade.  Manufacturer shall mark each package, giving kind of chemical and guarantee minimum quantity contained.  Fiberboard shall be 1/2" thick unless otherwise indicated, high density fiberboard.

      - WALKWAYS

Retain one of two paragraphs and associated subparagraphs below for preformed roof walkway products.  Revise to suit other walkway products if required.

        - Flexible Walkway pads or rolls: Factory-formed, nonporous, heavy-duty, solid-rubber, slip-resisting, surface-textured walkway pads or rolls, approximately 3/16 inch thick, and acceptable to membrane roofing system manufacturer.

Retain heavyweight roof pavers as walkways in paragraph and subparagraphs below if required.

      - FASCIAS , METAL FLASHING, and COUNTER FLASHINGS:

        - Fascia System with Scuppers: 24-gauge zinc coated steel Fascia System with Kynar 500 finish.  Shop fabricated fascia systems will be acceptable and must be fabricated to look similar in shape to the detail on the drawings maximum height of 8”.

          - Fascia Extender: 24 gauge zinc coated steel, with Manufacturer's standard, , Kynar 500 finish, and 24 gauge galvanized steel continuous fastening cleat

          - Blind nailers:  Shall be the same material and gauge as the fascia.

          - Down spouts:  Shall be the same material and gauge as the fascia and shall be a 3 sided opened face downspout fabricated per SMACNA fig. 1-32-E.

          - Color:   To match existing  fascia on adjacent parapet wall.

        - Counter Flashings:  16 oz. Alloy coated Copper equal to Revere FreedomGray Z-T Alloy coated copper.

          - Solder for coated Copper:  Use non-lead, Tin solders, i.e. pure tin or zinc/tin alloys.  Prepare the substrate in accordance with the manufactures latest recommended practices.  Use a Zinc-chloride (killed acid) flux.  When done soldering neutralize the area soldered by flushing with a mild baking soda/ water solution.

          - Nails for coated Copper Sheet:  Copper or hardware bronze, 0.109 inch (2.8 mm) minimum and not less than 7/8 inch (22 mm) long, barbed with large head.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with the following requirements and other conditions affecting performance of roofing system:

          - Verify that roof openings and penetrations are in place and set and braced and that roof drains are securely clamped in place.

          - Verify that wood blocking, curbs, and nailers are securely anchored to roof deck at penetrations and terminations and that nailers match thicknesses of insulation.

Retain subparagraph below for steel roof deck.

          - Verify that surface plane flatness and fastening of steel roof deck complies with requirements in Division 5 Section "Steel Deck."

Retain or revise first three subparagraphs below for concrete roof decks.

          - Proceed with installation only after unsatisfactory conditions have been corrected.

          - Install new gravel stops on existing gravel roof per industry standards.

      - PREPARATION

        - Clean substrate of dust, debris, moisture, and other substances detrimental to roofing installation according to roofing system manufacturer's written instructions.  Remove sharp projections.

        - Prevent materials from entering and clogging roof drains and conductors and from spilling or migrating onto surfaces of other construction.  Remove roof-drain plugs when no work is taking place or when rain is forecast.

        - Complete terminations and base flashings and provide temporary seals to prevent water from entering completed sections of roofing system at the end of the workday or when rain is forecast.  Remove and discard temporary seals before beginning work on adjoining roofing.

        - Install acoustical roof deck rib insulation strips, specified in Division 5 Section "Steel Deck," according to acoustical roof deck manufacturer's written instructions

      - INSULATION INSTALLATION

        - Coordinate installing membrane roofing system components so insulation is not exposed to precipitation or left exposed at the end of the workday.

        - Comply with membrane roofing system manufacturer's written instructions for installing roof insulation.

Retain paragraph below if tapered insulation is required.

        - Install tapered insulation under area of roofing to conform to slopes indicated.

Revise thickness in first paragraph below to suit Project.

        - Install one or more layers of insulation under area of roofing to achieve required thickness.  Where overall insulation thickness is 2 inches or greater, install 2 or more layers with joints of each succeeding layer staggered from joints of previous layer a minimum of 12 inches in each direction.

        - Trim surface of insulation where necessary at roof drains so completed surface is flush and does not restrict flow of water.

          - Provide a square sump at all roof drains as indicated on the drawings.  If not indicated, provide a four foot square sump (roof drain to be in center of sump) with a 1/4" per foot pitch from the four sides of the sump toward the roof drain.

        - Install insulation with long joints of insulation in a continuous straight line with end joints staggered between rows, abutting edges and ends between boards.  Fill gaps exceeding 1/4 inch with insulation.

          - Cut and fit insulation within 1/4 inch of nailers, projections, and penetrations.

Retain paragraph below for loosely laid and ballasted roofing membranes.

Retain paragraph below if mechanically fastening each insulation layer.

        - Mechanically Fastened Insulation:  Install cover boards over insulation with long joints in continuous straight lines with end joints staggered between rows.  Loosely butt cover boards together and fasten to roof deck using mechanical fasteners specifically designed and sized for fastening specified board-type roof insulation to deck type:

Retain first subparagraph below when Project is FMG insured or FMG requirements are proposed as a performance standard.  Retain second subparagraph if number of fasteners will be based on ASCE 7's uplift pressure or SPRI's factored design uplift pressure.  Coordinate with "Performance Requirements" Article in Part 1.  Fastener numbers will increase at corners and perimeter over number required for field of roof.

          - Fasten insulation according to requirements in FMG's "Approval Guide" for specified Windstorm Resistance Classification.1-90.

          - Fasten insulation to resist uplift pressure at corners, perimeter, and field of roof.

          - Mechanical fasteners at exposed metal deck in finished areas shall only be fastened to the high point of the metal decking with a penetration not exceeding 3/4".  Fastening to the low point of the metal decking in these areas will not be acceptable.

Retain paragraph below if mechanically fastening the first layer of insulation and adhering the remaining layers.  This is the most common application method.

      - ADHERED ROOFING MEMBRANE INSTALLATION

Retain this Article for adhered roofing membrane installations.

        - Install EPDM roofing membrane over area to receive roofing according to membrane roofing system manufacturer's written instructions.  Unroll roofing membrane and allow to relax before installing.

Delete first paragraph below if not applicable.

        - Start installation of roofing membrane in presence of membrane roofing system manufacturer's technical personnel.

        - Accurately align roofing membrane and maintain uniform side and end laps of minimum dimensions required by manufacturer.  Stagger end laps.

Retain paragraph below for adhesive bonding membrane to substrate.

        - Bonding Adhesive:  Apply bonding adhesive to substrate and underside of roofing membrane at rate required by manufacturer and allow to partially dry before installing roofing membrane.  Do not apply bonding adhesive to splice area of roofing membrane.

Retain paragraph below for bonding fleece-backed membrane in hot roofing asphalt.

        - Apply roofing membrane with side laps shingled with slope of roof deck where possible.

Retain paragraph below for adhesive-splicing roofing membrane seams.

Retain first paragraph below for tape-splicing roofing membrane seams.

        - Tape Seam Installation:  Clean and prime both faces of splice areas, apply splice tape, and firmly roll side and end laps of overlapping roofing membranes according to manufacturer's written instructions to ensure a watertight seam installation.  Apply lap sealant and seal exposed edges of roofing membrane terminations.

        - Repair tears, voids, and lapped seams in roofing that does not meet requirements.

        - Spread sealant or mastic bed over deck drain flange at deck drains and securely seal roofing membrane in place with clamping ring.

Retain paragraph below if tie-ins to existing roofing are required.

        - Install roofing membrane and auxiliary materials to tie in to existing roofing.

Delete below if not required.

      - WALKWAY INSTALLATION

Delete this Article if walkways are not required.

        - Flexible Walkways:  Install walkway products in locations indicated.  Adhere walkway products to substrate with compatible adhesive according to roofing system manufacturer's written instructions.

      - FASCIA:

        - Fascia System: Installation of fascias, scuppers, and downspouts shall be as indicated on the drawings and in strict accordance with manufacturer's recommendations.

          - All Metal Work:  Flashing, sheet metal, and accessories shall be fabricated as specified herein and indicated on the drawings; if not specified or indicated, comply with applicable details and requirements of the latest editions of the Revere "Copper and Common Sense" Manual and the SMACNA "Architectural Sheet Metal" Manual and other recognized practices of the industry.  The completed installation shall be fabricated and installed for waterproof and weather-tight performance.

          - All fastening of metal shall be installed in a way to ascertain the metal work will not either pull free or buckle which could eventually cause roofing problems.

      - MISCELLANEOUS INSTALLATIONS

        - Roof scuppers and down spouts:  Installation of roof scuppers and downspouts shall be as indicated on the drawings and in strict accordance with SMACNA standard.

        - Expansion Joints shall be installed as shown on details and manufacturer's recommendations.

        - Unusual Penetrations:  Clusters of pipes and unusual shaped penetrations shall be sealed with pourable sealer, 2" deep minimum, in a pitch pocket type seal.

      - FIELD QUALITY CONTROL

        - Testing Agency:  Owner may at their option engage a qualified independent testing and inspecting agency to perform roof tests and inspections and to prepare test reports.

A roof inspection is required by manufacturer before warranty issue.  Revise scope of inspection and source of report to a qualified roofing consultant or an independent testing and inspecting agency if preferred.

        - Final Roof Inspection:  Arrange for roofing system manufacturer's technical personnel to inspect roofing installation on completion and submit report to the engineer.

Retain subparagraph below if Architect or Owner wants to be present during manufacturer's final inspection.

          - Notify Engineer and Owner 48 hours in advance of date and time of inspection.

        - Repair or remove and replace components of membrane roofing system where test results or inspections indicate that they do not comply with specified requirements.

        - Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

      - PROTECTING AND CLEANING

        - Protect membrane-roofing system from damage and wear during remainder of construction period.  When remaining construction will not affect or endanger roofing, inspect roofing for deterioration and damage, describing its nature and extent in a written report, with copies to Engineer and Owner.

        - Correct deficiencies in or remove membrane roofing system that does not comply with requirements, repair substrates and repair or reinstall membrane roofing system to a condition free of damage and deterioration at time of Substantial Completion and according to warranty requirements.

Retain below if coating membrane or if using fluid-applied bonding materials.

        - Clean overspray and spillage from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

END OF SECTION 07531