Copyright 1997 , The American Institute of Architects (AIA)

SECTION 07920 - JOINT SEALANTS

This Section uses the term "Architect." change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - SUMMARY

        - This Section includes sealants for the following applications, including those specified by reference to this Section:

- Delete paragraph above or below.  Retain above if other Sections refer to this Section for sealant-related requirements; if not, retain below.

        - This Section includes sealants for the following applications:

- Adjust list below to suit Project.  List summarizes typical sealant joints; complement with schedules, details, and drawing designations indicating exactly where and what products are required.

          - Exterior joints in the following vertical surfaces:

            - Control and expansion joints in cast-in-place concrete.

            - Control and expansion joints in unit masonry.

            - Joints between different materials listed above.

            - Other joints as indicated.

- Joints below cover traffic surfaces that are part of a building and not those in roads, sidewalks, and parking lots, which should be specified in Division 2 Section "Pavement Joint Sealants."

          - Interior joints in the following vertical surfaces:

            - Perimeter joints of exterior openings where indicated.

            - Vertical control joints on exposed surfaces of interior unit masonry and concrete walls and partitions.

            - Perimeter joints between interior wall surfaces and frames of interior doors, windows, and elevator entrances.

            - Joints between plumbing fixtures and adjoining walls, floors, and counters.

            - Other joints as indicated.

        - Related Sections include the following:

- List below only construction that the reader might expect to find in this Section but is specified elsewhere.  Subparagraphs below do not include Sections that cross-reference this Section for requirements.

          - Division 7 Section "Through-Penetration Firestop Systems" for fire-resistant building joint-sealant systems.

      - PERFORMANCE REQUIREMENTS

        - Provide elastomeric joint sealants that establish and maintain watertight and airtight continuous joint seals without staining or deteriorating joint substrates.

- Delete above or below if not applicable.  Modify wording to reflect performance required for both interior and exterior joints.  Add specific applications where watertight or water-resistant performance may not be required or attainable with products selected.

        - Provide joint sealants for interior applications that establish and maintain airtight and water-resistant continuous joint seals without staining or deteriorating joint substrates.

      - SUBMITTALS

        - Product Data:  For each joint-sealant product indicated.

        - Samples for Selection:  Manufacturer's color charts consisting of strips of cured sealants showing the full range of colors available for each product exposed to view.

- Delete paragraph above if colors are preselected and specified or scheduled according to manufacturers' color designations in text or separate schedule, or if required to match Architect's Samples.  Retain below with or without above.

        - Warranties:  Special warranties specified in this Section.

      - QUALITY ASSURANCE

- If a manufacturer's warranty is specified requiring manufacturer's approval or licensing of Installer, revise paragraph below accordingly.

        - Installer Qualifications:  An experienced installer who has specialized in installing joint sealants similar in material, design, and extent to those indicated for this Project and whose work has resulted in joint-sealant installations with a record of successful in-service performance.

        - Source Limitations:  Obtain each type of joint sealant through one source from a single manufacturer.

- Delete paragraph below if not required.  Coordinate with panel mockups specified in other Sections that include sealant joints.

- Delete below if work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1 Section "Project Meetings."

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver materials to Project site in original unopened containers or bundles with labels indicating manufacturer, product name and designation, color, expiration date, pot life, curing time, and mixing instructions for multicomponent materials.

        - Store and handle materials in compliance with manufacturer's written instructions to prevent their deterioration or damage due to moisture, high or low temperatures, contaminants, or other causes.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Do not proceed with installation of joint sealants under the following conditions:

          - When ambient and substrate temperature conditions are outside limits permitted by joint sealant manufacturer.

- Delete subparagraph above or below.  Below could be deleted for silicones applied to nonporous joint substrates provided they are kept dry during sealant application.

          - When ambient and substrate temperature conditions are outside limits permitted by joint sealant manufacturer or are below 40 deg F (4.4 deg C).

          - When joint substrates are wet.

        - Joint-Width Conditions:  Do not proceed with installation of joint sealants where joint widths are less than those allowed by joint sealant manufacturer for applications indicated.

        - Joint-Substrate Conditions:  Do not proceed with installation of joint sealants until contaminants capable of interfering with adhesion are removed from joint substrates.

- PRODUCTS

      - PRODUCTS AND MANUFACTURERS

        - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products listed in other Part 2 articles.

- Retain above for nonproprietary or below for semiproprietary specification.  Refer to Division 1 Section "Product Requirements."

      - MATERIALS, GENERAL

        - Compatibility:  Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by sealant manufacturer based on testing and field experience.

- Retain one paragraph below.  If retaining second, indicate colors in a separate schedule.

        - Colors of Exposed Joint Sealants:  As selected by Engineer from manufacturer's full range for this characteristic.

      - ELASTOMERIC JOINT SEALANTS

- Retain paragraph below with entries in the Elastomeric Joint-Sealant Schedule at end of Part 3 that are needed to specify elastomeric joint sealants for each application.  See Editing Instruction No. 2 and a sample schedule in the Evaluations for guidance.

        - Elastomeric Sealant Standard:  Comply with ASTM C 920 and other requirements indicated for each liquid-applied chemically curing sealant, including those referencing ASTM C 920 classifications for type, grade, class, and uses.

- Delete paragraph below if corresponding requirement is not retained in the Elastomeric Joint-Sealant Schedule at end of Part 3.  This requirement applies only to Class 25 sealants capable of movement in excess of 25 percent in both compression and extension per ASTM C 719.

        - Additional Movement Capability:  Where additional movement capability is specified in the Elastomeric Joint-Sealant Schedule, provide products with the capability, when tested for adhesion and cohesion under maximum cyclic movement per ASTM C 719, to withstand the specified percentage change in the joint width existing at the time of installation and remain in compliance with other requirements of ASTM C 920 for uses indicated.

- Generally retain paragraph below with silicones applied to porous substrates such as marble, limestone, granite, and sandstone.

- Delete paragraph below if no sealants are indicated for applications where they will be immersed continuously in water.  Revise if a liquid other than water applies.

- Delete below if no sealants are indicated for applications where sealants will come in contact with food.  Indicate, on Drawings or by inserts in the Elastomeric Joint-Sealant Schedule, which products must comply.

- Delete any generic description of joint sealants in articles below if not required and not indicated in schedules at end of Part 3.

        - Single-Component Nonsag Urethane Sealant:  Where joint sealants of this type are indicated, provide products complying with the following:

          - Products:  Provide one of the following.

            - Vulkem 116; Mameco International.

            - Vulkem 230; Mameco International.

            - Sikaflex - 1a; Sika Corporation.

            - NP 1; Sonneborn Building Products Div., ChemRex Inc.

          - Type and Grade:  S (single component) and NS (nonsag).

          - Class: 25.

          - Applications:

            - Metal flashing joints.

            - Joints between exterior metal frames and adjacent Work (except masonry).

            - Under exterior door thresholds.

        - Multicomponent Nonsag Urethane Sealant:  Where joint sealants of this type are indicated, provide products complying with the following:

          - Products:  Provide one of the following:

            - Chem-Calk 500; Bostik Inc.

            - Vulkem 922; Mameco International.

            - Dynatrol 2; Pecora Corporation.

            - PSI-270; Polymeric Systems, Inc.

            - NP 2; Sonneborn Building Products Div., ChemRex Inc.

            - Sikaflex-2c, NS; Sika

          - Type and Grade:  M (multicomponent) and NS (nonsag).

          - Class:  25.

- Below are examples of Use O substrates.  Retain only those that apply or insert others.

          - Exterior Applications:

            - Control, expansion, and soft joints in masonry and concrete.

            - Between masonry and adjacent Work.

            - Exterior joints for which no other sealant type is indicated.

- Modify this and succeeding schedules to suit Project.  Retain requirements in Part 2 that reference sealant standards but do not duplicate requirements in Part 2.  When editing schedules, remove brackets [ ] and boldfacing from text selected; also remove <uppercase editor's notes>. Refer to Editing Instruction No. 2 and a completed sample in the Evaluations for an explanation on how to use schedules.

- For each type of sealant product, insert descriptions of applications where each sealant type is required, unless designations in paragraph titles are exclusively used on Drawings for this purpose.  If designations are retained, insert No. in place of [#] to complete designations. If product names are retained, see Editing Instruction No. 1 in the Evaluations for cautions about naming products and manufacturers. Retain only those products that comply with requirements retained for uses related to exposure and joint substrates. See tables in the Evaluations.

- High-modulus neutral-curing silicone products above are those with movement capability of plus or minus 25 percent and those below, of plus or minus 50 percent.

        - Mildew Resistant Silicone Sealant: Where joint sealants of this type are indicated provide products complying with the following:

          - Products:  Provide one of the following:

            - 786; Dow Corning

            - Sanitary 1700; GE Silicones.

            - 898 Silicone Sanitary Sealant; Pecora Corporation.

            - PSI-611; Polymeric Systems, Inc.

            - Tremsil 600 White; Tremco.

          - Type and Grade: S (single component), and NS (nonsag).

          - Class 25

          - Additional Movement Capability:  50 percent movement in extension and 50 percent movement in compression for a total of 100 percent movement.

          - Applications:

            - Use for sealing interior joints with non-porous substrates in wet areas with ceramic tile or epoxy paint around sinks, and between equipment or counters and non-porous walls.

- Below are examples of Use O substrates.  Retain only those that apply or insert others.

- Type M, Grade NS products listed above are suitable for traffic and, for selected products, nontraffic uses; products below are for nontraffic use only.

        - Multicomponent Pourable Urethane Sealant:  Where joint sealants of this type are indicated, provide products complying with the following:

          - Products:  Provide one of the following:

            - Chem-Calk 550; Bostik Inc.

            - Vulkem 245; Mameco International.

            - NR-200 Urexpan; Pecora Corporation.

            - Sikaflex - 2c SL; Sika Corporation.

            - SL 2; Sonneborn Building Products Div., ChemRex Inc.

            - THC-900; Tremco.

          - Type and Grade:  M (multicomponent) and P (pourable).

          - Class:  25.

- Below are examples of Use O substrates.  Retain only those that apply or insert others.

          - Applications:

            - Joints in exterior and interior concrete slabs on grade.

            - Joints in existing concrete slabs on grade.

            - At penetrations to new and existing slabs on grade.

      - LATEX JOINT SEALANTS

        - Latex Sealant Standard:  Comply with ASTM C 834 for each product of this description indicated.

        - Latex Sealant:  Where joint sealants of this type are indicated, provide products complying with the following:

          - Products:  Provide one of the following.

            - Chem-Calk 600; Bostik Inc.

            - NuFlex 330; NUCO Industries, Inc.

            - LC 160 All Purpose Acrylic Caulk; Ohio Sealants, Inc.

            - AC-20; Pecora Corporation.

            - PSI-701; Polymeric Systems, Inc.

            - Sonolac; Sonneborn Building Products Div., ChemRex, Inc.

            - Tremflex 834; Tremco.

          - Applications:  Interior joints in field painted vertical and overhead joints not indicated otherwise below.

      - PREFORMED JOINT SEALANTS

        - Preformed Foam Sealants: Provide manufacturer's standard preformed, precompressed, impregnated, open-cell foam sealant manufactured from high-density urethane foam impregnated with a nondrying, water-repellent agent; factory produced in precompressed sizes and in roll or stick form to fit joint widths indicated and to develop a watertight and airtight seal when compressed to the degree specified by manufacturer; and complying with the following:

          - Properties:  Permanently elastic, mildew resistant, nonmigratory, nonstaining, and compatible with joint substrates and other joint sealants.

- Retain one agent below.  Correlate with product list.  First is nonspecific; second is used with Emseal Joint Systems' "Emseal 25V"; third is used with Emseal's "Emseal Greyflex" and with Salamander Industrial Products' "Blocoband BF" and "Blocoband HF"; and fourth is used with Polytite Manufacturing Corporation's "Polytite Standard" and "Polytite B" and with Sealform's "Wilseal 600."

          - Impregnating Agent:  Manufacturer's standard.

- Retain one density below.  Correlate with product list.  First density is nonspecific; second is for Salamander's "Blocoband HF"; third is for Emseal's "Emseal Greyflex"; fourth is for Sealform's "Wilseal 600"; and fifth is for Salamander's "Blocoband BF" and for Polytite's "Polytite Standard" and "Polytite B."

          - Density:  Manufacturer's standard.

          - Backing:  Pressure-sensitive adhesive, factory applied to one side with protective wrapping.

          - Available Products:

            - Emseal 25V; Emseal Joint Systems, Ltd.

            - Emseal Greyflex; Emseal Joint Systems, Ltd.

            - Polytite B; Polytite Manufacturing Corporation.

            - Polytite Standard; Polytite Manufacturing Corporation.

            - Wilseal 600; Sealform, Ltd.

          - Application:  Exterior expansion joints in masonry veneers.

      - JOINT-SEALANT BACKING

        - General:  Provide sealant backings of material and type that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

        - Backer Rod:  ASTM C 1330, of type indicated below and of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance:

- Retain one of three subparagraphs below or, if retaining more than one, also retain fourth subparagraph.  Product described in third subparagraph is "Sof Rod" by Nomaco.  Verify acceptability of each material for sealants selected.  Type O sealant backings, which are open-cell urethane foams, are unsuitable for horizontal surfaces.  See Evaluations.

          - Type C:  Closed-cell material with a surface skin.

- Retain or revise paragraph below.  Tubing is used as temporary seal and secondary water barrier.  Verify acceptability of tubing for sealants selected.  See Evaluations.

        - Bond-Breaker Tape:  Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint where such adhesion would result in sealant failure.  Provide self-adhesive tape where applicable.

      - MISCELLANEOUS MATERIALS

- Generally retain paragraph below unless it is known that priming of substrates is not required with sealants specified.  Purpose of primers is to improve adhesion of sealant to substrate.

        - Primer:  Material recommended by joint sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

        - Cleaners for Nonporous Surfaces:  Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants with joint substrates.

        - Masking Tape:  Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

- EXECUTION

      - EXAMINATION

        - Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Surface Cleaning of Joints:  Clean out joints immediately before installing joint sealants to comply with joint sealant manufacturer's written instructions and the following requirements:

          - Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, paints (except for permanent, protective coatings tested and approved for sealant adhesion and compatibility by sealant manufacturer), old joint sealants, oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

          - Clean porous joint substrate surfaces by brushing, grinding, blast cleaning, mechanical abrading, or a combination of these methods to produce a clean, sound substrate capable of developing optimum bond with joint sealants.  Remove loose particles remaining from above cleaning operations by vacuuming or blowing out joints with oil-free compressed air.  Porous joint surfaces include the following:

- Delete porous substrates below if not applicable.  Insert additional items to suit Project.

            - Concrete.

            - Masonry.

            - Unglazed surfaces of ceramic tile.

          - Remove laitance and form-release agents from concrete.

          - Clean nonporous surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues capable of interfering with adhesion of joint sealants.

- Delete nonporous substrates below if not applicable.  Insert additional items to suit Project.

- As previously noted in "Miscellaneous Materials" Article, purpose of primers is to improve adhesion of sealant to substrate.

        - Joint Priming:  Prime joint substrates where indicated and recommended in writing by joint sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

          - Apply primer on all porous surfaces such as exterior masonry or precast concrete.

- Delete below if not required.

        - Masking Tape:  Use masking tape where required to prevent contact of sealant with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears.  Remove tape immediately after tooling without disturbing joint seal.

      - INSTALLATION OF JOINT SEALANTS

        - General:  Comply with joint sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

        - Sealant Installation Standard:  Comply with recommendations of ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

- Delete paragraph below if the only use of acoustical sealants is specified in other Sections without reference to this Section.

        - Install sealant backings of type indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

          - Do not leave gaps between ends of sealant backings.

          - Do not stretch, twist, puncture, or tear sealant backings.

          - Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

- Retain paragraph below for sealants installed in moving joints without sealant backings.

        - Install bond-breaker tape behind sealants where sealant backings are not used between sealants and back of joints.

        - Install sealants by proven techniques to comply with the following and at the same time backings are installed:

          - Place sealants so they directly contact and fully wet joint substrates.

          - Completely fill recesses provided for each joint configuration.

          - Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

        - Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

          - Remove excess sealants from surfaces adjacent to joint.

          - Use tooling agents that are approved in writing by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

- Retain one or more subparagraphs below to suit joint configurations required for Project.  First subparagraph makes concave configuration the default requirement; second and third subparagraphs, if retained, require that other configurations be indicated on Drawings.  Revise if one of the latter two configurations needs to become the default requirement.

          - Provide concave joint configuration per Figure 5A in ASTM C 1193, unless otherwise indicated.

            - Use masking tape to protect adjacent surfaces of recessed tooled joints.

        - Installation of Preformed Foam Sealants:  Install each length of sealant immediately after removing protective wrapping, taking care not to pull or stretch material, to produce seal continuity at ends, turns, and intersections of joints.  For applications at low ambient temperatures where expansion of sealant requires acceleration to produce seal, apply heat to sealant to comply with sealant manufacturer's written instructions.

      - CLEANING

        - Clean off excess sealants or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of joint sealants and of products in which joints occur.

      - PROTECTION

        - Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from the original work.

END OF SECTION 07920