SECTION 03320 - CONCRETE FLOOR TOPPING

PART 1 - GENERAL

1.01	SUMMARY

A.	Provide concrete floor topping over existing concrete slabs to repair and level floors and prepare surface for floor finishes.

1.02	SUBMITTALS

A.	Submit for approval product data, mock-ups, test reports.

1.03	QUALITY ASSURANCE

A.	Comply with governing codes and regulations. Provide products of acceptable manufacturers which have been in satisfactory use in similar service for three years. Use experienced installers. Deliver, handle, and store materials in accordance with manufacturer's instructions.

PART 2 - PRODUCTS

2.01	MATERIALS

A.	Portland-cement based topping mix with minimum compressive strength of 3,500 psi.

1.	Level-Right Self-leveling underlayment by Maxxon Corp., 0” - 3” installation depths, 5,500 psi compressive strength at 28 days.

PART 3 - EXECUTION

3.01	INSTALLATION

A.	Prepare surfaces in strict compliance with manufacturer’s instructions and recommendations.  Remove all oil and grease.  Fill cracks with crack filler or an elastomeric compound.

B.	Prime surfaces and install topping following manufacturer’s recommendations.

C.	Level surfaces to within plus 1/8” in 10’.

D.	Cure and protect.

END OF SECTION 03320