SECTION 09250 - GYPSUM BOARD

PART 1 GENERAL

1.01	SUMMARY

A.	Section Includes:

1.	Gypsum Board.

2.	Fasteners.

3.	Accessories.

1.02	QUALITY ASSURANCE

A.	Design Criteria:

1.	Fire-Resistance Rating:

a.	Where gypsum drywall systems with fire resistance ratings are indicated, provide materials and installations identical with applicable assemblies tested per ASTM E119 by fire testing laboratories acceptable to authorities having jurisdiction.

b.	Provide fire-resistance rated assemblies identical to those indicated by reference to GA File No's. in GA Fire Resistance Design Manual or to design designations in UL Fire Resistance Directory or in listing of other testing and agencies acceptable to authorities having jurisdiction.

2.	Gypsum Board Terminology Standard: GA505 by Gypsum Association.

3.	Single Source Responsibility: Obtain Gypsum board products from single manufacturer or from manufacturers recommended by the prime manufacturer of gypsum board.

1.03	SUBMITTALS

A.	Product Data: Submit manufacturer's product specifications and installation instructions for each gypsum drywall component, including other data as required to show compliance with Specifications.

1.04	PROJECT/SITE CONDITIONS

A.	Environmental Requirements:

1.	General: Comply with requirements of referenced gypsum board application standards and recommendations of gypsum board manufacturer for environmental conditions before, during, and after application of gypsum board.

2.	Cold Weather Protection: When ambient outdoor temperatures are below 55 deg. F, maintain continuous, uniform, comfortable building working temperatures min. 55 deg. F min. 48 hour period before, during, and following application of gypsum board and joint treatment materials or bonding adhesives.

3.	Ventilation:

a.	Ventilate building spaces as required to remove water in excess of that required for drying of joint treatment material immediately after application.

b.	Avoid drafts during dry, hot weather to prevent too rapid drying.

PART 2 PRODUCTS

2.01	MATERIALS

A.	Ceiling Support Materials and Systems:

1.	Furring Members:

a.	ASTM C645, min. 0.0179 in. thickness of base metal, hat-shaped.

b.	Where shown as resilient, provide manufacturer's special type designed to reduce sound transmission.

c.	Provide members at spacing recommended by manufacturer of system for indicated ceiling, including closer spacing of members as required for moisture resistant g.wb.

2.	Furring Anchorages: 16 ga. galvanized wire ties, manufacturer's standard wire type clips, bolts, nails, or screws as recommended by furring manufacturer and complying with ASTM C754.

B.	Gypsum Board:

1.	Gypsum Wallboard:

a.	ASTM C36, in maximum lengths available to minimize end-to-end butt joints.

b.	Type: Regular or Type X for fire-resistant rated assemblies and where indicated.

c.	Edges: Tapered

d.	Thickness: 5/8 in. or 1/2 in. as indicated.

2.	Water-Resistant Backing Board:

a.	ASTM C630, tapered edges, in maximum lengths available to minimize end-to-end butt joints

b.	Type: Regular or Type X for fire-resistant rated assemblies and where indicated.

c.	Thickness: 5/8 in. or 1/2 in. as indicated.

3.	Foil-backed Gypsum Wallboard:

a.	Approved equal to USG Regular Foil-Back FIRECODE gypsum panels.

b.  Per ASTM E96 (desiccant method), ½ inch foil-back panels with a vapor permeance of 0.06 perm.

4.	Glass-Mat Gypsum Sheathing Board:

a.	Product:  Subject to compliance with requirements, provide "Dens-Glass Gold" by G-P Gypsum, 5/8”, Type X, ASTM C 1177/C 1177M.

C.	Trim Accessories:

1.	General:

a.	Provide manufacturer's standard trim accessories of types indicated for drywall work, formed of galvanized steel unless otherwise indicated, with either knurled and perforated or expanded flanges for nailing or stapling, and beaded for concealment of flanges in joint compound.

b.	Provide corner beads, L-type edge trim-beads U-type edge trim-beads, special L-kerf-type edge trim-beads, and one-piece control joint beads.

D.	Screws, Adhesives, and Sealants:

1.	Screws:

a.	ASTM C1002, Grade 1013 to 1022 steel wire meeting ASTM A548.

b.	Gypsum Board to Wood Framing: Type W.

2.	Sealant: Refer to Section 07900, Joint Sealers, for materials and application.

3.	Concealed Acoustical Sealant: Non-drying, non hardening, non-skinning, non-staining, non-bleeding, gunnable sealant for concealed applications per ASTM C919.

4. Sound Attenuation Blankets: Refer to Section 07210, Insulation.

E.	Joint Treatment:

1.	General: ASTM C475; type recommended by manufacturer for application indicated, except as other wise indicated.

2.	Joint Tape: Paper reinforcing tape.

3.	Joint Compound: Ready-mixed vinyl-type for interior use.

4.	Water-Resistant Joint Compound: Special water-resistant type for treatment of joints, fastener heads, and cut edges of water-resistant backing board.

PART 3 EXECUTION

3.01	INSTALLATION

A.	Wall/Partition Support System: Install supplementary framing, runners, furring, blocking, and bracing at openings and terminations in gypsum drywall and where required for support of other work which cannot be adequately supported on gypsum board alone.

B.	Drywall Installation and Finishing:

1.	Install gypsum boards in lengths and directions which will minimize number of end joints, and avoid end joints in central area of ceilings.

2.	Install foil-backed gypsum panels with foil backing toward studs.

3.	Install walls and partitions with exposed gypsum boards vertical, with joints offset on opposite sides of partitions.

4.	Install boards with edges perpendicular to supports, with end joints staggered over supports, except where recommended in a different arrangement by manufacturer.

5.	Form control joints with 1/2 in. space between boards.

6.	Install acoustical sealant at base of space, and apply trim accessory at face.

7.	Acoustical Sealant: Where work is indicated as sound retarding or shown with STC rating, apply acoustical sealant as recommended by manufacturer.

8.	Form floating construction for gypsum boards at internal corners, except where special isolation or edge trim is indicated.

9.	Isolate drywall work from abutting structural and masonry work; provide edge trim and acoustical sealant as recommended by manufacturer.

10.	Install sound attenuation blankets where shown, without gaps; and support where necessary to prevent movement or dislocation.

11.	Screw gypsum board to metal supports.

C.	Drywall Finishing:

1.	Except as otherwise indicated, apply joint tape and joint compound at joints, both directions, between gypsum boards.

2.	Apply compound at accessory flanges, penetrations, fasteners heads and surface defects.

3.	Install compound in 3 coats plus prefill of cracks where recommended by manufacturer; sand after last 2 coats.

4.	Treat joints, fastener heads, cut edges and penetrations in water-resistant backing board using water-resistant joint compound to comply with water-resistant joint compound manufacturer's directions.

END OF SECTION 09250