SECTION 09950 - WALLCOVERINGS

PART 1 GENERAL

1.01	SUMMARY

A.	Section Includes:

1.	Vinyl.

2.	Accessories.

1.02	DESIGN CRITERIA

A.	Fire Hazard Classification: Provide materials bearing UL label for following:

1.	Flame Spread: Max. 25.

2.	Fuel Contributed: Max. 15.

3.	Smoke Developed: Max. 25.

1.03	SUBMITTALS

A.	Samples: 3 full width samples of each type of wall covering; 3 sets of sample moldings.

B.	Replacement Materials: 6 lin. yds. each type, color, and pattern wallcovering installed.

C.	Certification: Submit manufacturer's certification that materials supplied comply with specified requirements.

1.04	PROJECT/SITE CONDITIONS

A.	Environmental Requirements:

1.	Maintain constant min. temperature of 60 deg. F at areas of installation for min. 72 hours before and 48 hours after installation.

2.	Remove wrappings from wallcoverings and allow to acclimatize to areas of installation for min. 24 hours before installation.

PART 2 PRODUCTS

2.01	MATERIALS

A.	Vinyl Wallcovering:

1.	General: Comply with requirements of FS CCC-W-408

2.	Medium Duty: Type II, min. 13 oz./sq. yd.

3.	Stain Resistant: Type II, 1/2 mil polyvinylfluoride film (Tedlar) by DuPont

4.	Mildew Resistance: Fabric backing and vinyl coating treated with fungicides to inhibit mildew growth.

5.	Color/Pattern/Texture: As selected.

6.	Product: As indicated in the Room Finish Schedule and Finish Specifications.

B.	Accessory Items:

1.	Adhesive/Primer/Sealer: As recommended by manufacturer of wallcovering for use with particular substrate shown; mildew-resistant, non-staining to wallcovering. Strippable.

2.	Release Coat: Oil bass sealer or enamel undercoater for drywall.

PART 3 EXECUTION

3.01	PREPARATION

A.	Remove wall plates and surface-mounted fixtures in areas where wallcovering to be installed.

B.	Prime and seal substrates in accordance with wallcovering manufacturer's instructions; apply release coat to gypsum drywall.

C.	Test substrates for moisture; verify max. 4 percent.

3.02	INSTALLATION

A.	Place wallcovering panels consecutively in order cut from rolls; hang by reversing alternate strips except on match patterns.

B.	Apply adhesive in accordance with manufacturer's recommendations; install seams plumb, min. 6 in. from corners; horizontal seams not permitted.

C.	Trim selvages as required to assure color uniformity and pattern match; overlap seams and double-cut for tight closure, unless otherwise recommended by manufacturer.

D.	Install wallcovering with intimate substrate bond, smooth, clean, and without wrinkles, gaps, and overlaps.

E.	Remove excess adhesive promptly, using clean sponge and warm water; replace panels which cannot be completely cleaned.

F.	Replace wall plates and fixtures removed to permit wallcovering installation; verify cut edges of wallcovering completely concealed.

END OF SECTION 09950