Copyright 2006 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 079200 - JOINT SEALANTS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Silicone joint sealants.

          - Latex joint sealants.

        - Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Division 09 Section "Gypsum Board" for sealing perimeter joints.

          - Division 09 Section "Acoustical Panel Ceilings" for sealing edge moldings at perimeters with acoustical sealant.

Preconstruction compatibility and adhesion testing in first paragraph below is performed off-site by sealant manufacturer.  Tests require many Samples, and some tests require four weeks to complete.  If retaining, also retain "Preconstruction Compatibility and Adhesion Test Reports" Paragraph in "Submittals" Article.

Testing in paragraph below is performed on-site, either on field-constructed mock-ups or on actual construction, but far enough in advance of sealant work to allow curing of sealants and retesting if necessary.  If retaining, also retain "Preconstruction Field-Adhesion Test Reports" Paragraph in "Submittals" Article.

      - SUBMITTALS

First five paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

        - Product Data:  For each joint-sealant product indicated.

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for interior sealants and primers.

          - For sealants and sealant primers used inside the weatherproofing system, including printed statement of VOC content.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

        - Samples:  For each kind and color of joint sealant required, provide Samples with joint sealants in 1/2-inch-wide joints formed between two 6-inch-long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

        - Joint-Sealant Schedule:  Include the following information:

          - Joint-sealant application, joint location, and designation.

          - Joint-sealant manufacturer and product name.

          - Joint-sealant formulation.

          - Joint-sealant color.

Remaining paragraphs are defined in Division 01 Section "Submittal Procedures" as "Informational Submittals."

Coordinate first paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

        - Qualification Data:  For qualified Installer and testing agency.

Retain first paragraph below for product certificates from manufacturers.

        - Product Certificates:  For each kind of joint sealant and accessory, from manufacturer.

Retain first paragraph below if retaining subparagraph requiring testing to obtain SWRI validation in "Quality Assurance" Article.

        - Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, indicating that sealants comply with requirements.

Correlate test reports in first two paragraphs below with testing requirements in "Preconstruction Testing" Article.

Correlate test reports in first paragraph below with testing requirements in "Field Quality Control" Article.

      - QUALITY ASSURANCE

        - Installer Qualifications:  Manufacturer's authorized representative who is trained and approved for installation of units required for this Project.

        - Source Limitations:  Obtain each kind of joint sealant from single source from single manufacturer.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

        - Preinstallation Conference:  Conduct conference at Project site.

      - PROJECT CONDITIONS

        - Do not proceed with installation of joint sealants under the following conditions:

          - When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer.

          - When joint substrates are wet.

          - Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

          - Where contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

- PRODUCTS

      - MATERIALS, GENERAL

        - Compatibility:  Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint-sealant manufacturer, based on testing and field experience.

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.  Coordinate product selection in other Part 2 articles to be sure that products selected comply.

        - VOC Content of Interior Sealants:  Provide sealants and sealant primers for use inside the weatherproofing system that comply with the following limits for VOC content when calculated according to 40 CFR 59, Part 59, Subpart D (EPA Method 24):

          - Architectural Sealants:  250 g/L.

          - Sealant Primers for Nonporous Substrates:  250 g/L.

          - Sealant Primers for Porous Substrates:  775 g/L.

Generally retain first paragraph below with silicones applied to porous substrates such as marble, limestone, granite, and sandstone.

        - Stain-Test-Response Characteristics:  Where sealants are specified to be nonstaining to porous substrates, provide products that have undergone testing according to ASTM C 1248 and have not stained porous joint substrates indicated for Project.

Retain first paragraph below for applications where sealants will come in contact with food.  Indicate on Drawings or by inserts which products must comply with this requirement.

        - Suitability for Contact with Food:  Where sealants are indicated for joints that will come in repeated contact with food, provide products that comply with 21 CFR 177.2600.

Retain paragraph below if sealant colors are not specified in the Joint-Sealant Schedule in Part 3 or on Drawings.

        - Colors of Exposed Joint Sealants:  As selected by Contracting Officer from manufacturer's full range.

      - SILICONE JOINT SEALANTS

Coordinate paragraphs in this article with Joint-Sealant Schedule in Part 3.

        - Mildew-Resistant, Single-Component, Nonsag, Neutral-Curing Silicone Joint Sealant:  ASTM C 920, Type S, Grade NS, Class 25, for Use NT.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

          - Products:  Subject to compliance with requirements, provide the following:

            - Pecora Corporation; 898.

      - LATEX JOINT SEALANTS

Coordinate paragraph in this article with Joint-Sealant Schedule in Part 3.

In addition to Type OP (for opaque sealants containing color or extended pigments) in paragraph below, ASTM C 834 includes Type C (for clear or translucent sealants).  Also, in addition to Grade NF (not tested for low temperature flexibility) in paragraph below, ASTM C 834 includes Grades -18 deg C and 0 deg C (for sealants that meet requirements for flexibility at minus 18 deg C and 0 deg C, respectively).

        - Latex Joint Sealant:  Acrylic latex or siliconized acrylic latex, ASTM C 834, Type OP, Grade NF.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

          - Products:  Subject to compliance with requirements, provide the following:

            - BASF Building Systems; Sonolac.

            - Bostik, Inc.; Chem-Calk 600.

            - Pecora Corporation; AC-20+.

            - Tremco Incorporated; Tremflex 834.

      - JOINT SEALANT BACKING

        - General:  Provide sealant backings of material that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

        - Cylindrical Sealant Backings:  ASTM C 1330, Type C (closed-cell material with a surface skin), Type O (open-cell material), Type B (bicellular material with a surface skin) or any of the preceding types, as approved in writing by joint-sealant manufacturer for joint application indicated, and of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance.

Retain one of three type options in first paragraph below; if retaining more than one, also retain fourth option.  Type B products include "Sof Rod" by Nomaco and "Sonolastic Soft Backer Rod" by BASF Building Systems.  Verify with joint-sealant manufacturers the suitability of each material for sealants selected.  Type O sealant backings, which are open-cell urethane foams, are unsuitable for horizontal surfaces.  See Evaluations.

        - Bond-Breaker Tape:  Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint.  Provide self-adhesive tape where applicable.

      - MISCELLANEOUS MATERIALS

Retain first paragraph below if joint priming is retained in Part 3.

        - Masking Tape:  Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

- EXECUTION

      - EXAMINATION

        - Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Surface Cleaning of Joints:  Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions and the following requirements:

          - Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, paints (except for permanent, protective coatings tested and approved for sealant adhesion and compatibility by sealant manufacturer), old joint sealants, oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

          - Clean nonporous joint substrate surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues capable of interfering with adhesion of joint sealants.  Nonporous joint substrates include the following:

Retain nonporous substrates in subparagraphs below if applicable.  Insert additional items to suit Project.

            - Metal.

            - Glass.

        - Joint Priming:  Prime joint substrates where recommended by joint-sealant manufacturer or as indicated by preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint-sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

        - Masking Tape:  Use masking tape where required to prevent contact of sealant or primer with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears.  Remove tape immediately after tooling without disturbing joint seal.

      - INSTALLATION OF JOINT SEALANTS

        - General:  Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

        - Sealant Installation Standard:  Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

        - Install sealant backings of kind indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

          - Do not leave gaps between ends of sealant backings.

          - Do not stretch, twist, puncture, or tear sealant backings.

          - Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

Retain first paragraph below for sealants installed in moving joints without sealant backings.

        - Install sealants using proven techniques that comply with the following and at the same time backings are installed:

          - Place sealants so they directly contact and fully wet joint substrates.

          - Completely fill recesses in each joint configuration.

          - Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

        - Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified in subparagraphs below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

          - Remove excess sealant from surfaces adjacent to joints.

          - Use tooling agents that are approved in writing by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

Retain one or more of three subparagraphs below to suit joint configurations required for Project.  First subparagraph makes concave configuration the default requirement; second and third subparagraphs require that other configurations be indicated on Drawings.  Revise if one of the latter two configurations is the default requirement.

          - Provide concave joint profile per Figure 8A in ASTM C 1193, unless otherwise indicated.

            - Use masking tape to protect surfaces adjacent to recessed tooled joints.

Retain first paragraph below if preformed silicone sealants are retained in Part 2.

Retain first paragraph below if preformed foam sealants are retained in Part 2.

Retain first paragraph below if acoustical sealants are retained in Part 2.

      - CLEANING

        - Clean off excess sealant or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of joint sealants and of products in which joints occur.

      - PROTECTION

        - Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from original work.

      - JOINT-SEALANT SCHEDULE

Joint-sealant applications in this Article represent only a limited number of examples; modify to suit Project.  For projects with more than one kind or color of sealant for joint locations listed, copy paragraph and create an additional set of requirements and products for each variation.

For each sealant scheduled, retain corresponding product requirements in Part 2 that reference sealant standards, specify product properties and, if required, name manufacturers and products.

If designations are retained in "Joint-Sealant Application" paragraphs below, insert number to complete designation.  Coordinate with designations used on Drawings.

        - Joint-Sealant Application:  Interior joints in vertical surfaces and horizontal nontraffic surfaces.

          - Joint Locations:

            - Vertical joints on exposed surfaces of walls and partitions.

            - Perimeter joints between interior wall surfaces and frames of interior doors and windows.

            - Other joints as required.

          - Joint Sealant:  Latex.

          - Joint-Sealant Color:  As selected by Contracting Officer from manufacturer's full range of colors.

        - Joint-Sealant Application:  Mildew-resistant interior joints in vertical surfaces and horizontal nontraffic surfaces.

          - Joint Sealant Location:

            - Joints between plumbing fixtures and adjoining walls, floors, and counters.

            - Other joints as required.

          - Joint Sealant:  Mildew resistant, single component, nonsag, neutral curing, Silicone.

          - Joint-Sealant Color:  As selected by Contracting Officer from manufacturer's full range of colors.

END OF SECTION 079200