Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 081113 – HOLLOW METAL DOORS AND FRAMES

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

Retain first subparagraph below for standard hollow metal doors and frames that are fabricated according to ANSI/SDI A250.8; retain second subparagraph for custom hollow metal doors and frames that are fabricated according to ANSI/NAAMM-HMMA 861.  See Evaluations for discussion of differences between standard and custom hollow metal work.

          - Standard hollow metal doors and frames.

        - Related Sections

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Division 8 Section "Door Hardware" for door hardware for hollow metal doors.

          - Division 9 Sections "Interior Painting" for field painting hollow metal doors and frames.

      - DEFINITIONS

Retain definitions remaining after this Section has been edited.

Retain first paragraph below to indicate that metal thicknesses specified are base-metal measurements and do not include metallic coatings or finishes.  Thicknesses indicated in this Section are expressed in decimals and are according to ANSI/SDI A250.8 and ANSI/NAAMM-HMMA 861, both of which use the same values for minimum steel sheet thicknesses.  See Evaluations for discussion.

        - Minimum Thickness:  Minimum thickness of base metal without coatings.

Retain one of two paragraphs below; retain both if both standard and custom hollow metal work are specified.

        - Standard Hollow Metal Work:  Hollow metal work fabricated according to ANSI/SDI A250.8.

        - Custom Hollow Metal Work:  Hollow metal work fabricated according to ANSI/NAAMM-HMMA 861.

      - SUBMITTALS

First five paragraphs below are defined in Division 1 Section "Submittal Procedures" as "Action Submittals."

        - Product Data:  For each type of product indicated.  Include construction details, material descriptions, core descriptions, fire-resistance rating, and finishes.

Retain first paragraph below for standard or custom hollow metal work.  ANSI/SDI A250.8 indicates that manufacturer's published details can replace Shop Drawings for standard hollow metal work unless otherwise specified.

        - Shop Drawings:  Include the following:

          - Elevations of each door design.

          - Details of doors, including vertical and horizontal edge details and metal thickness.

          - Frame details for each frame type, including dimensioned profiles and metal thicknesses.

          - Locations of reinforcement and preparations for hardware.

          - Details of each different wall opening condition.

          - Details of anchorages, joints, field splices, and connections.

          - Details of conduit and preparations for power, signal, and control systems.

        - Other Action Submittals:

          - Schedule:  Provide a schedule of hollow metal work prepared by or under the supervision of supplier, using same reference numbers for details and openings as those on Drawings.  Coordinate with door hardware schedule.

Remaining paragraphs are defined in Division 1 Section "Submittal Procedures" as "Informational Submittals."

Retain first paragraph below for oversized fire-rated assemblies.

Retain paragraph below for fire-rated assemblies.

      - QUALITY ASSURANCE

        - Source Limitations:  Obtain hollow metal work from single source from single manufacturer.

Retain first paragraph below if applicable.  Do not retain both UL 10B and UL 10C.  UL 10B is a neutral-pressure test; UL 10C is a positive-pressure test.  NFPA 252 contains two choices for test pressure: "positive pressure" and "as close to neutral pressure as possible."  UBC Standard 7-2 requires testing at positive pressure for "side-hinged or pivoted swinging doors" and at "as nearly equal to the atmosphere's pressure as possible" for "other types of doors, including swinging elevator doors."

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver hollow metal work palletized, wrapped, or crated to provide protection during transit and Project-site storage.  Do not use nonvented plastic.

          - Provide additional protection to prevent damage to finish of factory-finished units.

Retain first paragraph below for welded frames.  Temporary spreader bars are intended for shipping and handling purposes only.

        - Deliver welded frames with two removable spreader bars across bottom of frames, tack welded to jambs.

        - Store hollow metal work under cover at Project site.  Place in stacks of five units maximum in a vertical position with heads up, spaced by blocking, on minimum 4-inch- (102-mm-) high wood blocking.  Do not store in a manner that traps excess humidity.

          - Provide minimum 1/4-inch (6-mm) space between each stacked door to permit air circulation.

      - PROJECT CONDITIONS

        - Field Measurements:  Verify actual dimensions of openings by field measurements before fabrication.

      - COORDINATION

        - Coordinate installation of anchorages for hollow metal frames.  Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors.  Deliver such items to Project site in time for installation.

- PRODUCTS

      - MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  See Division 1 Section "Product Requirements."

        - Manufacturers:  Subject to compliance with requirements, available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Manufacturers listed below produce either standard or custom hollow metal work unless otherwise indicated.  Verify specific capabilities with individual manufacturers.

          - Amweld Building Products, LLC.

          - Ceco Door Products; an Assa Abloy Group company.

          - Fleming Door Products Ltd.; an Assa Abloy Group company.

Manufacturer listed in first subparagraph below produces only custom hollow metal work.

          - Kewanee Corporation (The).

          - Pioneer Industries, Inc.

          - Steelcraft; an Ingersoll-Rand company.

      - MATERIALS

        - Cold-Rolled Steel Sheet:  ASTM A 1008/A 1008M, Commercial Steel (CS), Type B; suitable for exposed applications.

Retain first paragraph below, which describes electrolytic zinc-coated steel, for frame anchors only.

        - Frame Anchors:  ASTM A 591/A 591M, Commercial Steel (CS), 40Z (12G) coating designation; mill phosphatized.

          - For anchors built into exterior walls, steel sheet complying with ASTM A 1008/A 1008M or ASTM A 1011/A 1011M, hot-dip galvanized according to ASTM A 153/A 153M, Class B.

        - Inserts, Bolts, and Fasteners:  Hot-dip galvanized according to ASTM A 153/A 153M.

Retain first paragraph below if powder-actuated fasteners are allowed.

Retain first paragraph below for grouted frames.  ANSI A250.11 and ANSI/NAAMM-HMMA 861 both recommend that grout for hollow metal frames have a maximum 4-inch (102-mm) slump.  See Evaluations for discussion.

        - Mineral-Fiber Insulation:  ASTM C 665, Type I (blankets without membrane facing); consisting of fibers manufactured from slag or rock wool with 6- to 12-lb/cu. ft. (96- to 192-kg/cu. m) density; with maximum flame-spread and smoke-development indexes of 25 and 50, respectively; passing ASTM E 136 for combustion characteristics.

      - STANDARD HOLLOW METAL DOORS

        - General: Provide doors of design indicated, not less than thickness indicated; fabricated with smooth surfaces, without visible joints or seams on exposed faces unless otherwise indicated. Comply with ANSI/SDI A250.8.

        - Interior Doors: Face sheets fabricated from cold-rolled steel sheet. Provide doors complying with requirements indicated below by referencing ANSI/SDI A250.8 for level and model and ANSI/SDI A250.4 for physical performance level:

          - Level 1 and Physical Performance Level C (Standard Duty), Model 1 (Full Flush).

            - Width: As indicated on Drawings.

        - Hardware Reinforcement: Fabricate according to ANSI/SDI A250.6 with reinforcing plates from same material as door face sheets.

        - Fabricate concealed stiffeners and hardware reinforcement from either cold- or hot-rolled steel sheet.

      - STANDARD HOLLOW METAL FRAMES

Retain this article for door, sidelight, transom, and borrowed-light frames fabricated to ANSI/SDI A250.8 requirements for standard hollow metal work.  Do not specify standard hollow metal frames for custom hollow metal doors or hardware coordination problems may result.  See Evaluations for discussion.

        - General:  Comply with ANSI/SDI A250.8 and with details indicated for type and profile.

        - Interior Frames:  Fabricated from cold-rolled steel sheet.

          - Fabricate frames with mitered or coped corners.

Retain one of three options in first subparagraph below.  According to ANSI/SDI A250.8, frames are supplied as knocked down unless otherwise indicated.  Face-welded frames are welded only along the face and not along the soffit, stops, and rabbets.  Fully welded frames are completely welded along all elements.

          - Fabricate frames as welded in place, unless otherwise indicated.

Retain first subparagraph below for gypsum board partitions.

          - Frames for Wood Doors:  (1.0-mm-)(1.3-mm-)16 GA.

        - Hardware Reinforcement:  Fabricate according to ANSI/SDI A250.6 with reinforcement plates from same material as frames.

      - FRAME ANCHORS

        - Jamb Anchors:

Retain types in four subparagraphs below to suit Project.

Wire anchors in first subparagraph below are often used to permit unobstructed grouting of frames.

          - Stud-Wall Type:  Designed to engage stud, welded to back of frames; not less than 0.042 inch (1.0 mm) thick.

        - Floor Anchors:  Formed from same material as frames, not less than 0.042 inch (1.0 mm) thick, and as follows:

          - Monolithic Concrete Slabs:  Clip-type anchors, with two holes to receive fasteners not less than 2-inch (50-mm) height adjustment.  Terminate bottom of frames at finish floor surface.

      - ACCESSORIES

Retain paragraphs in this article to suit Project; revise if necessary.

        - Ceiling Struts:  Minimum 1/4-inch-thick by 1-inch- (6.4-mm-thick by 25.4-mm-) wide steel.

      - FABRICATION

        - Fabricate hollow metal work to be rigid and free of defects, warp, or buckle.  Accurately form metal to required sizes and profiles, with minimum radius for thickness of metal.  Where practical, fit and assemble units in manufacturer's plant.  To ensure proper assembly at Project site, clearly identify work that cannot be permanently factory assembled before shipment.

Retain first option in first paragraph below for standard hollow metal work.  Retain second option for custom hollow metal work.

        - Tolerances:  Fabricate hollow metal work to tolerances indicated in ANSI/NAAMM-HMMA 861.

        - Hollow Metal Doors:

          - Steel-Stiffened Door Cores: Provide minimum thickness 0.026 inch, steel vertical stiffeners of same material as face sheets extending full-door height, with vertical webs spaced not more than 6 inches apart. Spot weld to face sheets no more than 5 inches o.c. Fill spaces between stiffeners with glass- or mineral-fiber insulation.

          - Fire Door Cores: As required to provide fire-protection ratings indicated.

          - Vertical Edges for Single-Acting Doors: Provide beveled or square edges at manufacturer’s discretion.

          - Top Edge Closures: Close top edges of doors with inverted closures of same material as face sheets.

          - Bottom Edge Closures: Close bottom edges of doors where required for attachment of weather stripping with end closures or channels of same material as face sheets.

        - Hollow Metal Frames:  Where frames are fabricated in sections due to shipping or handling limitations, provide alignment plates or angles at each joint, fabricated of same thickness metal as frames.

          - Welded Frames:  Weld flush face joints continuously; grind, fill, dress, and make smooth, flush, and invisible.

          - Provide countersunk, flat- or oval-head exposed screws and bolts for exposed fasteners unless otherwise indicated.

          - Floor Anchors:  Weld anchors to bottom of jambs and mullions with at least four spot welds per anchor.

          - Jamb Anchors:  Provide number and spacing of anchors as follows:

Fire ratings may require additional anchors.

            - Stud-Wall Type:  Locate anchors not more than 18 inches (457 mm) from top and bottom of frame.  Space anchors not more than 32 inches (813 mm) o.c. and as follows:

              - Three anchors per jamb up to 60 inches (1524 mm) high.

              - Four anchors per jamb from 60 to 90 inches (1524 to 2286 mm) high.

              - Five anchors per jamb from 90 to 96 inches (2286 to 2438 mm) high.

              - Five anchors per jamb plus 1 additional anchor per jamb for each 24 inches (610 mm) or fraction thereof above 96 inches (2438 mm) high.

              - Two anchors per head for frames above 42 inches (1066 mm) wide and mounted in metal-stud partitions.

          - Door Silencers:  Drill stops to receive door silencers as follows.  Keep holes clear during construction.

            - Single-Door Frames:  Drill stop in strike jamb to receive three door silencers.

        - Fabricate concealed stiffeners, edge channels, and hardware reinforcement from either cold- or hot-rolled steel sheet.

        - Hardware Preparation:  Factory prepare hollow metal work to receive templated mortised hardware; include cutouts, reinforcement, mortising, drilling, and tapping according to the Door Hardware Schedule and templates furnished as specified in Division 8 Section "Door Hardware."

Retain first option in first subparagraph below for standard hollow metal work.  Retain second option for custom hollow metal work.

          - Locate hardware as indicated, or if not indicated, according to ANSI/SDI A250.8.

          - Reinforce frames to receive nontemplated, mortised and surface-mounted door hardware.

          - Comply with applicable requirements in ANSI/SDI A250.6 and ANSI/DHI A115 Series specifications for preparation of hollow metal work for hardware.

          - Coordinate locations of conduit and wiring boxes for electrical connections with Division 16 Sections.

      - STEEL FINISHES

Retain one of two paragraphs in this article.  According to some manufacturers, galvannealed steel does not require prime painting.

        - Prime Finish:  Apply manufacturer's standard primer immediately after cleaning and pretreating.

          - Shop Primer:  Manufacturer's standard, fast-curing, lead- and chromate-free primer complying with ANSI/SDI A250.10 acceptance criteria; recommended by primer manufacturer for substrate; compatible with substrate and field-applied coatings despite prolonged exposure.

Factory-applied finishes are not covered by ANSI/NAAMM-HMMA 861.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

        - Examine roughing-in for embedded and built-in anchors to verify actual locations before frame installation.

Retain first paragraph below if required.

        - For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

Retain first two paragraphs below for installation of welded frames.

        - Remove welded-in shipping spreaders installed at factory.  Restore exposed finish by grinding, filling, and dressing, as required to make repaired area smooth, flush, and invisible on exposed faces.

Tolerances in first paragraph below are required by ANSI/NAAMM-HMMA 861.

        - Prior to installation, adjust and securely brace welded hollow metal frames for squareness, alignment, twist, and plumbness to the following tolerances:

          - Squareness:  Plus or minus 1/16 inch (1.6 mm), measured at door rabbet on a line 90 degrees from jamb perpendicular to frame head.

          - Alignment:  Plus or minus 1/16 inch (1.6 mm), measured at jambs on a horizontal line parallel to plane of wall.

          - Twist:  Plus or minus 1/16 inch (1.6 mm), measured at opposite face corners of jambs on parallel lines, and perpendicular to plane of wall.

          - Plumbness:  Plus or minus 1/16 inch (1.6 mm), measured at jambs on a perpendicular line from head to floor.

        - Drill and tap frames to receive nontemplated, mortised, and surface-mounted door hardware.

      - INSTALLATION

        - General:  Install hollow metal work plumb, rigid, properly aligned, and securely fastened in place; comply with Drawings and manufacturer's written instructions.

Retain first option in first paragraph below for installation of standard hollow metal frames.  Retain second option for installation of custom hollow metal frames.

        - Hollow Metal Frames:  Install hollow metal frames of size and profile indicated.  Comply with ANSI/SDI A250.11.

          - Set frames accurately in position, plumbed, aligned, and braced securely until permanent anchors are set.  After wall construction is complete, remove temporary braces, leaving surfaces smooth and undamaged.

Retain any of first seven subparagraphs below to suit Project.

            - Where frames are fabricated in sections because of shipping or handling limitations, field splice at approved locations by welding face joint continuously; grind, fill, dress, and make splice smooth, flush, and invisible on exposed faces.

            - Install door silencers in frames before grouting.

            - Remove temporary braces necessary for installation only after frames have been properly set and secured.

            - Check plumbness, squareness, and twist of frames as walls are constructed.  Shim as necessary to comply with installation tolerances.

          - Floor Anchors:  Provide floor anchors for each jamb and mullion that extends to floor, and secure with postinstalled expansion anchors.

Retain first subparagraph below if permitted.

            - Floor anchors may be set with powder-actuated fasteners instead of postinstalled expansion anchors if so indicated and approved on Shop Drawings.

          - Metal-Stud Partitions:  Solidly pack mineral-fiber insulation behind frames.

Retain one or both of first two subparagraphs below if grouted frames are required.  See Evaluations for discussion.

          - In-Place Gypsum Board Partitions:  Secure frames in place with postinstalled expansion anchors through floor anchors at each jamb.  Countersink anchors, and fill and make smooth, flush, and invisible on exposed faces.

          - Ceiling Struts:  Extend struts vertically from top of frame at each jamb to overhead structural supports or substrates above frame unless frame is anchored to masonry or to other structural support at each jamb.  Bend top of struts to provide flush contact for securing to supporting construction.  Provide adjustable wedged or bolted anchorage to frame jamb members.

          - Installation Tolerances:  Adjust hollow metal door frames for squareness, alignment, twist, and plumb to the following tolerances:

            - Squareness:  Plus or minus 1/16 inch (1.6 mm), measured at door rabbet on a line 90 degrees from jamb perpendicular to frame head.

            - Alignment:  Plus or minus 1/16 inch (1.6 mm), measured at jambs on a horizontal line parallel to plane of wall.

            - Twist:  Plus or minus 1/16 inch (1.6 mm), measured at opposite face corners of jambs on parallel lines, and perpendicular to plane of wall.

            - Plumbness:  Plus or minus 1/16 inch (1.6 mm), measured at jambs at floor.

        - Hollow Metal Doors: Fit hollow metal doors accurately in frames, within clearances specified below. Shim as necessary.

          - Non-Fire Rated Standard Steel Doors:

            - Jambs and Heads: 1/8 inch plus or minus 1/16 inch.

            - Between Edges of Pairs of Doors: 1/8 inch plus or minus 1/16 inch.

            - Between Bottom of Door and Top of Threshold: Maximum 3/8 inch.

            - Between Bottom of Door and Top of Finish Floor (No Threshold): Maximum ¾ inch.

          - Fire-Rated Doors: Install doors with clearances according to NFPA 80.

      - ADJUSTING AND CLEANING

        - Final Adjustments:  Check and readjust operating hardware items immediately before final inspection.  Leave work in complete and proper operating condition.  Remove and replace defective work, including hollow metal work that is warped, bowed, or otherwise unacceptable.

Retain one of two paragraphs below.

        - Prime-Coat Touchup:  Immediately after erection, sand smooth rusted or damaged areas of prime coat and apply touchup of compatible air-drying, rust-inhibitive primer.

        - Metallic-Coated Surfaces:  Clean abraded areas and repair with galvanizing repair paint according to manufacturer's written instructions.

END OF SECTION 08113