Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 081416 - FLUSH WOOD DOORS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Solid-core doors.

          - Factory finishing flush wood doors.

        - Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain one of first two options in first subparagraph below, depending on which Section is used to specify wood door frames if used.  Fire-rated and non-fire-rated wood door frames are specified in both Sections.

          - Division 8 Section "Door Hardware”.

          - Division 8 Section “Hollow Metal Doors and Frames.”

      - SUBMITTALS

        - Product Data:  For each type of door indicated.  Include details of core and edge construction and trim for openings.  Include factory-finishing specifications.

        - Shop Drawings:  Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data; location and extent of hardware blocking; and other pertinent data.

          - Indicate dimensions and locations of mortises and holes for hardware.

          - Indicate dimensions and locations of cutouts.

          - Indicate requirements for veneer matching.

          - Indicate doors to be factory finished and finish requirements.

          - Indicate fire-protection ratings for fire-rated doors.

        - Samples:

          - Corner sections of doors, approximately 8 by 10 inches (200 by 250 mm), with door faces and edges representing actual materials to be used.

            - Provide samples for each species of veneer and solid lumber required.

            - Finish veneer-faced door samples with same materials proposed for factory-finished doors.

        - Warranty:  Sample of special warranty.

      - QUALITY ASSURANCE

Retain first paragraph below if required for LEED-NC or LEED-CI Credit MR 7.  Before retaining, verify that manufacturers selected comply.  Note that USGBC will allow credit for the full value of the door as certified wood if the door manufacturer is listed for chain-of-custody certification and at least 70 percent of wood materials in the door are from certified forests; otherwise, it only allows credit for the value of certified wood materials used in making the door.

        - Manufacturer Qualifications:  A qualified manufacturer that is certified for chain of custody by an FSC-accredited certification body.

Revise first paragraph below or insert exceptions where types of doors specified are not available from a single manufacturer.

        - Source Limitations:  Obtain flush wood doors from single manufacturer.

Retain one standard in first paragraph below.  Verify applicability of selected standard for Project's geographic location.  Review selected standard and coordinate its requirements with selected options.  See Evaluations.

        - Quality Standard:  In addition to requirements specified, comply with AWI's "Architectural Woodwork Quality Standards Illustrated."

Retain first subparagraph below if AWI standard is referenced in paragraph above.  Retain second and third subparagraphs if WI standard is referenced in paragraph above.

Retain first paragraph below if wood products are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  Before retaining, verify availability of required door types made from certified wood products.  See Evaluations.  An alternative method of meeting Credit MR 7 requirement is to retain requirement in Division 1 Section "LEED Requirements" that gives Contractor option and responsibility for determining how Credit MR 7 requirement will be met.

        - Forest Certification:  Provide doors made with all wood products obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Retain first paragraph below and one of first two options, together with one or more of last five options, if fire-rated doors are required.

Retain first subparagraph below if applicable and acceptable to authorities having jurisdiction.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with requirements of referenced standard and manufacturer's written instructions.

Retain first paragraph below for factory-finished doors and high-quality unfinished doors.  Second option is standard with some manufacturers, extra with others.

        - Package doors individually in cardboard cartons and wrap bundles of doors in plastic sheeting.

        - Mark each door on bottom rail with opening number used on Shop Drawings.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Do not deliver or install doors until spaces are enclosed and weathertight, wet work in spaces is complete and dry, and HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

Generally retain paragraph above; retain paragraph below if humidity will be controlled during occupancy.  If retaining below, retain one of three relative humidity ranges or insert another based on local climatological data.  First option applies to Ontario, Quebec, and most of U.S.  Second applies to damp coastal areas of southern U.S. and the Maritime Provinces.  Third applies to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan.  See map and discussion about relative humidity and moisture content in AWI's quality standards.

      - WARRANTY

See Evaluations for door warranties.

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace doors that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Warping (bow, cup, or twist) more than 1/4 inch (6.4 mm) in a 42-by-84-inch (1067-by-2134-mm) section.

            - Telegraphing of core construction in face veneers exceeding 0.01 inch in a 3-inch (0.25 mm in a 76.2-mm) span.

Requirements in first subparagraph below are not standard with many manufacturers and could be an added cost if retained.

          - Warranty shall also include installation and finishing that may be required due to repair or replacement of defective doors.

Warranties for exterior doors vary from no warranty to a warranty for a period of up to five years.  Before retaining first subparagraph below, verify availability of warranty period with manufacturers selected; delete if retaining manufacturers that offer no warranty.  Standard manufacturer's warranty generally goes into effect on date of shipment, not date of Substantial Completion.

First subparagraph below is typical; revise if required.

          - Warranty Period for Solid-Core Interior Doors:  Life of installation.

Warranties for hollow-core doors vary with manufacturer and type of hollow core.  Before retaining subparagraph below, verify availability of warranty period with manufacturers selected.  Standard manufacturer's warranties generally go into effect on date of shipment, not date of Substantial Completion.

- PRODUCTS

      - MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain paragraph and list of manufacturers in this article.  See Division 1 Section "Product Requirements."

        - Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

Manufacturers listed are representative only; many others make flush wood doors.  See WDMA's and AWI's Web sites for listings of door manufacturers.  Retain only manufacturers offering doors complying with requirements selected for each type used, and add other manufacturers offering suitable products.  See Evaluations and manufacturers' catalogs.

          - Algoma Hardwoods, Inc.

          - Ampco, Inc.

          - Eagle Plywood & Door Manufacturing, Inc.

          - Marlite.

          - Marshfield Door Systems, Inc.

          - Mohawk Flush Doors, Inc.; a Masonite company.

      - DOOR CONSTRUCTION, GENERAL

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.  Before retaining, verify availability with manufacturers selected.

        - Low-Emitting Materials:  Provide doors made with adhesives and composite wood products that do not contain urea formaldehyde.

Retain one of first two paragraphs below to specify performance grade if WDMA I.S.1-A is referenced, or delete both paragraphs and specify performance grades for each door type in "Veneer-Faced Doors for Transparent Finish," "Doors for Opaque Finish," and "Plastic-Laminate-Faced Doors" articles.  See Evaluations.

        - WDMA I.S.1-A Performance Grade:  Extra Heavy Duty.

Retain first paragraph below if doors have particleboard cores.

        - Interior Solid-Core Doors:

Grade AA faces are required for AWI and WI Premium grade doors; Grade A faces are required for WDMA I.S.1-A Premium grade doors.  See Evaluations.  WDMA and WI have no Economy grade for doors.

          - Grade:  Architectural, with Grade AA faces.

Options in first subparagraph below are examples only; revise or insert another species.  Last two options are examples of tropical species available as FSC-certified veneers (available from ForestWorld Group).

          - Species:  Red Oak.

Option for rift cut in first subparagraph below applies only to oak.

          - Cut:  To match existing doors.

Pleasing match in first subparagraph below is available only for Economy grade doors (Grade B faces).  See Evaluations.

          - Match between Veneer Leaves:  Pleasing match.

Center-balance match in first subparagraph below is expensive and is not standard with any grade of door.  Balance match is required for AWI and WI Premium grade doors.  Running match is standard for Custom grade and WDMA Premium grade doors.  See Evaluations.

          - Assembly of Veneer Leaves on Door Faces:  Running match.

          - Room Match:  Match door faces within each separate room or area of building.  Corridor-door faces do not need to match where they are separated by 20 feet (6 m) or more.

Retain subparagraph above or first subparagraph below only for highest quality work with Premium grade doors.  Below is based on requirement for WI Premium grade doors.

          - Room Match:  Provide door faces of compatible color and grain within each separate room or area of building.

Before retaining first subparagraph below, verify availability of veneers for selected matching; usually retainfirst option.  See referenced standards.

          - Transom Match:  Continuous match.

Retain first option in first subparagraph below if top edges of doors will be visible, such as doors in multistory spaces.  Retainone of four remaining options; last two require factory prefitting.

          - Exposed Vertical and Top Edges:  Same species as faces or a compatible species.

Retainone of five options in first subparagraph below.

          - Core:  Either glued wood stave or structural composite lumber.

Retainone of first two options in subparagraph above or retain first subparagraph below.  Third option above applies to some five-ply doors.  Glued-wood-stave core is only available with bonded construction and nonglued-wood-stave core is only available with nonbonded construction.

          - Construction:  Five plies, either bonded or nonbonded construction. Rabbet Top required for corridor door only.

Delete subparagraph below if WDMA I.S.1-A is not referenced or if performance grades are specified in "Door Construction, General" Article.

          - WDMA I.S.1-A Performance Grade:  Extra Heavy Duty.

Retain one or more of three paragraphs below if light openings are required.

      - FABRICATION

Delete first paragraph below if no doors are required to be factory fitted.  Retain paragraph and revise to indicate exceptions if only some doors are required to be factory fitted.  Plastic-laminate-edged and factory-finished doors must be factory fitted and machined.  Fire-rated and plastic-laminate-faced doors with wood edges should also be factory fitted and machined.  Factory fitting and machining for other doors are optional.  See Evaluations.

Standard fitting may be inadequate for doors 2-1/2 inches (64 mm) thick or more or for doors exposed to wide changes in humidity and temperature.

        - Factory fit doors to suit frame-opening sizes indicated.  Comply with clearance requirements of referenced quality standard for fitting unless otherwise indicated.

          - Comply with requirements in NFPA 80 for fire-rated doors.

Delete first paragraph below if no doors are required to be factory machined.  Retain paragraph and revise to indicate exceptions if only some doors are required to be factory machined.  See Evaluations.

        - Factory machine doors for hardware that is not surface applied.  Locate hardware to comply with DHI-WDHS-3.  Comply with final hardware schedules, door frame Shop Drawings, DHI A115-W series standards, and hardware templates.

Retain first subparagraph below for metal frames for wood doors.

          - Coordinate with hardware mortises in metal frames to verify dimensions and alignment before factory machining.

Retain subparagraph below with pairs of factory-fitted, fire-rated doors where astragals, etc., are required.

Retain first paragraph below if applicable.  Indicate here or on Drawings if doors and transoms are rabbeted.  Verify that transom sizes and attachment methods comply with fire-protection ratings if fire-rated doors with transoms are used.

Usually retain paragraph below to provide additional weather resistance.

      - FACTORY FINISHING

Retain this article if factory finishing is required.  Factory finishing can be used to help comply with LEED-NC or LEED-CI Credit EQ 4.2, which limits VOC content of paints and coatings used within building.  Factory finishing also has other advantages.  See Evaluations.

        - General:  Comply with referenced quality standard for factory finishing.  Complete fabrication, including fitting doors for openings and machining for hardware that is not surface applied, before finishing.

          - Finish faces, all four edges, edges of cutouts, and mortises.  Stains and fillers may be omitted on bottom edges, edges of cutouts, and mortises.

Retainone of first three paragraphs below.  Revise if finishing is performed at another location such as a woodworking shop.

        - Finish doors at factory that are indicated to receive transparent finish.  Field finish doors indicated to receive opaque finish.

Two paragraphs below are examples only; revise to suit Project.  Verify availability with manufacturers selected.  Caution:  Finish systems can vary among manufacturers.  Require Samples for verification.

        - Transparent Finish:

Usually retainsame grade for finish as specified for doors.

          - Grade:  Premium.

Retain one of three "Finish" subparagraphs below and one or more options in subparagraph ror insert another option.  Before specifying, verify availability of finishes with manufacturers selected.

          - Finish:  WDMA TR-6 catalyzed polyurethane.

          - Staining:  As selected by Contracting Officer from manufacturer's full range.

Retainone of three options in subparagraph above and usually one of three options in first subparagraph below.  Some door manufacturers will not provide filled finish because filling is best done by hand, which cannot be done on a finishing line; instead, some will offer semifilled finish as described below.  Delete below if only closed-grain wood species are used.

          - Effect:  Open-grain finish.

Retainone of two options in subparagraph below or revise to suit Project.

          - Sheen:  Satin.

- EXECUTION

      - EXAMINATION

        - Examine doors and installed door frames before hanging doors.

          - Verify that frames comply with indicated requirements for type, size, location, and swing characteristics and have been installed with level heads and plumb jambs.

          - Reject doors with defects.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION

        - Hardware:  For installation, see Division 8 Section "Door Hardware."

        - Installation Instructions:  Install doors to comply with manufacturer's written instructions and the referenced quality standard, and as indicated.

Retain subparagraph below for fire-rated doors.

Retain first paragraph below if all doors are not factory fitted.  Factory fitting of fire-rated doors is preferred to job fitting because of limitations on trimming narrower stiles and rails.

        - Job-Fitted Doors:  Align and fit doors in frames with uniform clearances and bevels as indicated below; do not trim stiles and rails in excess of limits set by manufacturer or permitted for fire-rated doors.  Machine doors for hardware.  Seal edges of doors, edges of cutouts, and mortises after fitting and machining.

          - Clearances:  Provide 1/8 inch (3.2 mm) at heads, jambs, and between pairs of doors.  Provide 1/8 inch (3.2 mm) from bottom of door to top of decorative floor finish or covering unless otherwise indicated.  Where threshold is shown or scheduled, provide 1/4 inch (6.4 mm) from bottom of door to top of threshold unless otherwise indicated.

Retain first subparagraph below for fire-rated doors or if doors are not factory fitted.

        - Factory-Fitted Doors:  Align in frames for uniform clearance at each edge.

        - Factory-Finished Doors:  Restore finish before installation if fitting or machining is required at Project site.

      - ADJUSTING

        - Operation:  Rehang or replace doors that do not swing or operate freely.

        - Finished Doors:  Replace doors that are damaged or that do not comply with requirements.  Doors may be repaired or refinished if work complies with requirements and shows no evidence of repair or refinishing.

END OF SECTION 081416