Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 099123 - INTERIOR PAINTING

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

        - Refer to specification section “Cutting and Patching” for patching requirements.

      - SUMMARY

        - This Section includes surface preparation and the application of paint systems on the following interior substrates:

Adjust list below to suit Project.

          - Steel.

          - Gypsum board.

      - SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Samples for Initial Selection:  For each type of topcoat product indicated.

Delete paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph and subparagraphs below with or without above.

        - Product List:  For each product indicated, include the following:

          - Cross-reference to paint system and locations of application areas.  Use same designations indicated on Drawings and in schedules.

See "Writing Guide" Article in the Evaluations in Division 09 Section "Painting" for discussion of subparagraph below.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.2; coordinate with requirements selected in Part 2 for paints and coatings.  Retain option for LEED-CI.

        - Product Data:

          - For paints, including printed statement of VOC content and chemical components.

      - QUALITY ASSURANCE

        - MPI Standards:

          - Products:  Complying with MPI standards indicated and listed in "MPI Approved Products List."

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise subparagraph below and paint systems specified in Part 3.

          - Preparation and Workmanship:  Comply with requirements in "MPI Architectural Painting Specification Manual" for products and paint systems indicated.

Delete paragraph and subparagraphs below if not required.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F.

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

If necessary, add special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

      - PROJECT CONDITIONS

        - Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F.

        - Do not apply paints when relative humidity exceeds 85 percent; at temperatures less than 5 deg F above the dew point; or to damp or wet surfaces.

      - EXTRA MATERIALS

Extra materials may not be allowed for publicly funded projects.

        - Furnish extra materials described below that are from same production run (batch mix) as materials applied and that are packaged for storage and identified with labels describing contents.

Retain subparagraph below for projects that require only limited quantities of extra materials.  If necessary, replace percentage with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Quantity:  Furnish an additional 5 percent, but not less than 1 gal. of each material and color applied.

To efficiently edit Part 2, first edit the Interior Painting Schedule in Part 3; then retain, delete, and insert appropriate products in Part 2 to correspond with paint systems specified in the Interior Painting Schedule.

- PRODUCTS

"Manufacturers" Article lists manufacturers with MPI-approved products for MPI paint categories included in the Section Text.  The list was current when this Section was updated; see current "MPI Approved Products List" at www.paintinfo.com for updated lists of manufacturers.

If preferred, delete Article below and insert product names under each paint category specified in subsequent articles.  See lists of products currently approved by MPI in its "MPI Approved Products List," which is easily reached via the electronic version of the Supporting Documents (accessed via MASTERWORKS pull-down menu).  See "Writing Guide" Article in the Evaluations in Division 09 Section "Painting" for further discussion.

      - MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Painting" for cautions about naming manufacturers and products.  Retain one of two paragraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

        - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

        - Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

          - Benjamin Moore & Co.

For this Section, ChemRex offers only clear concrete floor sealers; if not required, delete ChemRex.

          - Duron, Inc.

          - Valspar Corporation.

For this Section, Kryton Canada Corporation offers only clear concrete floor sealers and stains; if not required, delete Kryton.

      - PAINT, GENERAL

        - Material Compatibility:

Systems could fail if paints used for individual coats are incompatible.  MPI's paint systems match primers and topcoats and take compatibility into consideration.

          - Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each coat in a paint system, provide products recommended in writing by manufacturers of topcoat for use in paint system and on substrate indicated.

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.2; coordinate with products selected.  If retaining, consider deleting "VOC Content" subparagraph from each paint type paragraph retained in subsequent articles to avoid the appearance of conflicting requirements.  For names of products that comply, see products listed as complying with LEED requirements for VOCs on "MPI Approved Products List" (available at www.paintinfo.com).

        - VOC Content of Field-Applied Interior Paints and Coatings:  Provide products that comply with the following limits for VOC content, exclusive of colorants added to a tint base, when calculated according to 40 CFR 59, Subpart D (EPA Method 24); these requirements do not apply to paints and coatings that are applied in a fabrication or finishing shop:

First six subparagraphs below apply to LEED-NC.

          - Nonflat Paints, Coatings, and Primers:  VOC content of not more than 150 g/L.

Ten subparagraphs below apply to LEED-CI.

          - Nonflat Topcoat Paints:  VOC content of not more than 150 g/L.

          - Primers, Sealers, and Undercoaters:  VOC content of not more than 200 g/L.

Verify that three subparagraphs below are acceptable for LEED-CI before retaining.

Retain first paragraph below if low-emitting materials are required for LEED-CI Credit EQ 4.2; coordinate with products selected.

        - Chemical Components of Field-Applied Interior Paints and Coatings:  Provide topcoat paints and anti-corrosive and anti-rust paints applied to ferrous metals that comply with the following chemical restrictions; these requirements do not apply to paints and coatings that are applied in a fabrication or finishing shop:

          - Aromatic Compounds:  Paints and coatings shall not contain more than 1.0 percent by weight of total aromatic compounds (hydrocarbon compounds containing one or more benzene rings).

          - Restricted Components:  Paints and coatings shall not contain any of the following:

            - Acrolein.

            - Acrylonitrile.

            - Antimony.

            - Benzene.

            - Butyl benzyl phthalate.

            - Cadmium.

            - Di (2-ethylhexyl) phthalate.

            - Di-n-butyl phthalate.

            - Di-n-octyl phthalate.

            - 1,2-dichlorobenzene.

            - Diethyl phthalate.

            - Dimethyl phthalate.

            - Ethylbenzene.

            - Formaldehyde.

            - Hexavalent chromium.

            - Isophorone.

            - Lead.

            - Mercury.

            - Methyl ethyl ketone.

            - Methyl isobutyl ketone.

            - Methylene chloride.

            - Naphthalene.

            - Toluene (methylbenzene).

            - 1,1,1-trichloroethane.

            - Vinyl chloride.

        - Colors:  As selected by Contracting Officer from manufacturer's full range, including custom colors.

Paints in subsequent articles are specified by reference to MPI paint categories.  Retaining requirements for VOC content or Environmental Performance Rating (EPR) further limits product selection; coordinate selections with products of manufacturers retained in "Manufacturers" Article.

      - PRIMERS/SEALERS

        - Interior Latex Primer/Sealer:

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

          - VOC Content:  E Range of E2.

          - Environmental Performance Rating:  EPR 2.

      - METAL PRIMERS

        - Quick-Drying Alkyd Metal Primer:

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

          - VOC Content:  E Range of E2.

      - LATEX PAINTS

        - Interior Latex (Waterborne Eggshell Interior Paint):  (Gloss as indicated in schedule).

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

          - VOC Content:  E Range of E3.

          - Environmental Performance Rating:  EPR 3.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of work.

        - Maximum Moisture Content of Substrates:  When measured with an electronic moisture meter as follows:

Percentages in five subparagraphs below are based on "MPI Architectural Painting Specification Manual."

          - Gypsum Board:  12 percent.

        - Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers.

        - Begin coating application only after unsatisfactory conditions have been corrected and surfaces are dry.

          - Beginning coating application constitutes Contractor's acceptance of substrates and conditions.

      - PREPARATION

        - Protect all adjacent interior surfaces and areas, rating and instruction labels on doors, frames, equipment, piping, etc., from painting operations and damage by drop cloths, shields, masking, templates, or other suitable protective means and make good any damage caused by failure to provide such protection.

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Interior Painting Schedule.

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates indicated.

        - Remove plates, machined surfaces, and similar items already in place that are not to be painted.  If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed.  Remove surface-applied protection if any.

          - Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

        - Clean substrates of substances that could impair bond of paints, including dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

          - Remove incompatible primers and reprime substrate with compatible primers as required to produce paint systems indicated.

Delete paragraph below if primers are shop applied and will not be removed in the field.

Galvanized-metal substrates should not be chromate passivated (commercially known as "bonderized") if primers are field applied.  If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Gypsum Board Substrates:  Sand all gypsum board substrates to a level 4 finish.  Patch and repair walls with drywall compound patch.  Resand patched areas to assure seamless smooth finish.  Do not begin paint application until substrate is dry and sanded smooth to a level 4 finish.

      - APPLICATION

        - Apply primer and paints according to manufacturer's written instructions.

          - Prime all surfaces scheduled to receive paint per manufacturer’s recommendations.

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

          - Use applicators and techniques suited for primer, paint and substrate indicated.

          - Prime and paint surfaces behind movable equipment and furniture same as similar exposed surfaces.  Before final installation, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

          - Prime and paint front and backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

If tinting is not required, delete first paragraph below.  Different tints will show through as topcoat erodes.

        - Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied.  Tint undercoats to match color of topcoat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

        - Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections.  Cut in sharp lines and color breaks.

Paragraph and subparagraphs below are examples of painting requirements for mechanical and electrical work.  Revise to suit Project.

      - FIELD QUALITY CONTROL

Retain this Article for large projects or critical coatings where additional control is desired.  Delete if tests are not required.

        - Testing of Paint Materials:  Owner reserves the right to invoke the following procedure at any time and as often as Owner deems necessary during the period when paints are being applied:

          - Owner will engage the services of a qualified testing agency to sample paint materials being used.  Samples of material delivered to Project site will be taken, identified, sealed, and certified in presence of Contractor.

          - Testing agency will perform tests for compliance with product requirements.

          - Owner may direct Contractor to stop applying paints if test results show materials being used do not comply with product requirements.  Contractor shall remove noncomplying-paint materials from Project site, pay for testing, and repaint surfaces painted with rejected materials.  Contractor will be required to remove rejected materials from previously painted surfaces if, on repainting with complying materials, the two paints are incompatible.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing paint application, clean spattered surfaces.  Remove spattered paints by washing, scraping, or other methods.  Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from paint application.  Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

To efficiently edit the Section Text, first edit the Interior Painting Schedule below; then retain, delete, and insert appropriate products in Part 2 to correspond with paint systems specified in the schedule.

      - INTERIOR PAINTING SCHEDULE

Paint systems in this Article are based on "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").  For renovation projects, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

Coordinate substrates and paint systems retained in this Article with products retained in Part 2.

For areas subject to wetting, consider inserting epoxy system, MPI INT 4.2G; see Division 09 Section "High-Performance Coatings"  for system description and products.

        - Steel Substrates:

          - Latex Over Alkyd Primer System:

            - Prime Coat:  Alkyd anticorrosive metal primer.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

            - Intermediate Coat:  Interior latex matching topcoat.

            - Topcoat:  Interior latex (semigloss).

Galvanized-metal substrates should not be chromate passivated (commercially known as "bonderized") if primers are field applied.  If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

        - Gypsum Board Substrates:

          - Latex System:

For a Premium Grade system, select primer/sealer option in subparagraph below.

            - Prime Coat:  Interior latex primer/sealer.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

            - Intermediate Coat:  Interior latex matching topcoat.

            - Topcoat:  Interior latex (waterborne eggshell interior paint).

Delete system in subparagraph and associated subparagraphs below if high-performance architectural latex systems are specified in Division 09 Section "High-Performance Coatings."  They are recommended for use in high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

END OF SECTION 099123