SECTION 02510

BITUMINOUS CONCRETE PAVING

PART 1   GENERAL

1.01	WORK INCLUDED

A.	Bituminous concrete paving for roads, parking areas, driveways, walkways, and associated preparatory work, including overlay of roads established under Contract 2.

B.	Gravel subbase and base courses.

C.	Final grading of subbase and base courses.

D.	Installation of subbase, base binder course.

1.02	REFERENCE STANDARDS

A.	State of Maine, Department of Transportation, for Highways and Bridges, April 1995, including the latest revisions of adopted Supplemental Specifications.

1.03	SUBMITTALS

A.	Submit certification prepared by manufacturer certifying that the component materials and finished product to be delivered to site conforms to job mix data, MDOT Standard Specifications Division 300, Division 400, and Division 700.  Submittals should be in conformance to Section 01330 - Submittals.

PART 2   PRODUCTS

2.01	MATERIALS

A.	Subbase and base aggregate: Material shall be in accordance with MDOT Section 703.06, described in specification Section 02225 - Excavating, Backfilling, and Compacting.

B.	Hot Bituminous Pavement, Grading B.

C.	Hot Bituminous Pavement, Grading C.

D.	Hot Bituminous Pavement, Grading D.

PART 3   EXECUTION

3.01	GENERAL

A.	The placement of subbase and base courses shall be in accordance with MDOT Standard Specification, Section 304.03.  The number and thickness of each course shall conform to the drawings.

B.	Bituminous concrete material shall be placed in accordance with MDOT Standard Specification 401.07 through and including 401.18.  The quality assurance of all pavement items shall be agreed upon by Contractor and ARCHITECT prior to any placement.

C.	The number of paving courses and the thickness of each course shall conform to the Drawings or as directed by the ARCHITECT.

3.02	COMPACTION TESTING

A.	Compaction testing for base(s) and pavement will be performed in accordance with MDOT Standard Specification Section 304.04 and 401.

3.03	TEMPORARY TRENCH PATCH

A.	Temporary trench patch shall be placed upon a properly installed subbase, as specified herein, in all trenches within existing pavement areas.

B.	Temporary trench patch shall be binder course mix, minimum 2 inches thick.

C.	Temporary trench patch shall be placed within 5 days of backfilling.  The CONTRACTOR shall schedule his paving operations so that temporary pavement is installed prior to the end of each work week.

D.	All edges of the adjacent pavements shall be trimmed back as necessary to sound pavement and to neat straight lines and cleaned to provide a firm, regular and clean surface to bond the new pavement.  All edges shall be coated with an emulsified asphalt to improve the bond between the old and new pavement.  Care shall be exercised not to adversely alter original street drainage.

E.	The CONTRACTOR shall maintain temporary trench patch under this Contract and shall promptly refill and repave areas which have settled or are otherwise unsatisfactory for traffic until the temporary trench patch is removed, or until the temporary trench patch is resurfaced, whichever occurs first.

3.04	PERMANENT TRENCH PATCH

A.	The CONTRACTOR shall remove temporary trench patch, regrade subbase and install permanent trench patch as specified upon authorization by the ARCHITECT.

Temporary trench patch shall not be removed sooner than 90 days after installation unless otherwise authorized by the ARCHITECT.

B.	All edges of the adjacent pavements shall be trimmed back a minimum of 6 inches or to sound pavement and to neat straight lines and cleaned to provide a firm, regular and clean surface to bond the new pavement prior to placement of pavement.  All edges shall be coated with an emulsified asphalt to improve the bond between the old and new pavement.  Care shall be exercised not to adversely alter original street drainage.

C.	Permanent trench patch shall be a minimum of 2 inches of binder course mix and a minimum of 1 inch of top course mix in two separate and compacted layers for a minimum total of 3 inches or as shown on the Drawings.

D.	The final pavement shall butt or overlap the existing pavement along all edges providing a smooth uniform joint.

E.	The CONTRACTOR shall maintain permanent pavement under this Contract during the contract guarantee period and shall promptly refill and repave areas which have settled or are otherwise unsatisfactory for traffic.

3.05	SURFACE TOLERANCE

A.	The completed surface of the base and subbase courses shall be shaped and maintained to a tolerance, above and below the required cross sectional shape of 3/8 inch.

B.	The completed surface of the pavement courses shall be shaped and finished within the tolerances of MDOT Specification, 401.111.  The Contractor shall provide the required straightedge for the ARCHITECT's use.

END OF SECTION